Supplementary Information

Preparation and Study of Straw Porous Biochar with Aromatic Ring Structure for Adsorption Performance and Mechanism towards TNT Red Water

# Nengsheng Liu, Jiangzhou Qin, Xinrui Ge, Yanyu Lu, Jihan Zhang, Quanlin Zhao, and Zhengfang Ye

# The Key Laboratory of Water and Sediment Sciences, Ministry of Education, College of Environmental Sciences and Engineering, Peking University, Beijing, 100871, P. R. China

# Number of pages: 15

# Number of tables: 4

# Number of figures: 8

Table of Contents

| Index | Caption | Page |
| --- | --- | --- |
| Test S1. | Details of chemicals. | S3 |
| Text S2. | Details of characterization instruments. | S3 |
| Text S3. | Details of kinetics curve fitting. | S4 |
| Table S1. | Details of compounds in TNT red water. | S5-S6 |
| Table S2. | Element information of Spectrum 7. | S7 |
| Table S3. | Element information of Spectrum 8. | S7 |
| Table S4. | Element information of Spectrum 9. | S7 |
| Fig. S1. | Crushed rice straw and TNT red water. | S8 |
| Fig. S2. | High resolution XPS spectra of O 1 s. | S9 |
| Fig. S3. | High resolution XPS spectra of N 1 s. | S10 |
| Fig. S4. | EDS spectra of SBC. | S11 |
| Fig. S5. | EDS spectra of element information on Spectrum 7. | S12 |
| Fig. S6. | EDS spectra of element information on Spectrum 8. | S13 |
| Fig. S7. | EDS spectra of element information on Spectrum 9. | S14 |
| Fig. S8. | Zeta potential of straw-derived biochar at different pH. | S15 |

Text S1

The initial COD of TNT red water is 50,000-53,000mg /L, and the pH range is between 6.5 and 7.4. (NH4)2HPO4, NaOH, HCl, were purchased from Tongguang Chemical Co., Ltd.(Beijing, China). KOH, acetone and other chemicals with analytical grade used in this study were from Sigma-Aldrich chemical company.

Text S2

Scanning electron microscopy (SEM, Gemini 300, ZEISS, Germany) was employed to determine the surface morphology of synthesized biochar. Energy Dispersive X-ray Spectroscopy (EDS, INCA X Act, Oxford) was used to determine elemental information on synthesized biochar surface. Fourier transformation infrared (FT-IR, Nicolet NEXUS 670, Thermo Fisher, USA) spectroscopy spectra was obtained to further confirm the organic structure and functional groups on the surface of biochar. The BET analysis was obtained from N2 adsorption-desorption isotherms using Porosimetry System (Quantachrome, Autosorb-iQ). X-ray photoelectron spectroscopy (XPS, ESCALAB 250xi, Jiaodahongrui Analytical Ltd., Shanghai, CN) were utilized to determine the elemental quantitative results and chemical state of P after pretreatment by (NH4)2HPO4. A zeta potential analyzer (Brookhaven Instruments ZetaPlus) was used to analyze the charge of the biochar. The pH values of the solutions were determined by an acidity meter (PHBJ-261L). The chemical oxygen demand (COD) was measured by HASH (DR 200). The organic components of TNT red water were measured using a High-Resolution Liquid Chromatography-Mass Spectrometry (LC-MS, Thermo Fisher, USA) system.

Text S3

To better describe the adsorption of COD of TNT red water, the kinetics experimental data were fitted with four kinetic models (pseudo-first order kinetic model, pseudo-second order kinetic model, Elovich kinetic model, and intraparticle diffusion model).

The fitted equation are as follows:

Pseudo-first order kinetic model: Y=3.92267-0.04679x

Pseudo-second order kinetic model: Y=0.00856+0.00707x

Elovich kinetic model: Y=80.05591+12.89518x

Intraparticle diffusion model: Y=19.38558+49.20495x; Y=117.93382+2.29331x.

Table S1. The organic components in TNT red water.

|  | Molecular Formula | Name | Structure |
| --- | --- | --- | --- |
| 1 | C6H3N3O7 | 2,4,6-Trinitrophenol |  |
| 2 | C6H3N3O8 | 2,4,6-TRINITRORESORCINOL |  |
| 3 | C6H4N2O4 | 1,3-Dinitrobenzene |  |
| 4 | C6H4N2O5 | 2,4-Dinitrophenol |  |
| 5 | C6H4N2O7S | 2,4-Dinitrobenzenesulfonic acid hydrate |  |
| 6 | C6H4N2O8S | 4-Hydroxy-3,5-dinitrobenzenesulphonic acid |  |
| 7 | C6H4N4O6 | 2,3,4,6-Tetranitroaniline |  |
| 8 | C6H5N3O4 | 2,4-Dinitroaniline |  |
| 9 | C6H5N3O7S | 4-Amino-3,5-dinitrobenzenesulfonic acid |  |
| 10 | C7H3N3O9 | 3-Hydroxy-2,4,6-trinitrobenzoic acid |  |
| 11 | C7H4N2O7 | 3,5-Dinitrosalicylic acid |  |
| 12 | C7H4N2O9S | 3,5-Dinitro-4-sulfobenzoic acid |  |
| 13 | C7H5N3O6 | 2,4,6-Trinitrotoluene |  |
| 14 | C7H5N3O7 | 5-Methoxy-1,2,3-trinitrobenzene |  |
| 15 | C7H5N3O9S | 2,4,6-Trinitrophenol |  |
| 16 | C7H6N2O5 | 4,6-Dinitro-O-cresol |  |
| 17 | C7H6N2O7S | 2,6-Dinitrotoluene-4-sulfonic acid |  |
| 18 | C7H6N2O7S | 2,4-Dinitrotoluene-6-sulfonic acid |  |
| 19 | C7H7NO6S | 3-amino-2-hydroxy-5-sulfobenzoic acid |  |
| 20 | C7H7N3O4 | 2-Amino-4,6-dinitrotoluene |  |

Table S2. Element information of Spectrum 7.

| Element | Apparent Concentration | Wt% | Wt% Sigma |
| --- | --- | --- | --- |
| C | 188.64 | 88.41 | 0.20 |
| N | 0.00 | 0.00 | 0.63 |
| O | 13.60 | 11.51 | 0.20 |
| P | 0.29 | 0.08 | 0.03 |
| Total |  | 100 |  |

Table S3. Element information of Spectrum 8.

| Element | Apparent Concentration | Wt% | Wt% Sigma |
| --- | --- | --- | --- |
| C | 171.18 | 82.07 | 0.59 |
| N | 0.70 | 0.59 | 0.66 |
| O | 22.69 | 17.22 | 0.24 |
| P | 0.41 | 0.11 | 0.03 |
| Total |  | 100 |  |

Table S4. Element information of Spectrum 9.

| Element | Apparent Concentration | Wt% | Wt% Sigma |
| --- | --- | --- | --- |
| C | 170.24 | 86.02 | 0.22 |
| N | 0.00 | 0.00 | 0.71 |
| O | 16.09 | 13.84 | 0.22 |
| P | 0.46 | 0.14 | 0.03 |
| Total |  | 100 |  |

Fig. S1. (a) crushed rice straw; (b) TNT red water, on the far left is the initial TNT red water (COD: ~53000 mg/L), diluted 5 times from left to right.

Fig. S2. High resolution XPS spectra of O 1 s.

Fig. S3. High resolution XPS spectra of N 1 s.

Fig. S4. EDS spectra of SBC.

Fig. S5. EDS spectra of element information on Spectrum 7.

Fig. S6. EDS spectra of element information on Spectrum 8.

Fig. S7. EDS spectra of element information on Spectrum 9.

Fig. S8. Zeta potential of straw-derived biochar at different pH values.

* Corresponding author: E-mail address: zhengfangye@163.com