Supporting Information

3D toilet-paper based carbon fiber for excellent solar assisted steam generation performance

Xidong Suo1, *, Yao Li1, Peiqi Liu1, Yingying Li1, Cuirong Guo1, Jie Yang1, *, Hongtao Qiao1, Sheng Han2, *, Chenqi Liu1, Aiping yin1

Xidong Suo, Yao Li, Peiqi Liu, Yingying Li contributed equally to this work.

Corresponding Author: Xidong Suo, Jie Yang, Sheng Han

Xidong Suo

xidsuo@126.com

Jie Yang

yangjie_10@126.com

Sheng Han

hansheng654321@sina.com

Yao Li

1191871264@qq.com

Peiqi Liu

2249421306@qq.com

Yingying Li

2646335895@qq.com

Cuirong Guo

2923185329@qq.com

Hongtao Qiao

469494248@qq.com

Chenqi Liu

1550525329@qq.com

Aiping yin

Aipingyin1964@163.com

1Department of Chemistry, Xinzhou Normal University, No. 1 Dun Qi Street, Xinzhou, Shan Xi, 034000, China

2School of Chemical and Environmental Engineering, Shanghai Institute of Technology, Shanghai, 201418, China

Keywords: 3D solar steam generation, toilet paper, porous carbon materials, carbon fiber.

Figure S1. SEM images of CTP.

Figure S2. SEM images of CFTP based evaporator.

Figure S3. SEM images of CFTP based evaporator.

Figure S4. N2 adsorption–desorption curves of TP based evaporator.

Table S1. BET surface area of the samples.

| Samples | CTP | CFTP | Na-CFTP | K-CFTP | P-CFTP | Cu-CFTP | Zn-CFTP |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Surface area (m2 g-1) | 178.8 | 91.9 | 1164.1 | 1.9 | 7.6 | 1.3 | 1.8 |

Figure S5. UV–vis-NIR absorption curve of TP based evaporators.

Figure S6. Water contact angle for K-CFTP, P-CFTP, Cu-CFTP and Zn-CFTP.

Figure S7. Water transporting performance of different height Na-CFTP based evaporator.