Supporting Information

for

Photocatalytic degradation of polyethylene and polystyrene microplastics by α-Fe2O3/g-C3N4

Chao Chaia, Hao Liangb, Ruike Yaoa, Fangli Wanga, Ningning Songa, Juan Wua, Yan Lic,*

Corresponding author at: Institute of Agricultural Resource and Environment, Shandong Academy of Agricultural Sciences, Jinan 250100, China

E-mail address: nkyliyan@126.com

a School of Resources and Environment, Qingdao Engineering Research Center for Rural Environment, Qingdao Agricultural University, Qingdao, 266109, China

b School of Engineering, China Pharmaceutical University, Nanjing 210009, China

c Institute of Agricultural Resource and Environment, Shandong Academy of Agricultural Sciences, Jinan 250100, China

- Characterization of α-Fe2O3/g-C3N4

The SEM image of α-Fe2O3/g-C3N4 composite in Fig. S1a indicates that the α-Fe2O3 are decorated on the g-C3N4 substrate, which results in the formation of a heterogeneous interface. The existence of C, N, O and Fe elements in the α-Fe2O3/g-C3N4 composite is proved by the EDX pattern (Fig. 1c). Meanwhile, the characteristic morphology of α-Fe2O3 in the TEM images of the α-Fe2O3/g-C3N4 composite (Fig. 1b) demonstrates the existence of α-Fe2O3 in the α-Fe2O3/g-C3N4 composite.

In order to reveal the crystalline and phase structures of the prepared α-Fe2O3/g-C3N4 composites, the XRD pattern of the α-Fe2O3/g-C3N4 composites was measured and shown in Fig. 1d. For α-Fe2O3/g-C3N4, the two diffraction peaks at 12.91 and 27.53 are index to (100) and (002) planes of g-C3N4. The diffraction peaks of the derived α-Fe2O3 are corresponding with that of typical hematite (JCPDS No. 33-0664). Only reflection peaks of the corresponding components can be seen in the XRD patterns of the α-Fe2O3/g-C3N4 composite. No other impurity peaks can be detected, which indicates the final synthetic substance with high purity.

Fig. S1. SEM image (a) TEM image (b) EDX (c) XRD pattern of α-Fe2O3/g-C3N4 composite.