Supplementary Information

Table S1 The fractional atomic coordinates in Cmcm coordinate system and the splitting of the Wyckoff positions under the change of symmetry of Na2SO4 high-temperature phase (P63/mmc, Cmcm). Based on the data of Rasmussen et al., 1996.

| P63/mmc |  |  |  |  | Cmcm |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | WP | x | y | z | Atom | WP | x | y | z |
| Na2 | 2a | 0 | 0.15 | 0.25 | Na1 | 4c | 0 | 0.1830 | 0.25 |
| Na1 | 2d | 0 | 0.5 | 0 | Na2 | 4b | 0 | 0.5 | 0 |
| S1 | 2c | 0 | 0.85 | 0.25 | S1 | 4c | 0 | 0.8483 | 0.25 |
| O2 | 12k | 0.3015 | 0.4355 | 0.25 | O1 | 8g | 0.2823 | 0.4385 | 0.25 |
| O1 | 12j | 0 | 0.2462 | 0.4059 | O2 | 8f | 0 | 0.2432 | 0.5684 |