# Adsorption of pyrolysis oil model compound (phenol) with plasma-modified hydro-chars and mechanism exploration

Qing An a,b, Dezhen Chen a,b*, Yuzhen Tanga,b, Yuyan Hu a,b, Yuheng Feng a,b, Kezhen Qian a,b, Lijie Yin a,b

a Thermal and Environmental Engineering Institute, Mechanical Engineering College, Tongji University, Shanghai 201800, China

b Shanghai Engineering Research Center of Multi-source Solid Wastes Co-processing and Energy Utilization

* Corresponding author.

E-mail address: chendezhen@tongji.edu.cn (D, Chen).

Table S1. The characteristics of raw materials and the prepared hydro-char samples

| Sample | Proximate analysis/ (wt%, ad 1) |  |  | Ultimate analysis/ (wt%, db 2) |  |  |  |  | Atomic ratio |  | BET surface area (m2g-1) | Pore volume (cm3g1) | Average pore size (nm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ash (wt %) | VM 3 | FC 4 | N | C | H | S | O | H/C | O/C |  |  |  |
| SS | 45.43 | 48.01 | 6.56 | 4.09 | 25.12 | 4.34 | 0.54 | 20.47 | 2.07 | 0.61 | 4.276 | 0.024 | 20.95 |
| WS | 10.37 | 69.53 | 20.1 | 0.31 | 59.45 | 2.81 | 0.31 | 26.75 | 0.57 | 0.34 | — | — | — |
| HC | 13.57 | 20.92 | 65.51 | 2.34 | 33.48 | 3.19 | 0.07 | 47.35 | 1.14 | 1.06 | 120.24 | 0.10 | 3.45 |
| HC-NH3-P-25 | 9.64 | 11.88 | 78.48 | 2.59 | 57.41 | 2.26 | 0.03 | 28.07 | 0.47 | 0.37 | 178.43 | 0.22 | 6.36 |
| HC-NH3-P-500 | 6.13 | 5.58 | 88.29 | 4.72 | 63.49 | 1.91 | 0.01 | 23.74 | 0.36 | 0.28 | 374.14 | 0.04 | 1.91 |

1ad: air-dry basis; 2db: dry basis; 3VM: volatile matter; 4FC: fixed carbon

Figure. S1 Sorption isotherms of phenol onto HC, HC-NH3-P-25 and HC-NH3-P-500 and comparision between experimental and the modeling results.