Interactions between C-steel and blended-cement in concrete under radwaste repository conditions at 80 °C

Margit Fabian1*, Otto Czompoly1, Istvan Tolnai1, Laurent De Windt2

1Centre for Energy Research, Konkoly Thege st 29-33, 1121 Budapest, Hungary, fabian.margit@ek-cer.hu

2Mines Paris, PSL University, Centre for geosciences and geoengineering, 77300 Fontainebleau, France

Supplementary information

Fig. SI-1 Modeling grid of the experimental cell in cylindrical symmetry.

Fig. SI-2 Effect of the diffusion coefficient on the time evolution of the non-reactive Na+ concentration; the experimental data of the reservoir are added (blue circles) for the sake of comparison.

Table SI-1. Oxide composition of the clinker and slag considered in the modeling

| Composition [wt. %] | Clinker | Slag |
| --- | --- | --- |
| SiO2 | 21.3 | 37.4 |
| Al2O3 | 5.0 | 7.3 |
| Fe2O3 | 3.4 | 1.2 |
| CaO | 64.8 | 43.9 |
| MgO | 2.1 | 5.7 |
| K2O | 1.0 | 0.56 |
| Na2O | 0.11 | 0.55 |
| Cl | 0.03 | 0.03 |
| CaSO4 | 2.50 | - |