Supplementary Material

Tea grounds inspiration for a renewable biomass-based carbon aerogel with CMC and PVA reinforcements: Dye adsorption and supercapacitor prospects

Ton That Buu1,2,3, Phan Minh Tu1,2,3, Che Quang Cong1,2,3, Nguyen Duy Hai1,2,3, Dang Thanh Cong Minh1,2,3, Nguyen Thanh Hoai Nam1,2,3, Vo Minh Quan1,3,4, Bo Khanh Ngoc1,3,4, Le Gia Han1,2,3, Huynh Ky Phuong Ha1,2,3, Nguyen Truong Son1,2,3, and Nguyen Huu Hieu1,2,3*

1VNU-HCM, Key Laboratory of Chemical Engineering and Petroleum Processing (Key CEPP Lab),

Ho Chi Minh City University of Technology (HCMUT), 268 Ly Thuong Kiet Street, District 10,

Ho Chi Minh City, Vietnam

2Faculty of Chemical Engineering, Ho Chi Minh City University of Technology (HCMUT),

268 Ly Thuong Kiet Street, District 10, Ho Chi Minh City, Vietnam
3Vietnam National University Ho Chi Minh City (VNU), Linh Trung Ward, Thu Duc City, Vietnam

4Faculty of Chemistry, University of Science (HCMUS), 227 Nguyen Van Cu Street, District 5,

Ho Chi Minh City, Vietnam

*Corresponding author, email: nhhieubk@hcmut.edu.vn

- Results and discussions

| Table 1: PFO and PSO kinetic parameters for RhB dye sorption on TG-CA800 materials |  |  |  |
| --- | --- | --- | --- |
| Pseudo-first-order (PFO) |  |  |  |
| Parameters | Qecal (mg/g) | K1 (min-1) | R2 |
|  | 25.07 | 0.086 | 0.8789 |
| Pseudo-second-order (PSO) |  |  |  |
| Parameters | Qecal (mg/g) | K2 (g/mg.min) | R2 |
|  | 21.29 | 0.010 | 0.9407 |

| Table 2: Isotherm parameters for RhB dye sorption on TG-CA800 materials |  |  |  |
| --- | --- | --- | --- |
| Langmuir |  |  |  |
| Parameters | qmax (mg/g) | KL (L/mg) | R2 |
|  | 45.23 | 0.0502 | 0.9974 |
| Freudnlich |  |  |  |
| Parameters | n | KF [(mg.g-1)/(L.mg-1)1/n] | R2 |
|  | 2.32 | 4.7273 | 0.9045 |
| Temkin |  |  |  |
| Parameters | bT (J/mol) | KT (L/mg) | R2 |
|  | 8.066 | 0.7512 | 0.9825 |