Supplementary material

Silver nanoclusters as label free non-enzymatic fast glucose assay with the fluorescent enhancement signal

Razieh Moosavi, Naader Alizadeh∗

Departmentof Chemistry, Faculty of Basic Sciences, Tarbiat Modares University, P.O. Box 14115-175, Tehran, Iran

*Corresponding author: E-mail address: alizaden@modares.ac.ir

Workflow for literature searching and data mining

To the best of our knowledge, it is the first report for glucose determination without any intermediate by a label free mechanism in a widest response range till now depend on our investigations and based on similar studies (Sabu et al., 2019; Tian et al., 2014; Scognamiglio et al., 2013; Golsanamlou, et al., 2021; Peng, et al., 2022) [1-5].

As shown in Table S1 below, we collected glucose sensing research papers and extracted characteristics of methods according to the following steps:

a. Literature search with focus on enzymatic/non-enzymatic sensing of glucose by nanoclusters. All articles were searched by the keywords “nanocluster” and “glucose”, using the Scopus web and google scholar.

b. Data extraction: detailed information, including method advantages, enhancement/quenching mechanism, synthesis conditions and simplicities, response time, stability of NCs, limit of detection and linear range, was extracted from research papers for comparison.

In brief enzymatic based glucose sensors have been a challenging task due to their inherent problems of cost, instability and sample pre-treatment. On the other hand, non-enzymatic assays are cost-effective, were discussed by Naikoo et al. in 2021 [6]. As is clear between glucose biosensors, fluorescence technique offers high sensitivity and convenience. Among probes for the detection of glucose have been attempted recently, numerous fluorescent nanomaterial based techniques have been reported in the literature but are limited to the glucose detection range and/or sensitivity, response time, stability and interference effects [1-3, 7].

Here non-enzymatic fluorescence sensing of glucose by easily green synthesized BSA-Ag NCs overcome the main drawback of the existing systems. The comparison to other methods shown all of the sensors used for glucose detection observed before, have considerably narrower range than in this study. In addition, the simplicity of the preparation and direct simply operation in really a wide linear range, besides selectivity toward glucose and fast quantitative determination with highly accurate data makes the BSA-Ag NCs based sensor most preferred than the others.

Moreover, more than ten-fold enhancement of fluorescence intensity of NCs for low level precise glucose determination in this assay, enhances the detection sensitivity and selectivity, making it important to measure glucose upon BSA-Ag NC as an improved sensor. Likewise, some bottleneck like nonstability and pH dependency are limiting points in previous works [8, 9], which are ignorable here.

Table S1. Comparison of nanocluster based literature (enzymatic and non-enzymatic) reported works for glucose

| Nanocluster based spectroscopic sensor | Method conditions | Synthesis conditions: Reducing agent/ stabilizer etc. | Response time/ durability of NCs | LOD mmol L−1 | Linear range mmol L−1 | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Turn-on enzymatic sensor for H2O2 and glucose based on DNA-Ag NCs | Based on the cleavage of ssDNA by •OH and the fluorescence enhancement effect when guanine-rich (G-rich) DNA sequences are in proximity to DNA-silver NCs | Without special steps such as modification, separation, coating, and immobilization, which greatly decreases the operating difficulty. Accessible to numerous labs | 90 min/ Stability NS | 0.0004 | 0 to 3.75 | [10] |
| Polyethyleneimine-capped Ag NCs as a fluorescence quenching enzymatic probe for detection of hydrogen peroxide and glucose | Oxidation of glucose by glucose oxidase was coupled with ﬂuorescence quenching of PEI-Ag NCs by H2O2, and PEI-Ag NCs-based determination of glucose at RT established, too. Lower degree of sample matrix interference | Simple and direct synthesis of polyethyleneimine-capped Ag NCs. The possible reason for the blue emission has been discussed | Within 30 min/ Kept for 30 days | 0.0008 | 0.001 to 0.01 and 0.01 to 1.0 | [11] |
| Enzymatic fluorescent probes based on ovalbumin-stabilized Ag NCs and pH-switchable agglomeration-induced quenching | pH-dependent reversible response attributable to the pH-induced change in the electron-donating ability of the functional groups on the Ag NCs, absorption peak signals | An etching method for generating water-soluble ﬂuorescent Ag NCs. Stable at pH 2.0–14.0 and 20 to 37 °C temperature | 40 min/ Stable for at least 3 months | 0.00001 | 0.005 to 0.17 | [8] |
| Enzymatic OVA-stabilized fluorescent quenching Au NCs glucose sensor | based on the hydrogen peroxide-induced fluorescence quenching principle set at 37 °C and stable at pH 2.0–14.0. | the optimized conditions for OVA-AuNCs synthesis were determined to be incubation in an NaOH solution with OVA/HAuCl4 solution at 80 °C for 5 min | 15 min/ NS stability | 0.001 | 0.005 to 1.0 and 1.0 to 10 | [12] |
| Enzymatic Redox active, photoluminescent Ag NCs templated with oligonucleotides | The reversible emission change was measured and used to detect H2O2, which is a by-product of the reaction of glucose with glucose oxidase. Ag NCs can be reused | Ag NCs were synthesized by templating with oligonucleotides and reducing with NaBH4 | Within 10 min/ Stable for more than two weeks | Not found | 0 to 10 | [9] |
| Non-enzymatic surface enhanced Raman scattering (SERS) with Ag NCs and 2-Thienylboronic acid as linker | Pretreatment need as instrumentation for SERS and Ag NC ﬁlms deposition. Non-invasive detection of glucose in diabetic patients using saliva samples | NS | NS | NS | 0.001 to 0.5 | [13] |
| Non-enzymatic surface-enhanced Raman-mode quantitative glucose sensing in an on-chip microfluidic environment as well as in ex vivo rabbit eyes | SERS instrumentation and liquid phase deposition need. Potent for monitoring continuously changing glucose concentrations at levels observed in the aqueous humor and blood | The fabrication was performed in a two-step process: (1) hydrothermal synthesis of ZnO nanowires and (2) liquid phase deposition of Au nanoparticles on the ZnO NWs | 10 to 30 minutes depending on the glucose concentration/ Stable over a 30-day period | NS | 0.1 to 30 | [14] |
| Non-enzymatic Au cluster colloids emission quenching based glucose sensing | The FL emission spectra of Au cluster were collected at RT. No major interference (but BSA and C-peptide presented as interfering species). | Synthesis by reduction of AuCl4 with NaBH4 in the presence of l-cysteine | Very fast/ Stable for 5 month | 0.25 | 2.5 to 25.0 | [15] |
| Non-enzymatic fluorescent quenching of Ag NCs anchored with 3-aminophenyl boronic acid | Photoluminescence investigation of dilute aqueous Ag NCs-a-APBA colloids at RT. The interference study with the model solution. | Ag NCs-a-APBA have been synthesized and modified sonochemically in presence of sunlight and sonication | Sixty minutes/ NS stability | Claimed in nanomolar level (but NS) | Nanomolar to 1.0 milimolar (nonlinear plot) | [16] |
| Non-enzymatic gold nanoclusters/graphene quantum dots complex-based dual-emitting ratiometric fluorescence probe | Fe3+-sensitive orange-fluorescent gold NCs as the indicator probe. Fe3+-inert blue-fluorescent graphene quantum dots as the reference probe. | BSA and 3-mercaptopropionic acid solution were used and allowed to react at 4 °C, then dialyzed in phosphate buffer solution for 48 h, and then dialyzed in deionized water for 12 h | 15 minutes | 0.18 μmol/L | 1–15 μmol/L | [17] |
| Enzymatic silver nanoclusters as fluorescent probe for detection of hydrogen peroxide and glucose | Sensing platform based on BSA-Ag30NCs coupling with glucose oxidase (GOD) catalytic reaction | BSA-AgNCs with different ratio of Ag/BSA were systematically studied about their fluorescence properties. | 45 minutes | 3.4 μmol/L | 5–180 μmol/L | [18] |
| Enzymatic label-free fluorescent probe for detection of Fe2+ and glucose | AuNCs@C20 integrated with Fenton reaction was designed as ferrous ions and glucose detecting probe | Homocytosine-templated gold NCs AuNCs@C20 with stable blue fluorescence were prepared by a facile one-step synthesized method | 15 minutes / 30 days | 2.3 μmol/L | 10 to 90 μmol/L | [19] |
| Enzymatic ratiometric fluorometric and colorimetric dual-mode sensing of glucose based on gold-platinum bimetallic NCs | The bifunctional Au-Pt NCs-GMP possessed peroxidase-like mimetic activity and stable fluorescence were constructed for a dual-mode glucose assay for the first time | The Au-PtNCs-GMP were synthesized by an improved hydrothermal method. | NS | Fluorescence method 0.01–0.4 | 7 μmol/L | [20] |
|  |  |  |  | Colorimetric method 0.05–0.4 | 11 μmol/L |  |
| Copper nanocluster (Cu23 NC)-based biomimetic system with peroxidase activity utilized as enzymatic sensor | The dual PL response of the Cu23@pepsin-based probe is exploited in designing a ratiometric H2O2 sensor and therefore glucose | Blue luminescent, pepsin-templated Cu NCs were synthesized. The enzymatic activity of Cu23@pepsin is dependent on several physical parameters such as temperature, pH, OPD, and H2O2 concentration | 40 minutes / 15 days | 7.56 μmol/L | 0 to 1 mmol/L | [21] |
| Enzymatic glucose oxidase-anchored gold nanoclusters@ZIF-8 nanocomposites | A capillary-based fluorimetric platform for evaluation of glucose in blood by Gold nanoclusters and glucose oxidase in ZIF-8 Matrix | AuNCs, were synthesized through the biomineralization process, first attached with GOD to yield GOD-AuNCs and then encapsulated into ZIF-8 matrix through the protein-mediated formation of MOFs | 15 minutes / 6 month | 0.30 μmol/L | 5.0 μmol/L to 2.5 mmol/L | [22] |
| Stimuli‐Responsive luminescent copper nanoclusters in alginate and their sensing ability for glucose | Visually observable pH-responsive luminescent materials are fabricated after integrating the gel formation ability of alginate induced by free Ca2+ and the AIE properties of Cu NCs | Cu NCs were synthesized by using GSH as both reduction reagents and ligands to stabilize the as-synthesized clusters | 210 minutes/ 330 min of incubation | 0.32 | 0.1–2.0 | [23] |
| Enzymatic fluorescent quenching and visual assay of H2O2 and glucose based on copper nanoclusters-Ce(III) fluoroprobe | The fluorescent intensities of CuNCs-Ce3+ were selectively quenched by hydrogen peroxide via the redox reaction | CuNCs were synthesized by a simple one-pot chemical reduction method based on glutathione as capping and reducing agents | NS | 2.4 μmol/L | 8–48 μmol/L | [24] |
| Enzymatic aggregation-induced emission of copper NCs triggered by synergistic effect of dual metal ions and the application in the detection of H2O2 and related biomolecules | The method focused on the aggregation-induced emission (AIE) of nanoclusters triggered by metal ions | Cu(NO3)2 aqueous solution was added dropwise into glutathione under vigorous stirring at room temperature for 1 h. The solution pH was adjusted to about 6.0 by adding NaOH aqueous solution | 20 min | 0.37 μmol/L | 0.8 to 50 μmol/L | [25] |
| Bifunctional gold nanoclusters enable enzymatic ratiometric fluorescence nanosensing of hydrogen peroxide and glucose | Ratiometric fluorescent nanosensor was developed for the determination of H2O2 and glucose by integrating peroxidase–like catalytic and fluorescent bifunctional properties of glutathione protected gold nanoclusters (GSH–AuNCs) | In GSH–AuNCs synthesis, the color of the solution changed from yellow to colorless in a few minutes and then turned to light yellow slowly. The absorption peak of HAuCl4 solution at 288 nm disappeared accompanying with a weak shoulder peak emerging at 373 nm | 30 minutes/ 6 month | 20 nmol/L | 0.05–10.0 μmol/L | [26] |
| A ratiometric fluorescence nanoprobe based on copper NCs and graphitic carbon nitride nanosheets using Ce(III) as crosslinking agent and aggregation-induced effect initiator | The ratiometric nanoprobe based on g-C3N4 NSs-Ce3+-CuNCs used to visually detect H2O2 and glucose by naked eyes | glutathione-capped copper NCs and graphitic carbon nitride nanosheets (g-C3N4 NSs) were synthesized by a facile one-pot chemical reduction and directly thermal pyrolysis following ultrasonic exfoliation approaches, respectively | NS | 0.48 μmol/L | 1.6–320 μmol/L | [27] |
| Pd NCs confined in ZIF‑8 matrixes for enzymatic fluorescent detection of glucose and cholesterol | With the addition of glucose or cholesterol oxidase, the Pd@ZIF-8 can be utilized to construct a fluorescent sensor for glucose and cholesterol | Pd NCs were synthesized by using a metal organic framework, zeolitic imidazolate framework-8 (ZIF-8), as a matrix via an impregnation-reaction method | 20 min | 0.10 μmol/L | 15-1000 μmol/L | [28] |
| Enzymatic fluorescence detections of hydrogen peroxide and glucose with polyethyleneimine-capped silver nanoclusters | Fluorescence from Ag NCs could be quenched by reduced glutathione (GSH) through an interaction from its thiol group. As an oxidant, hydrogen peroxide converted GSH into an oxidized form with an elimination of the free thiols, and inhibited the quenching | Ag NCs were synthesized with a one-pot method. After formaldehyde was introduced and stirred product was kept at room temperature in dark for 4 days | 60 minutes | 0.11 μmol/L | 0.8–50 μmol/L | [29] |
| N Non-enzymatic turn on glucose biosensor based on BSA-Ag NCs | Enzyme free fluorescence probe at RT is based on the fluorescence enhancement of BSA-Ag NCs. | Simple one pot synthesis method with green conditions. Clusters were formed after the addition of a BSA in alkaline media of Ag+ ions solution without reductant | Ultra-fast/ Stable for 6 month | 0.031 μmol/L | 0.1 to 8 and 8 to 92 | This work |

NCs: Nanoclusters, NS: Not specified, RT: room temperature

References:

[1] C. Sabu, T. Henna, V. Raphey, K. Nivitha, K. Pramod, Advanced biosensors for glucose and insulin, Biosens. Bioelectron., 141 (2019) 111201.

[2] K. Tian, M. Prestgard, A. Tiwari, A review of recent advances in nonenzymatic glucose sensors, Mater. Sci. Eng. A ., 41 (2014) 100-118.

[3] V. Scognamiglio, Nanotechnology in glucose monitoring: Advances and challenges in the last 10 years, Biosens. Bioelectron., 47 (2013) 12-25.

[4] Z. Golsanamlou, M. Mahmoudpour, J. Soleymani, A. Jouyban, Applications of advanced materials for non-enzymatic glucose monitoring: from invasive to the wearable device, Crit. Rev. Anal. Chem., (2021) 1-16.

[5] Z. Peng, X. Xie, Q. Tan, H. Kang, J. Cui, X. Zhang, W. Li, G. Feng, Blood glucose sensors and recent advances: A review, J. Innov. Opt. Health Sci., 15 (2022) 2230003.

[6] G. A. Naikoo, H. Salim, I. U. Hassan, T. Awan, F. Arshad, M. Z. Pedram, W. Ahmed, A. Qurashi, Recent Advances in Non-Enzymatic Glucose Sensors Based on Metal and Metal Oxide Nanostructures for Diabetes Management- A Review, Front. Chem., 9 (2021) 748957.

[7] L. Chen, E. Hwang, J. Zhang, Fluorescent nanobiosensors for sensing glucose, Sensors, 18 (2018) 1440.

[8] J.X. Dong, Z.F. Gao, Y. Zhang, B.L. Li, W. Zhang, J.L. Lei, N.B. Li, H.Q. Luo, The pH-switchable agglomeration and dispersion behavior of fluorescent Ag nanoclusters and its applications in urea and glucose biosensing, NPG Asia Mater., 8 (2016) e335-e335.

[9] K.L. Schroeder, R.V. Goreham, T. Nann, Glucose sensor using redox active oligonucleotide-templated silver nanoclusters, Nanomaterials, 9 (2019) 1065.

[10] H.-X. Han, X. Tian, X.-J. Kong, R.-Q. Yu, X. Chu, A new label-free and turn-on fluorescence probe for hydrogen peroxide and glucose detection based on DNA–silver nanoclusters, Anal. Method., 7 (2015) 7989-7994.

[11] T. Wen, F. Qu, N.B. Li, H.Q. Luo, Polyethyleneimine-capped silver nanoclusters as a fluorescence probe for sensitive detection of hydrogen peroxide and glucose, Anal. Chim. Acta., 749 (2012) 56-62.

[12] L.-L. Wang, J. Qiao, L. Qi, X.-Z. Xu, D. Li, Construction of OVA-stabilized fluorescent gold nanoclusters for sensing glucose, Sci. China Chem., 58 (2015) 1508-1514.

[13] R. Botta, A. Rajanikanth, C. Bansal, Silver nanocluster films for glucose sensing by Surface Enhanced Raman Scattering (SERS), Sens. Bio-Sens., 9 (2016) 13-16.

[14] D. Yang, S. Afroosheh, J.O. Lee, H. Cho, S. Kumar, R.H. Siddique, V. Narasimhan, Y.-Z. Yoon, A.T. Zayak, H. Choo, Glucose sensing using surface-enhanced Raman-mode constraining, Anal. Chem., 90 (2018) 14269-14278.

[15] A. Hussain, S. Sarangi, J. Kesarwani, S. Sahu, Au-nanocluster emission based glucose sensing, Biosens. Bioelectron., 29 (2011) 60-65.

[16] S. Naaz, S. Poddar, S.P. Bayen, M.K. Mondal, D. Roy, S.K. Mondal, P. Chowdhury, S.K. Saha, Tenfold enhancement of fluorescence quantum yield of water soluble silver nanoclusters for nano-molar level glucose sensing and precise determination of blood glucose level, Sens. Actuators B Chem., 255 (2018) 332-340.

[17] G.-L. Hong, H.-H. Deng, H.-L. Zhao, Z.-Y. Zou, K.-Y. Huang, H.-P. Peng, Y.-H. Liu, W. Chen, Gold nanoclusters/graphene quantum dots complex-based dual-emitting ratiometric fluorescence probe for the determination of glucose, J. Pharm. Biomed. Anal., 189 (2020) 113480.

[18] Y. Chen, T. Feng, L. Chen, Y. Gao, J. Di, Bovine serum albumin stabilized silver nanoclusters as “signal-on” fluorescent probe for detection of hydrogen peroxide and glucose, Opt. Mater., 114 (2021) 111012.

[19] H. Wang, T. Zhou, W. Li, Z. Wang, Y. Liu, F. Wang, X. Wang, G. Zhang, Z. Zhang, Homocytosine-templated gold nanoclusters as a label-free fluorescent probe: Ferrous ions and glucose detection based on Fenton and enzyme-Fenton reaction, Colloids Surf. A: Physicochem. Eng. Asp., 628 (2021) 127229.

[20] H. Sun, J. Zhang, M. Wang, X. Su, Ratiometric fluorometric and colorimetric dual-mode sensing of glucose based on gold-platinum bimetallic nanoclusters, Microchem. J., 179 (2022) 107574.

[21] S. Maity, D. Bain, S. Chakraborty, S. Kolay, A. Patra, Copper nanocluster (Cu23 NC)-Based biomimetic system with peroxidase activity, ACS Sustain. Chem. Eng., 8 (2020) 18335-18344.

[22] L. Feng, J. Yang, S. Zhang, L. Zhang, X. Chen, P. Li, Y. Gao, S. Xie, Y. Zhang, H. Wang, A capillary-based fluorimetric platform for the evaluation of glucose in blood using gold nanoclusters and glucose oxidase in the ZIF-8 matrix, Analyst, 145 (2020) 5273-5279.

[23] S. Gou, Y.-e. Shi, P. Li, H. Wang, T. Li, X. Zhuang, W. Li, Z. Wang, Stimuli-responsive luminescent copper nanoclusters in alginate and their sensing ability for glucose, ACS Appl. Mater. Interfaces., 11 (2019) 6561-6567.

[24] H. Mei, Y. Ma, H. Wu, X. Wang, Fluorescent and visual assay of H2O2 and glucose based on a highly sensitive copper nanoclusters-Ce (III) fluoroprobe, Anal. Bioanal. Chem., 413 (2021) 2135-2146.

[25] F. Qu, Q. Yang, B. Wang, J. You, Aggregation-induced emission of copper nanoclusters triggered by synergistic effect of dual metal ions and the application in the detection of H2O2 and related biomolecules, Talanta, 207 (2020) 120289.

[26] Y. Wu, Y. Gao, J. Du, Bifunctional gold nanoclusters enable ratiometric fluorescence nanosensing of hydrogen peroxide and glucose, Talanta, 197 (2019) 599-604.

[27] H. Mei, Q. Wang, J. Jiang, X. Zhu, H. Wang, S. Qu, X. Wang, A novel ratiometric nanoprobe based on copper nanoclusters and graphitic carbon nitride nanosheets using Ce (III) as crosslinking agent and aggregation-induced effect initiator for sensitive detection of hydrogen peroxide and glucose, Talanta, 248 (2022) 123604.

[28] Y. Li, S. Li, M. Bao, L. Zhang, C. Carraro, R. Maboudian, A. Liu, W. Wei, Y. Zhang, S. Liu, Pd nanoclusters confined in ZIF-8 matrixes for fluorescent detection of glucose and cholesterol, ACS Appl. Nano Mater., 4 (2021) 9132-9142.

[29] T. Zhou, Z. Su, X. Wang, M. Luo, Y. Tu, J. Yan, Fluorescence detections of hydrogen peroxide and glucose with polyethyleneimine-capped silver nanoclusters, Spectrochim. Acta - A: Mol. Biomol., 244 (2021) 118881.