TiO2 coated SiO2 core-shell stationary phase with uniform and tunable TiO2 thickness for high performance liquid chromatography separation

Jiafei Wang,1 Xiang Wan,1 YingYing Li,1 Debby Mangelings,2 Fazhi Xie,1,3* Xianhuai Huang,3 Weihua Li,3 Donglin Zhao,1 Qishu Qu1*

Fig. S1. TEM images of TiO2 core-shell spheres prepared by the same method as the preparation of SST-0.5-60, but using non-porous SiO2 spheres.

Fig. S2. Pore size distribution of TiO2 core-shell spheres with non-porous SiO2.

Table S1

Chromatographic parameters of the separation of four acidic compounds on C18-SST-0.5-60 and C18-SST-0.7-30 columns.

| columns | samples | k | Rs |  | As | N (plates m-1) |
| --- | --- | --- | --- | --- | --- | --- |
| C18-SST-0.5-60 | p-nitrophenol | 0.39 | - | - | 1.3 | 7772 |
|  | phenol | 0.87 | 3.3 | 2.7 | 1.2 | 4722 |
|  | o-chlorophenol | 1.2 | 1.1 | 1.5 | 1.5 | 2644 |
|  | m-chlorophenol | 2.2 | 5.0 | 1.9 | 0.9 | 38342 |
| C18-SST-0.7-30 | p-nitrophenol | 0.52 | - | - | 1.4 | 1897 |
|  | phenol | 1.2 | 1.9 | 2.6 | 1.3 | 1240 |
|  | o-chlorophenol | 1.8 | 0.9 | 1.4 | 1.4 | 927 |
|  | m-chlorophenol | 4.5 | 5.4 | 1.7 | 1.1 | 27246 |

Table S2

Chromatographic parameters of the separation of a standard mixture of adenosine, ATP, ADP and AMP on C18-SST-0.5-60 and C18-SST-0.7-30 columns.

| columns | samples | k | Rs |  | As | N (plates m-1) |
| --- | --- | --- | --- | --- | --- | --- |
| C18-SST-0.5-60 | adenosine | 0.68 | - | - | 1.1 | 1402 |
|  | AMP | 4.1 | 1.9 | 6.0 | 2.0 | 162 |
|  | ADP | - | - | - | - | - |
|  | ATP | 40.1 | 3.9 | 9.8 | 1.1 | 1448 |
| C18-SST-0.7-30 | adenosine | 0.48 | - | - | 1.2 | 887 |
|  | AMP | 3.0 | 1.8 | 6.3 | 2.0 | 130 |
|  | ADP | - | - | - | - | - |
|  | ATP | 38.2 | 3.3 | 12.7 | 1.2 | 952 |