Electronic supporting information

### Sonochemical-assisted synthesis combined with the plant-mediated approach for efficient and green synthesis of copper oxide nanoparticles: Study the effect of extraction techniques and comparative evaluation of some biological activities

Hamid Reza Rajabia, *, Zinab Moradi Alvanda, Ali Mirzaeib

a Chemistry Department, Yasouj University, Yasouj, 75918-74831, Iran.

b Medicinal Plant Research Center, Yasouj University of Medical Sciences, Yasouj, Iran

*Corresponding author. Tel. /Fax: +98 741 2242164.

E-mail address: h.rajabi@mail.yu.ac.ir, hr.rajabi@gmail.com (H.R. Rajabi).

| Gram-positive |  |  |  |  |  | Gram-negative |  |  |  |  |  |  | Compound |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bacillus Subtilis |  |  | Staphylococcus oureus |  |  |  | Escherichia coli |  |  | Pseudomonas aeruginosa |  |  |  |  |
| 6.25 | 12.5 | 25 | 6.25 | 12.5 | 25 |  | 6.25 | 12.5 | 25 | 6.25 | 12.5 | 25 | mg/mL |  |
| 8.00 | 8.87 | 9.45 | 7.73 | 8.43 | 9.10 |  | 8.08 | 8.92 | 9.65 | 8.36 | 9.08 | 10.16 | MAE | aqueous extract |
| 8.50 | 9.00 | 9.95 | 8.30 | 9.00 | 9.73 |  | 8.72 | 9.35 | 10.20 | 9.13 | 9.80 | 10.35 | UAE |  |
| 10.60 | 11.40 | 11.70 | 10.30 | 11.10 | 11.40 |  | 10.80 | 11.60 | 11.80 | 11.00 | 11.80 | 12.00 | MAE | CuO NPs |
| 11.40 | 11.60 | 12.00 | 11.00 | 11.50 | 11.70 |  | 11.50 | 11.80 | 12.10 | 11.70 | 12.00 | 12.40 | UAE |  |
| 8.10 | 8.70 | 9.50 | 7.80 | 8.70 | 9.00 |  | 7.89 | 9.00 | 9.75 | 8.0 | 8.72 | 9.63 | Uncoated |  |

Table S1. The results of antibacterial studies by disk diffusion method.

Table S2. MIC and MBC data of the samples (in mg/mL) for gram-negative and gram-positive bacteria.

| Gram-positive |  |  |  | Gram-negative |  |  |  | Compound |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bacillus Subtilis |  | Staphylococcus oureus |  | Escherichia coli |  | Pseudomonas aeruginosa |  |  |  |
| MIC | MBC | MIC | MBC | MIC | MBC | MIC | MBC |  |  |
| 3.20 | 3.20 | 3.20 | 3.20 | 1.60 | 1.60 | 1.60 | 1.60 | MAE | Aqueous Extract |
| 1.60 | 3.20 | 3.20 | 3.20 | 0.80 | 1.60 | 0.80 | 0.8 | UAE |  |
| 0.80 | 0.80 | 0.40 | 0.80 | 0.10 | 0.10 | 0.05 | 0.05 | MAE | CuO NPs |
| 0.40 | 0.40 | 0.80 | 0.80 | 0.05 | 0.10 | 0.05 | 0.05 | UAE |  |
| 3.20 | 6.40 | 6.40 | 6.40 | 3.20 | 3.20 | 1.60 | 3.20 | Uncoated | CuO NPs |

Table S3. Antifungal activities of constructed disks based on diameter zone (mm) of inhibition against two funguses

| Compound |  | Antifungal |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Candida albicans |  |  | Aspergillus oryzae |  |  |
| mg/mL |  | 25 | 12.5 | 6.25 | 25 | 12.5 | 6.25 |
| extract CuO NPs | MAE | 8.20 | 7.30 | 6.70 | 8.50 | 7.60 | 6.90 |
|  | UAE | 8.60 | 8.00 | 7.50 | 8.80 | 8.30 | 7.80 |
|  | MAE | 9.80 | 9.60 | 9.00 | 9.80 | 9.70 | 9.10 |
|  | UAE | 10.20 | 9.80 | 9.30 | 10.45 | 10.20 | 9.70 |
|  | Uncoated | 8.00 | 7.50 | 7.00 | 8.10 | 7.70 | 7.20 |