SUPPORTING INFORMATION

Current Collectors Corrosion Behaviours and Rechargeability of TiO2 in Aqueous Electrolyte Aluminium-ion Batteries

Burcu Unala,b, Ozlem Selc,d and Rezan Demir-Cakana,b*

a Department of Chemical Engineering, Gebze Technical University, Gebze, Kocaeli, 41400, Turkey

b Institute of Nanotechnology, Gebze Technical University, Gebze, Kocaeli, 41400, Turkey

c Chimie du Solide et de l’Energie, UMR 8260, Collège de France, 11 Place Marcelin Berthelot, 75231 Paris Cedex 05, France

d Réseau sur le Stockage Electrochimique de l’Energie (RS2E), CNRS FR 3459, 33 Rue Saint Leu, 80039 Amiens Cedex, France

*Corresponding author: demir-cakan@gtu.edu.tr

Figure S1. pH and ionic conductivities of a) AlCl3, b) Al2(SO4)3 and c) Al(NO3)3 aqueous electrolytes at different concentrations.

Figure S2. SEM images of current collectors, before and after CV measurements in 1.0 M AlCl3: GP, Ti, Ni, SS (from up to down, respectively).

Figure S3. Potentiodynamic polarization curves between (-1.0 – 1.0) V at 1mV/s scan rate in 1.0 M AlCl3. a) SS, b) Ni, c) Ti, d) GP.

Figure S4. Electrochemical test of TiO2 on Ti current collector cycled in 1.0 M AlCl3 containing aqueous electrolyte at 3A/g a) galvanostatic charge-discharge curves and b) capacity retention profile

Figure S5. Images of TiO2 coated SS, Ni, Ti and GP current collectors demonstrating the macroscopic changes in electrolyte after galvanostatic charge-discharge experiment in 1.0 M AlCl3 containing aqueous electrolyte.

Table S1. Lattice spaces attributed to the Miller Index of anatase TiO2 from selected area electron diffraction (SAED).

|  | 1/2r (nm-1) | 1/r (nm-1) | r (nm) | d-space (Å) | Miller Index (hkl) |
| --- | --- | --- | --- | --- | --- |
| 1 | 5.973 | 2.987 | 0.335 | 3.348 | 101 |
| 2 | 8.441 | 4.221 | 0.237 | 2.369 | 004 |
| 3 | 10.621 | 5.311 | 0.188 | 1.883 | 200 |
| 4 | 11.928 | 5.964 | 0.168 | 1.677 | 105 |
| 5 | 13.605 | 6.803 | 0.147 | 1.470 | 204 |
| 6 | 14.982 | 7.491 | 0.133 | 1.335 | 220 |

Table S2. An electrochemical performance comparison of TiO2 electrodes for aqueous electrolyte Al-ion batteries.

| Electrode | Electrolyte | Current Collector | Current Density | Discharge Capacity | Efficiency (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Anodic treated TiO2-NTA | 0.25 M Al2(SO4)3 1.5 M NaCl mixed soln. | Ti foil | 4mA/cm2 | 74.5 mAh/g | N/A | (15) |
| TiO2, anatase nanotube | 1.0 M AlCl3 | Ti foil | 4mA/cm2 | 75 mAh/g (14 cycles) | N/A | (18) |
| Treated- TiO2 | 1.0 M AlCl3/1.0 M KCl | Carbon polymer | 0.2 - 10 A/g (various current densities) | 23.1 mAh/g (60 cycles at 1.0 A/g) 15.3 mAh/g at 10 A/g | 96.2 99.95 | (20) |
| TiO2-NSs | 1.0 M AlCl3 | Nickel disks | 0.15C and 6.0C | 183 mAh/g at 0.15C (initial capacity) 108 mAh/g at 6.0 C (initial) | N/A | (19) |
| TiO2/CNT | 1.0 M AlCl3 | Nickel disks | 1C (335 mA/g) | 170 mAh/g (100 cycles) | 99.9 | (29) |
| TiO2, anatase | 1.0 M AlCl3 | Graphite Ti foil | 4A/g | 140 mAh/g (20 cycles) 35 mAh/g (30 cycles) | ~48 ~50 | (43) |
| Ti-deficient rutile TiO2 | 1.0 M AlCl3/1.0 M NaCl | Tantalum foil | 3A/g | 64 mAh/g (110 cycles) | ~50 | (44) |
| TiO2, anatase | 1.0 M AlCl3 | Graphite plate | 3 A/g | 249 mAh/g (initial) 105 mAh/g (50 cycles) | ~73.9 | Present work |