Experimental Section

NMR Measurements
1H NMR spectra were recorded on a Bruker AVANCE III spectrometer operating at 500 MHz. CDCl3 was used as the solvent, and chemical shifts were reported relative to solvent residual signals.

SEC Measurements
SEC measurements were performed using a Waters e-2695 high-speed liquid chromatograph equipped with RI and UV detectors. THF was used as the eluent at a flow rate of 0.50 mL min−1 at 40 °C and a Shodex KF-603 column was employed. The calibration curve was obtained with TSK standard polystyrenes (Tosoh Co.); the Mw(LS)s were 189000, 37200, 9490, 2500, and 589.

Rheological analyses
Rheological analyses were performed on an Anton Paar MCR 102 rheometer equipped with a Peltier temperature control device. Time-dependent analyses of G’ and G’’ for the PDMS samples with a thickness of 0.3 mm were conducted using a parallel plate with a diameter of 12 mm at a frequency of 5 Hz at 25 °C.

Tensile tests
Tensile tests were conducted on a Shimadzu AGS-X mechanical testing machine with a 5 N load cell operating at a crosshead speed of 100 mm min−1 at room temperature. The tensile modulus (E), elongation at break (B), tensile strength (T), and fracture energy () of a specimen were calculated with TRAPEZIUM X software built into the instrument.

Supplementary Figure 1. 1H NMR spectra (80 MHz, THF) of (a) I3, (b) U(Cy), (c) I3 + U(Cy) ([I3] : [U(Cy)] = 1 : 3), (d) I3 + TBD ([I3] : [TBD] = 1 : 0.75), and (e) I3 + TBD + U(Cy) ([I3] : [TBD] : [U(Cy)] = 1 : 0.75 : 3). [I3] = 0.018 M. The asterisks indicate satellite signals of two THF-derived signals appearing at 1.79 and 3.62 ppm.

Supplementary Figure 2. SEC trace of (a) PH. and (b) PV.