# Supporting information

# A novel copper-based metal-organic framework: Synthesis, characterization and evaluation for the hydrogenation of furfural to furfuryl alcohol

# Pamela S. Moyoa, Gift Mehlanab*, Leah C. Matsinhaa* and Banothile C.E. Makhubelaa*

aResearch Centre for Synthesis and Catalysis, Department of Chemical Sciences, University of Johannesburg, Auckland Park 2006, Johannesburg,  South Africa.

bDepartment of Chemical Sciences, Midlands State University, 9055 Senga Road, Gweru, Zimbabwe.

Author Information

Corresponding authors

# Email*: leahmatsinha@uj.ac.za, mehlanag@staff.msu.ac.zw and bmakhubela@uj.ac.za.

Characterizations

b

e

DMSO-d6

d c

a

Figure SI 1: 1H NMR spectrum of L1.

10 9

7-2

8

1

DMSO-d6

Figure SI 2: 13C{H} NMR spectrum of L1, recorded in DMSO-d6.

m/z = 403.0918 for [M-H]-

Figure SI 3: HR-ESI-MS spectrum of ligand L1.

1609 cm-1

1683 cm-1

NH = 3276 cm-1

Figure SI 4: FT-IR spectra of L1.

H2O

DMSO-d6

Figure SI 5: 1H NMR spectrum of digested Cu-MOF recorded in DMSO-d6.

Figure SI 6: EDX image for Cu-MOF.

# Catalytic hydrogenation of furfural

DMF+FF

FF+FA

FF

CDCI3+ FA

FA

MeOH

MeOH

DMF

Figure SI 7: A typical 1H NMR of the hydrogenation of FF reaction using molecular H2, temperature (140 ⁰C), methanol (5 mL), FF (2.5 mmol), Cu-MOF (33 µmol), time (24 hours) and DMF (internal standard) showing product of FA only, recorded in CDCl3.

# Figure SI 8: HR-TEM images for Cu-MOF before catalysis at (a) 200 nm and (b) 100 nm.