Supplementary Information (SI)

Self-calibrating sensor based on S-CNF/Au NSs for the detection of malondialdehyde levels in the serum of patients with gastric cancer

Wenxi Wanga†, Sirui Hana†, Junjie Rena, Xiufeng Xiaoa, Jingbo Chenb, Ruiyun Youa*, Guifeng Zhangb*, Yudong Lua*

a College of Chemistry and Materials Science, Fujian Provincial Key Laboratory of advanced Oriented Chemical Engineer, Fujian Key Laboratory of Polymer Materials, Engineering Research Center of Industrial Biocatalysis, Fujian Province Higher Education Institutes, Fujian Normal University, Fuzhou, Fujian 350007, China

b Department of Oncology, Shengli Clinical Medical College Fujian Medical University, Fujian Provincial Hospital, Fuzhou, Fujian 350001, China

† These authors contributed equally to this work.

*Correspondence: youruiyun@fjnu.edu.cn; 984386537@qq.com; luyd@fjnu.edu.cn

Table S1 and S2

Table S1 Factor and level table

| Level | Factor |  |  |
| --- | --- | --- | --- |
|  | A | B | C |
|  | Time（min） | pH | Temperature（℃） |
| 1 | 5 | 2 | 25 |
| 2 | 10 | 4.13 | 30 |
| 3 | 15 | 5.19 | 40 |
| 4 | 20 | 6.34 | 50 |
| 5 | 30 | 7.6 | 60 |

Table S2 Orthogonal experimental table

| Number | Factors |  |  |
| --- | --- | --- | --- |
|  | A | B | C |
| 1 | 1 | 1 | 1 |
| 2 | 1 | 2 | 3 |
| 3 | 1 | 3 | 5 |
| 4 | 1 | 4 | 2 |
| 5 | 1 | 5 | 4 |
| 6 | 2 | 1 | 5 |
| 7 | 2 | 2 | 2 |
| 8 | 2 | 3 | 4 |
| 9 | 2 | 4 | 1 |
| 10 | 2 | 5 | 3 |
| 11 | 3 | 1 | 4 |
| 12 | 3 | 2 | 1 |
| 13 | 3 | 3 | 3 |
| 14 | 3 | 4 | 5 |
| 15 | 3 | 5 | 2 |
| 16 | 4 | 1 | 3 |
| 17 | 4 | 2 | 5 |
| 18 | 4 | 3 | 2 |
| 19 | 4 | 4 | 4 |
| 20 | 4 | 5 | 1 |
| 21 | 5 | 1 | 2 |
| 22 | 5 | 2 | 4 |
| 23 | 5 | 3 | 1 |
| 24 | 5 | 4 | 3 |
| 25 | 5 | 5 | 5 |

S1 Limit of detection

The LOD was then determined according to the following equation:

LOD(y) =3σ/s

σ for the measurement's standard deviation for the blank sample, and s for the calibration plot's slope. Where LOD (y) is represented LOD (I1655/I1078). The LOD (MDA) was calculated via the conversion of LOD (y) using the equation originated from the calibration curve.