Biopolymer-assisted enzyme-induced carbonate precipitation for Cu-contaminated loess remediation

Yi-Xin Xie1,3, Wen-Chieh Cheng2,3*, Lin Wang1,3, Zhong-Fei Xue1,3, and Yin-Long Xu3,4

1PhD student, School of Civil Engineering, Xi’an University of Architecture and Technology, Xi’an 710055, China. Email: xieyixin@xauat.edu.cn (Y.-X. Xie), wanglin@xauat.edu.cn (L. Wang), xuezhongfei@xauat.edu.cn (Z.-F. Xue)

2Professor, School of Civil Engineering, Xi’an University of Architecture and Technology, Xi’an 710055, China. *Corresponding author, email: w-c.cheng@xauat.edu.cn (W.-C. Cheng)

3Shaanxi Key Laboratory of Geotechnical and Underground Space Engineering (XAUAT), Xi’an 710055, China

4Graduate student, School of Civil Engineering, Xi’an University of Architecture and Technology, Xi’an 710055, China. Email: xylh@xauat.edu.cn (Y.-L. Xu)

These Supplemental files include

7 Pages

2 Figures

3 Tables

Figure and Table Legends

Figure S1 a Urease extraction and preparation of chitosan colloid; b Test tube experiments; c Soil column tests

Figure S2 Particle-size distribution curve for the loess soil

Table S1 Scheme applied to the test tube experiments

Table S2 Physical and mechanical properties of the loess soil

Table S3 Scheme applied to the one-dimensional soil column tests

Figure S1 a Urease extraction and preparation of chitosan colloid b Test tube experiments c Soil column tests

Figure S2 Particle-size distribution curve for the loess soil

Table S1 Scheme applied to the test tube experiments

|  | Concentration (mM) |  |  | Concentration (g/L) |  |
| --- | --- | --- | --- | --- | --- |
|  | Cu(NO3)2 | Urea | CaCl2 | Urease | Chitosan |
| 1 | 5-50 | 500 | 0 | 3 | 0 |
| 2 | 5-50 | 500 | 0 | 3 | 2 |
| 3 | 5-50 | 500 | 0 | 3 | 4 |
| 4 | 5-50 | 500 | 250 | 3 | 2 |
| 5 | 5-50 | 500 | 250 | 3 | 4 |

Table S2 Physical and mechanical properties of the loess soil

| ωL/% | ωP/% | IP | ωn/% | ρdmax/g·cm-3 | Gs | USCS symbol |
| --- | --- | --- | --- | --- | --- | --- |
| 24.4 | 14.2 | 10.2 | 17.25 | 1.745 | 2.66 | CL |
| Note: ωL = liquid limit; ωP = plastic limit; IP = plastic index; ωn = natural moisture content; Gs = specific gravity; USCS = Unified Soil Classification System |  |  |  |  |  |  |

Table S3. Scheme applied to the one-dimensional soil column tests.

|  | Group ID | Cu2+ concentration /mg·kg-1 | UC2 concentration /mM | UC1 concentration /g·L-1 |
| --- | --- | --- | --- | --- |
| Control group | CG | 500 | 0 | 0 |
|  | CG | 2000 | 0 | 0 |
|  | CG | 4000 | 0 | 0 |
| Test group 1 | TG2 | 500 | 1000/500 | 10/2 |
|  | TG2 | 2000 | 1000/500 | 10/2 |
|  | TG2 | 4000 | 1000/500 | 10/2 |
| Test group 2 | TG4 | 500 | 1000/500 | 10/4 |
|  | TG4 | 2000 | 1000/500 | 10/4 |
|  | TG4 | 4000 | 1000/500 | 10/4 |
| Note: UC1 = Urease and chitosan colloid; UC2 = Urea and CaCl2 |  |  |  |  |