Supporting information

Rotenone nanoparticles based on mesoporous silica to improve the stability, translocation and insecticidal activity of rotenone

Wangjin Xu, Dianjing Shen, Xiaojun Chen*, Ming Zhao, Tianle Fan, Qinchao Wu, Zhiyuan Meng, Jiajia Cui

College of Plant Protection, Yangzhou University/Joint International Research Laboratory of Agriculture & Agri-Product Safety (Yangzhou University), Jiangsu Yangzhou, 225009, People’s Republic of China.

Correspondence author: Xiaojun Chen, Professor, E-mail: cxj@yzu.edu.cn

The table of contents

Fig S1. Preparation of mesoporous silica nanoparticles (MSNs).

Fig S2. Application site of Rot@MSNs and sampling position of tomato plants.

Fig S3. TEM images of Rot@MSNs.

Fig S4. XRD pattern of Rotenone, MSNs and Rot@MSNs.

Table S1. Rotenone drug loading rate

Table S2. Transfer factors of rotenone in tomato plants treated with Rot@MSNs and ME.

Table S3. Degradation kinetic of rotenone on the tomato leaves.

Fig S1. Preparation of mesoporous silica nanoparticles (MSNs).

Fig S2. Application site of Rot@MSNs and sampling position of tomato plants.

| Fig S3. TEM images of Rot@MSNs |  |
| --- | --- |

Fig S4. XRD pattern of Rotenone, MSNs and Rot@MSNs.

Table S1. Rotenone drug loading rate

| Treatment | Rotenone quality（mg） | Drug loading rate（%） |
| --- | --- | --- |
| Treatment 1 | 3.341 | 33.41 |
| Treatment 2 | 3.318 | 33.18 |
| Treatment 3 | 3.319 | 33.19 |
| Average value | 3.326 | 33.26±0.13 |

Table S2. Transfer factors of rotenone in tomato plants treated with Rot@MSNs and ME

| Treatment times | Rot@MSN |  | ME |  |
| --- | --- | --- | --- | --- |
|  | TFUpper | TFLower | TFUpper | TFLower |
| 2 h | 0.0124 d | 0.0018 d | 0.1071 b | 0.0344 cd |
| 1 d | 0.0049 d | 0.0042 d | 0.0325 d | 0.0079 d |
| 5 d | 0.0051 d | 0.0020 d | 0 | 0 |
| 10 d | 0.0615 c | 0.1633 a | 0 | 0 |
| 14 d | 0.1347 b | 0.1384 ab | 0 | 0 |
| TFAverage | 0.0437 | 0.0619 | 0.0279 | 0.0085 |

*Means with the same letter are not significantly different (Duncan’s multiple range test, p≤0.05, n=3).

Table S3. Degradation kinetic of rotenone on the tomato leaves

| Treatments | Rot@MSNs | ME |
| --- | --- | --- |
| 24 | 13.5235 ±1.1348 | 11.4452 ± 1.1124 |
| 48 | 11.0842 ± 0.9213 | 7.2024 ± 0.9388 |
| 72 | 9.8816 ± 0.4382 | 5.7114 ± 0.6722 |
| 96 | 7.9932 ± 0.5673 | 4.0132± 0.5228 |
| 192 | 3.7268 ± 0.2397 | 1.1924± 0.2453 |
| Degradation kinetic equation | Ct=16.4712e-0.0077t | Ct=14.5813e-0.0132t |
| Half-life T1/2 (h) | 90.01 | 52.51 |