Table 3. Pyrolysis products of compound 4b.

| Peak | RT/min | Pyrolysis products | Structure | Match | Relative content/% |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | 300 °C | 350 °C | 400 °C |
| 1 | 13.93 | Ethyl maltol |  | 95 | - | 66.00 | 50.13 |  |
| 2 | 24.90 | 2-Methyl-1H-pyrrole |  | 89 | - | 28.92 | 42.80 |  |
| 3 | 27.90 | 4-(Methoxycarbonyl)-5-methyl-1-propyl-1H-pyrrole-2-carboxylic acid |  | 90 | - | 5.06 | 1.02 |  |