Supporting Information

Portable visual and electrochemical detection of hydrogen peroxide release from living cells based on dual functional Pt-Ni hydrogels

Guanglei Li1,2, Yao Chen1, Fei Liu1, Wenhua Bi1, Chenxin Wang1, Danfeng Lu3 and Dan Wen1*

Correspondence: Dan Wen (dan.wen@nwpu.edu.cn, ORCID: 0000-0001-6879-7982)

1State Key Laboratory of Solidification Processing, School of Materials Science and Engineering, NPU and Shaanxi Joint Laboratory of Graphene, Xi’an, 710072, P. R. China.

2Interdisciplinary Research Center of Biology & Catalysis, School of Life Sciences, Northwestern Polytechnical University (NPU), Xi'an, 710072, P. R. China.

3Faculty of Printing, Packaging Engineering, and Digital Media Technology, Xi’an University of Technology, Xi’an, 710048, P. R. China.

These authors contributed equally: Guanglei Li, Yao Chen, Fei Liu.

Fig. S1 The scanning electron microscopy (SEM) image of the (A) pure Pt, (B) PtNi, (C) PtNi5 and (D) pure Ni hydrogels. The transmission electron microscopy (TEM) images of the (E) pure Pt, (F) PtNi, (G) PtNi5 and (H) pure Ni hydrogels.

Fig. S2 Time-dependent absorbance at 652 nm measured from the reaction solutions containing 0.5 mM hydrogen peroxide (H2O2), 0.5 mM 3,3,5,5-tetramethylbenzidine (TMB), and 0.05 μg mL-1 PtNi3 hydrogel in 0.1 M phosphate buffer solution (PBS) (pH 5.0) at room temperature.

Fig. S3 Lineweaver-Burk curves and double-reciprocal diagrams of the initial reaction rates of the PtNi3 hydrogel for the (A) TMB and (B) H2O2.

Fig. S4 Lineweaver-Burk curves and double-reciprocal diagrams of the initial reaction rates of the PtNi hydrogel for the (A) TMB and (B) H2O2.

Fig. S5 Lineweaver-Burk curves and double-reciprocal diagrams of the initial reaction rates of the PtNi5 hydrogel for the (A) TMB and (B) H2O2.

Fig. S6 Lineweaver-Burk curves and double-reciprocal diagrams of the initial reaction rates of the Pt hydrogel for the (A) TMB and (B) H2O2.

Fig. S7 Lineweaver-Burk curves and double-reciprocal diagrams of the initial reaction rates of the Ni hydrogel for the (A) TMB and (B) H2O2.

Fig. S8 UV-vis absorption spectra of the PtNi3 hydrogel at (A-B) a temperature gradient of 25-75 ℃ and (C-D) a pH range of 2-9 in the presence of 0.5 mM TMB and 0.2 mM H2O2.

Table S1: Comparison of the kinetic parameters of the PtNix, pure Pt, Ni hydrogels and other artificial/natural enzymes.

| Samples | Km (mM) |  | Vmax (10-8 Ms-1) |  | Kcat (s-1) |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | TMB | H2O2 | TMB | H2O2 | TMB | H2O2 |  |
| PtNi3 hydrogel | 0.031 | 0.67 | 6.08 | 4.52 | 4.50×104 | 3.35×104 | This work |
| PtNi hydrogel | 0.048 | 0.818 | 5.43 | 3.37 | 2.76×104 | 1.71×104 | This work |
| PtNi5 hydrogel | 0.049 | 0.873 | 5.10 | 3.28 | 2.37×104 | 1.29×104 | This work |
| Pt hydrogel | 0.059 | 0.904 | 5.18 | 3.40 | 2.54×104 | 1.87×104 | This work |
| Ni hydrogel | 1.26 | 2.23 | 0.17 | 0.14 | 2.02×103 | 1.62×103 | This work |
| Pd@Pt core-frame | 0.43 | 14 | 5.10 | 9.0 | 7.20×10-3 | 1.30×10-2 | 1 |
| Pt/hBNNSs | 0.21 | 9.2 | / | / | / | / | 2 |
| Pt nanodendrites | 0.81 | 6.90 | 12 | 9.90 | 1.70×10-2 | 1.40×10-2 | 1 |
| Fe-N-C SAzymes | 3.6 | 12 | 116 | 35.6 | 0.78 | 0.24 | 3 |
| Fe-AL-E | 20.10 | 58.0 | 5.43 | 1.12 | 8.83×10-5 | 1.82×10-5 | 4 |
| Pd cubes | 0.054 | 700 | 9.7 | 6.5 | 6.9×104 | 4.6×104 | 5 |
| MoSA-N3-C | 0.79 | / | / | 37 | 4.0×104 | / | 6 |
| HRP | 0.43 | 3.70 | 10.0 | 8.71 | 4.0×103 | 3.48×103 | 7 |

Table S2: The comparison of the sensing performances between the as-prepared colorimetric H2O2 sensor and the others recently reported in the literatures.

| Sensing material | Linearity range | Limit of detection | Long-term stability (signal retention) | Ref. |
| --- | --- | --- | --- | --- |
| PtNi(1:3) hydrogel | 0.1 μM-10 mM | 0.03 μM | 60 days | This work |
| Pt nanoclusters | 0-200 μM | 0.46 μM | 1 months | 8 |
| B, N-PdRu aerogel | 10 μM-2 mM | 6 μM | / | 9 |
| Fe-AL | 10-100 mM | 54 μM | / | 10 |
| Fe0.8Ni0.2S2 | 1.25-12.5 μM | 0.77 μM | / | 11 |
| MSA/Cu NCs | 1 μM-1 mM | 0.5 μM | 10 months | 12 |
| PtNPs/Cu-TCPP(Fe) | 2-100 μM | 0.357 μM | / | 13 |
| Fe/CuSn(OH)6 | 30-1000 μM | 9.49 μM | 11 days | 14 |
| cysteine/I-/Au NPs | 0-80 μM | 2 μM | / | 15 |

Table S3: The measured R, G, B values at different concentrations of H2O2.

| H2O2 (μM) | B/(R+G+B) |
| --- | --- |
| 0 | 0.33433 |
| 0.5 | 0.33448 |
| 5 | 0.33645 |
| 50 | 0.34439 |
| 100 | 0.35086 |
| 500 | 0.39023 |
| 1000 | 0.44915 |

Supplemental References

- Wu, R. F. et al. Adv. Funct. Mater. 28, 1801484 (2018).

- Ivanova, M. N. et al. ACS Appl. Mater. Inter. 11, 22102-22112 (2019).

- Jiao, L. et al. Anal. Chem. 91, 11994-11999 (2019).

- Li, L. J. et al. ACS Sustain. Chem. Eng. 9, 12833-12843 (2021).

- Xia, X. H. et al. ACS Nano 9, 9994-10004 (2015).

- Wang, Y. et al. Chem 7, 436-449 (2021).

- Gao, L. et al. Nat. Nanotechnol. 22, 577-583 (2007).

- Jin, L. H. et al. ACS Appl. Mater. Inter. 9, 10027-10033 (2017).

- Zeng, Y. T. et al. ACS Appl. Mater. Inter. 13, 36816-36823 (2021).

- Li, L. J. et al. ACS Sustain. Chem. Eng. 9, 12833-12843 (2021).

- Zhang, C. Y. & Nan, Z. D. J. Phys. Chem. C 126, 4355-4364 (2022).

- Du, Y. B., Fang, J., Wang, H. L. & Yang, Y. ACS Appl. Mater. Inter.9, 11035-11044 (2017).

- Chen, H. Y. et al. ACS Appl. Mater. Inter. 10, 24108-24115 (2018).

- Liu, H. et al. ACS Sustainable Chem. Eng. 6, 14383-14393 (2018).

- Wang, F., Liu, X. Q., Lu, C. H. & Willner, I. ACS Nano 7, 7278-7286 (2013).