Supplementary Materials

Molecular mechanisms in metal oxide nanoparticle Tryptophan interactions

Alexandra Nefedova,a Fredric G. Svensson,b Alexander S. Vanetsev,a* Peter Agback,b Tatiana Agback,b Lars Kloo,c Tanel Tätte,a Angela Ivask,d Gulaim A. Seisenbaeva,b Vadim G. Kesslerb*

a Institute of Physics, University of Tartu, W.Ostwaldi 1, 50411 Tartu, Estonia. alexander.vanetsev@ut.ee

b Department of Solid State Physics, Ångström Laboratory, Uppsala University, Box 35, SE-75103 Uppsala, Sweden

c Department of Molecular Science, BioCenter, Swedish University of Agricultural Sciences, Box 7015, 75007 Uppsala, Sweden. vadim.kessler@slu.se

d Applied Physical Chemistry, KTH Royal Institute of Technology, Teknikringen 30, SE-100 44 Stockholm, Sweden.

e Institute of Molecular and Cell Biology, University of Tartu, Riia 23, 51010 Tartu, Estonia.

Fig  S1. Titration of 0.5mM Trp with Captigel (A), TiBALD (B), Ce(-)(C) and Ce(+)(D). The following colours of curves obtained at different ration of NP/Tript were used. (A), (B) Trp: Captigel/or TiBALD:  0.5mM: 0mM (black); 0.5mM:0.031mM (blue); 0.5mM:0.0625mM (red); 0.5mM:0.125mM (green); 0.5mM:0.250mM (light green);) 0.5mM:0.5mM (light blue); 0.5mM:1.0mM (ros). (C), (D) Trp: Ce(-)(C)/or Ce(+)(D): 0.5mM: 0mM (black); 0.5mM:0.0005mM (blue); 0.5mM:0.001mM (red); 0.5mM:0.002mM (green); 0.5mM:0.005mM (light green); 0.5mM:0.007mM (light blue).

Fig  S2. Normalized intensities (I/Io) of H6 proton resonance of Trp at 7.728 ppm vs to the ratio (R) of Trp: TiO2-I (blue line) and Trp: TiO2-II (black line) mixtures

Fig  S3. Particle size distribution by DLS after 72 h of storage for Trp solutions containing TiO2-I (left) and TiO2-II (right).

Fig  S4. NMR spectra with assignment of the oxidized product of Trp obtained in mixture with Ce(-)(C) NP. Superposition of the HMBC (blue)  and HSQC( red, black) spectra are presented  in the aromatic 8.0-6.5ppm (A) and aliphatic (C) regions. 1H spectrum is in the regions (B) and (D), respectively. Assignment and numbering was shown according structure on panel (A).

Fig  S5. Total Ion Current (TIC) chromatogram from a Bruker’s Maxis Impact Q-TOF mass spectrometer obtained after an HPLC-MS analysis of the sample using a Hypercarb (4.6x100mm) HPLC column (a); Mass spectrum of the peak at Rt. 3.1 min. i.e that of a mono-oxy compound (b); Mass spectrum of the peak at Rt. 10.9 min that of unreacted Tryptophan for comparison (c).

Fig  S6. UV-Vis spectra of the EtOH:H2O = 1:1 solutions of (HTrp)3PW12O405H2O.

Fig. S7  Assignment of the 1H and 13C chemical shifts of Trp in complex (HTrp)3PW12O405H2O.

In panel  (A)  the superposition of the one bond 1H-13C correlation, HSQC (red), and 2, 3 1H-13C bonds correlation, HMBC(blue), spectra dissolved in dmsod6 are presented with 13C projection (left) with assignment. In panel (B) and (C) 1D 1H spectra of Trp in complex (HTrp)3PW12O405H2O and free form are presented respectively. In HMBC spectrum one bond 1H-13C coupling is not suppressed.

Fig. S8 1H expended spectra in aromatic region (A) 8.05-7.65 (B) 6.9-4.9 ppm of the Trp:NP complex exposed to UV light filtered in in dmsod6 solution.

(black) Trypt: bare TiO2;(blue), Trypt: TiO2-I, (red) and Trypt: TiO2-II. There are signals of oxidation products after UV irradiation in solution of Trypt: bare-TiO2 but not Trypt: TiO2-I or Trypt: TiO2-II.

Table TS1

Table TS2

Table TS3. Key energies for the species involved in the reactions (1)-(3), in electron volts (eV).

| Species | HOMO* / eV | LUMO* / eV | Etot / eV |
| --- | --- | --- | --- |
| W12PO403-, C1 | -3.032 | +4.215 | -113265.42 |
| W12PO403-, T | -3.032 | +4.215 | -113265.42 |
| W12PO403-(aq), C1 | -9.849 | -2.583 | -113275.81 |
| HW12PO402-, C1 | -5.648 | +1.597 | -113281.19 |
| HW12PO403-(aq), C1 | -10.103 | -2.856 | -113286.43 |
| W12PO404- | +2.892/-0.142 | +7.135/+7.177 | -113261.58 |
| HW12PO403- | -0.426/-2.939 | +4.335/+4.334 | -113280.31 |
| HW12PO403-(aq) | -6.589/-9.638 | -2.317/-2.295 | -113290.87 |
| TRP | -7.136 | +0.467 | -18672.74 |
| TRP+ | -11.621/-12.111 | -4.251/-7.350 | -18665.46 |
| TRP+(aq) | -8.484/-9.079 | -0.953/-4.100 | -18667.49 |
| HTRP+ | -10.686 | -3.622 | -18682.81 |
| HTRP+(aq) | -7.527 | +0.111 | -18685.22 |
| HTRP2+ | -15.507/-15.912 | -7.907/-11.094 | -18671.89 |

*The HOMOs/LUMOs with two values correspond to doublet ground states with alpha and beta electron energies given separately.