Supplementary Information

Wood carbon electrode in microbial fuel cell enhances chromium reduction and bioelectricity generation

Hongyuhang Niac§, Aman Khana§, Zi Yangb§, Yuxin Gonga, Gohar Alia, Pu Liua, Fengjuan Chenb*, Xiangkai Lia*

a Ministry of Education Key Laboratory of Cell Activities and Stress Adaptations, School of Life Sciences, Lanzhou University, Lanzhou, Gansu, PR China 730000

b Key Laboratory of Nonferrous Metal Chemistry and Resources Utilization of Gansu Province, Lanzhou University, Lanzhou, Gansu, PR China 730000

c Department of Infectious Diseases and Public Health, Jockey Club College of Veterinary Medicine and Life Sciences, City University of Hong Kong, Kowloon, Hong Kong

*Corresponding Author

# E-mail: chenfj@lzu.edu.cn (F. Chen); xkli@lzu.edu.cn (X. Li)

# Tel: 86-0931-8912561

§These authors contributed equally to this work

Table. S1 Contents of C, N and H elements on the surface of nature wood and WC

| Electrodes | N [%] | C [%] | H [%] |
| --- | --- | --- | --- |
| Nature wood | 0.23 | 48.97 | 5.880 |
| WC | 0.52 | 85.34 | 1.165 |

Table. S2 Materials cost for electrodes

| Chemicals | Purchase link | Price | Dosage | Cost ($) | Reference |
| --- | --- | --- | --- | --- | --- |
| Basswood | https://detail.1688.com/offer/5 27306702834.html | 135 ($/m3) | 6.3*10-6 | 8.5*10-4 | [45] |
| Graphene felt |  | 150 ($/m2) | 7.6*10-4 | ≈0.114 | [46] |

Fig. S1 The characterization of Cr(VI) reduction in different cathodes of MFC.

(a) XPS spectra of survey for carbon felt; (b) XPS spectra of survey for WC; (c) XPS spectra of Cr 2p for carbon felt; (d) XPS spectra of Cr 2p for WC; (e) XPS spectra of O 1s for carbon felt; (f) XPS spectra of O 1s for WC