## Slide 1: Movies for Ordered aqueous structures from liquid-liquid phase separation by supramolecular polymerizations Hailin Fu, Jingyi Huang, Joost J. B. van der Tol, Lu Su, Swayandipta Dey, Peter Zijlstra, Ghislaine Vantomme, Patricia Y. W. Dankers, E. W. Meijer

## Slide 2
Movie S1 | 3D image of multi-layered tactoids in the solution from z-stacking. Solution condition: 1 wt% of UPy-Gly, labelled with 0.02 mol% of UPy-Cy5 (1.8 µM), 1 wt% of dextran, pH = 7.7, PBS x 0.25. The incubating spacer length is 800 μm. The horizontal lines on the tactoids are from the large step size (2 μm) in z-stacking.
Notes: Movie S1

## Slide 3
Movie S2 | Flipping and merging of horizontal/tilted tactoids with those vertical ones at the surfaces. Solution condition: 1 wt% of UPy-Gly, labelled with 0.02 mol% of UPy-Cy5 (1.8 µM), 1 wt% of dextran, pH = 7.7, PBS x 0.25. The time span of the movie starting from the sample preparation is 80 min to 15 hours.
Notes: Movie S2

## Slide 4
Movie S3 | The LLPS of UPy-Gly supramolecular polymers in the PEG/dextran aqueous two-phase solution. Solution condition: 1 wt% of UPy-Gly, 5 wt% of PEG, 5 wt% of dextran, pH = 9, PBS x 0.25. UPy-Gly is labelled with Nile Red (green) and dextran droplet is labelled with dextran-FITC (red). The time span of the movies starting from sample preparation is 3 to 71 hours.
Notes: Movie S3

## Slide 5
Movie S4 | The LLPS of BTA-Glc supramolecular polymers in the PEG/dextran aqueous two-phase solution. Solution condition: 0.22 wt% of BTA-Glc, 0.18 wt% of DPEG, 8 wt% of PEG, 2 wt% of dextran, pH = 9. BTA-Glc is labelled with Nile Red (green) and dextran droplet is labelled with dextran-FITC (red). The time span of the movies starting from sample preparation is 3 to 71 hours.
Notes: Movis S4