Supplementary Material

Rizatriptan benzoate-loaded dissolving microneedle patch for management of acute migraine therapy

Chao Zhong a,b, Xiufeng Zhang c, Zhong Shen c, Yanfang Sun d,*, Yanan Mao a,b, Tianqiu Liu a,b, Rui Wanga,b, Lei Nie e, Amin Shavandi f, Khaydar E. Yunusov g, Guohua Jiang a,b,*

a School of Materials Science and Engineering, Zhejiang Sci-Tech University, Hangzhou, 310018, China

b International Scientific and Technological Cooperation Base of Intelligent Biomaterials and Functional Fibers, Hangzhou, 310018, China

c Department of Coloproctology, Hangzhou Third People’s Hospital, Hangzhou, Zhejiang, 310009, China

d College of Life Sciences and Medicine, Zhejiang Sci-Tech University, Hangzhou, 310018, China

e College of Life Sciences, Xinyang Normal University, Xinyang 464000, China

f Université libre de Bruxelles (ULB), École polytechnique de Bruxelles, 3BIO-BioMatter, Avenue F.D. Roosevelt, 50 - CP 165/61, 1050 Brussels, Belgium

g Institute of Polymer Chemistry and Physics, Uzbekistan Academy of Sciences, Tashkent, 100128, Uzbekistan

E-mail: katherineyfs@zstu.edu.cn (Y. Sun) or ghjiang_cn@zstu.edu.cn (G. Jiang)

Figure S1. UV–Vis spectroscopy of RB for different concentrations in μg/mL.

Figure S2. Schematic illustrations of RB-loaded microneedle fabrication process.

Table S1. Effect of different administration methods on the number of head scratches in rats (X±S)

| group | n | 0-30min | 30-60min | 60-90min | 90-120min | 120-180min | 180-240min |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 4 | 30±2.83** | 36.5±2.12** | 32±5.66** | 32.5±7.78** | 32.5±2.11** | 29.5±0.71** |
| S.C. | 4 | 119.5±2.12** | 97.5±3.54** | 82.5±3.53** | 76±2.82** | 49±5.67** | 39±1.41** |
| MNs | 4 | 121±4.25** | 106.5±2.12** | 83±4.24** | 66±2.83** | 49±2.83** | 38.5±2.12** |
| Oral | 4 | 129±1.41** | 119.5±2.33** | 103.5±2.42** | 90±5.65** | 83±1.41** | 66.5±2.02** |
| Control | 4 | 145.5±3.54 | 130±2.84 | 121±1.43 | 109±1.41 | 96.5±2.12 | 92±2.85 |

Results are presented as the mean±S.E. of at least four experiments. **p<0.001, compared with the control group.

Table S2.  Effect of different administration methods on the number of head scratches in rats (X±S)

| group | n | 0-30min | 30-60min | 60-90min | 90-120min | 120-180min | 180-240min |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 4 | 3.5±2.24** | 2±1.71** | 3.5±0.71** | 3.5±1.41** | 4.5±0.32** | 2.5±0.77** |
| S.C. | 4 | 15±1.24** | 12.5±1.12** | 9.5±1.43** | 8.5±2.11** | 6±1.11** | 3.5±0.43** |
| MNs | 4 | 16.5±1.71** | 12±1.52** | 10.5±1.22** | 9.5±0.53** | 6.5±0.74** | 4.5±0.86** |
| Oral | 4 | 19±1.66** | 17.5±1.77** | 14.5±2.78** | 12.5±2.24** | 13.5±1.65** | 11±1.33** |
| Control | 4 | 27.5±2.76 | 28±2.98 | 26±3.22 | 31±3.12 | 25.5±2.07 | 23±2.08 |

Results are presented as the mean±S.E. of at least four experiments. **p<0.001, compared with the control group.

Table S3. Pharmacokinetic parameters of RB after application via different delivery routes in rats (n = 5).

| Groups | Dose（mg/kg） | Cmax（ng/mL） | Tmax（min） | AUC0-4h（ng/mL·min） |
| --- | --- | --- | --- | --- |
| S.C. | 0.5 | 69.23±4.93 | 60 | 5515.53±819.88 |
| MNs | 0.5 | 65.38±1.17 | 90 | 6114.31±207.82 |
| Oral | 0.5 | 6.27±0.19 | 90 | 571.63±10.74 |

Table S4. 5-HT levels in plasma at different time points in each group of rats (ng/mL, X±S)

| group | n | 5-HT(2h) | 5-HT(4h) |
| --- | --- | --- | --- |
| Blank | 4 | 198.75±1.80 | 199.08±2.75 |
| Control | 4 | 163.52±5.10## | 173.85±3.57## |
| S.C. | 4 | 182.22±2.99** | 191.22±2.64** |
| Oral | 4 | 172.00±5.95* | 180.33±3.90* |
| MNs | 4 | 182.26±2.05** | 187.26±4.63** |

Results are presented as the mean±S.E. of at least four experiments.  ##p<0.001, compared with blank administration. **p<0.001, compared with the control group. *p<0.05, compared with the control group.

Table S5. CGRP levels in plasma at different time points in each group of rats (pg/mL, X±S)

| group | n | CGRP(2h) | CGRP(4h) |
| --- | --- | --- | --- |
| Blank | 4 | 38.18±2.40 | 37.21±2.44 |
| Control | 4 | 84.83±2.24## | 76.92±3.42## |
| S.C. | 4 | 51.44±2.70** | 45.88±1.29** |
| Oral | 4 | 64.95±3.14** | 61.26±3.10** |
| MNs | 4 | 54.57±3.65** | 48.07±3.09** |

Results are presented as the mean±S.E. of at least four experiments. ##p<0.001, compared with blank administration. **p<0.001, compared with the control group.

Table S6. SP levels in plasma at different time points in each group of rats (pg/mL, X±S)

| group | n | SP (2h) | SP (4h) |
| --- | --- | --- | --- |
| Blank | 4 | 6.97±0.46 | 6.42±0.36 |
| Control | 4 | 18.36±1.15## | 16.79±0.61## |
| S.C. | 4 | 10.32±0.40** | 9.32±0.37** |
| Oral | 4 | 14.84±0.40** | 12.78±0.29** |
| MNs | 4 | 10.64±0.99** | 8.62±0.83** |

Results are presented as the mean±S.E. of at least four experiments.  ##p<0.001, compared with blank administration. **p<0.001, compared with the control group.

Table S7 Comparison of c-fos positive cells in brain stem of rats in each group(X±S)

| group | n | Number of positive cells |
| --- | --- | --- |
| Blank | 4 | 4.87±1.36* |
| Control | 4 | 24.24±4.32 |
| Oral | 4 | 16.77±2.84* |
| S.C. | 4 | 9.43±4.29* |
| MNs | 4 | 12.11±3.66* |

Results are presented as the mean±S.E. of at least four experiments. *p<0.05, compared with the control group.