Supplementary Information

A facile and on-demand optimizing strategy for polyurethane elastomers via programmable hydrogen bonding

Zichen Bai1, Xiaodong Li1, Tianhao Wu1, Hao Jiang1, Xudong Zhang2, Lichen Zhang1, Yi Yang1, Shuang Liu1, Lisha Lei1, Ningning Song1, Zhengdi Wang1, Xing Su1* and Meishuai Zou1*

1 School of Materials Science and Engineering, Beijing Institute of Technology, No. 5 South Zhongguancun Street, Haidian District, Beijing, 100081, China

2 Shandong AOZO New Materials Co., Ltd., Tengzhou, 277524, China

* Corresponding authors: Xing Su and Meishuai Zou

Corresponding authors’ e-mail: sx1020@126.com (X. Su),

zoums@bit.edu.cn (M. Zou).

Figure S1 The synthesis and microstructure of the polyurethane matrix (PUE)

Figure S2 FTIR spectra of PUE, TA/PUE, 70-48-TA/PUE, EG/PUE, 70-48-EG/PUE samples at the wavelength between 4000 to 600 cm-1.

Figure S3 The SEM images of the cross-sectional area for (a) EG/PUE, (b) 70-48-EG/PUE, (c) TA/PUE, (d) 70-48-TA/PUE.

Figure S4 The representative stress-strain curves for PUE and PUE soaked in THF solution for 12 h.

Figure S5 The representative stress-strain curves of EG/PUE , 70-48-EG/PUE, the half concentration of polyphenol solution treated EG/PUE and the half concentration of polyphenol solution treated 70-48-EG/PUE.

Figure S6 The SEM images of (a) 40-48-TA/PUE, (b) 50-48-TA/PUE, (c) 60-48-TA/PUE, (d) 70-48-TA/PUE, (e) 40-48-EG/PUE, (f) 50-48-EG/PUE, (g) 60-48-EG/PUE, (h) 70-48-EG/PUE, (i) EG/PUE, (j) 70-1-EG/PUE, (k) 70-9-EG/PUE, (l) 70-18-EG/PUE, (m) TA/PUE, (n) 70-1-TA/PUE, (o) 70-9-TA/PUE, (p) 70-18-TA/PUE

Figure S7 The representative stress-strain curves of PUE samples treated under different temperature(25, 50, 70 ℃) for a period of 48 h

Figure S8 The representative stress-strain curves of PUE, EG/PUE, 70-48-EG/PUE, 254-8@70-48-EG/PUE and 254-8@70-48-EG/PUE soaked in THF solution for 24 h.

Figure S9 The representative stress-strain curves of EG/PUE, 50-48-EG/PUE, 70-48-EG/PUE and 70-72-EG/PUE samples, which indicates the greatest heat treatment temperature.

Figure S10 The DMA curves (tanσ, Y-axis: damping factor) of PUE, TA/PUE, 70-48-TA/PUE, EG/PUE and 70-48-EG/PUE.

Figure S11 A typical stress-strain curve of polyphenol/PUE sample after a self-healing period for only 15 s.

Figure S12 The FTIR spectra of (a) EG/PUE, 70-48-EG/PUE, 254-8-70-48-EG/PUE, 365-8-70-48-EG/PUE samples and 365-8-70-48-EG/PU soaked in THF solution for 24 h samples at the wavelength between 4000 to 500 cm-1. The FTIR spectra of 70-48-EG/PUE exposed under UV radiation for 0 h, 0.5 h, 1 h, 4 h, 9 h under the UV wavelength of (b) 254 nm, (c) 365 nm.

Figure S13 The representative stress-strain curves of heated samples radiated under the different wavelength of ultraviolet light for a period of time (0, 0.5, 1, 4, 9, 18 h): (a) 70-48-EG/PUE under 254 nm, (b) 70-48-EG/PUE under 365 nm, (c) 70-48-TA/PUE under 254 nm, (d) 70-48-TA/PUE under 365 nm

Figure S14 A representative stress-strain curve of PUE samples treated with UV radiation at wavelength of 254 or 365 nm.

Figure S15 The DMA curves (tanσ, Y-axis: damping factor) of (a) 70-48-EG/PUE samples radiated ultraviolet light for a period of time(0.5, 1, 4 h), (b) 70-48-TA/PUE samples radiated ultraviolet light for a period of time(0.5, 1, 4 h).

Figure S16 The FESEM images of EG/PUE samples before and after the UV radiation process. The size of polyphenol aggregates were hardly changed before and after UV radiation.

Figure S17 TA/PUE samples were soaked in solutions with different pH environment (a) pH= 12.38, (b) pH= 7.81, (c) pH= 6.97, (d) pH= 5.31, (e) pH= 1.09, which indicated the strong alkaline environment was able to remove polyphenols from the polyphenol/PUE systems.

Figure S18 A representative stress-strain curve for PUE samples soaked in deionized water for a week

Figure S19 The image of bacteriostatic zones formed by EG/PUE, 70-48-EG/PUE, TA/PUE, 70-48-TA/PUE and empty group samples in (a) E.coil environment, (b) S.aureus environment, where D is diameter of bacteriostatic zone. The diameters of the tested samples mentioned in our work is 6 mm.

Figure S20 The image of spread plate method by soaking EG/PUE, 70-48-EG/PUE and empty group in (a) E.coil environment, (b) S.aureus environment with different concentrations (×1, ×10, ×100 or ×1000).

| Sample | pH=12.38 | pH=7.81 | Deionized water(pH=6.97) |
| --- | --- | --- | --- |
| Average mass change fraction of TA/PUE (%) | 7.89 (±1.12) | 3.00 (±1.12) | 1.71 (±1.12) |
| Average mass change fraction of EG/PUE (%) | 3.83 (±0.25) | 1.20 (±1.18) | 0.27 (±0.03) |

| Sample | Deionized water(pH=6.97) | pH=5.31 | pH=1.09 |
| --- | --- | --- | --- |
| Average mass change fraction of TA/PUE (%) | 1.71 (±1.12) | 1.93 (±0.13) | 2.31 (±0.18) |
| Average mass change fraction of EG/PUE (%) | 0.27 (±0.03) | 0.97(±0.01) | 0.29 (±0.10) |

Table S1 The average results of the mass change of TA/PUE and EG/PUE samples soaked in the solution at different pH values for a week.

| Sample | Average percentage of polyphenol (%) |
| --- | --- |
| TA/PUE | 12.21 |
| EG/PUE | 21.54 |

Table S2 The results of mass content for polyphenols inside polyphenol/PUE samples by soaking PUE samples in saturated solution of polyphenols.

| Sample | Element content of Na (%) |
| --- | --- |
| Diffused TA sodium salt from TA/PUE (pH=8) | 2.63 |
| Diffused EG sodium salt from EG/PUE (pH=8) | 0.73 |

Table S3 The element content of Na in the TA/EG sodium salts (pH=8) by ICP equipment.