Use of structureding of me systems as a strategy to minimize the deactivation of Ni-based catalysts applied in dry reformthane

Table  S1 - Fitted parameters of MDAR 1 for the different spatial velocities of the Ni/La-Al structured catalyst, at CH4:CO2= 4 ratio, in the deactivation curves.

| WHSV (L·h-1·gcat-1) | RMSE | R² | Fstatistic | p_value |
| --- | --- | --- | --- | --- |
| 20 | 0,0047 | 0,9754 | 0,0740 | 0,0588 |
|  | d | as | φdmin-1 |  |
|  | 0,9075 ± 0,1535 | 0,4449 ± 0,0096 | 0,0085 ± 0,0014 |  |
| 30 | RMSE | R² | Fstatistic | p_value |
|  | 0,0068 | 0,9723 | 0,1288 | 0,1021 |
|  | d | as | φdmin-1 |  |
|  | 0,9209 ± 0,1704 | 0,4184 ± 0,0109 | 0,0103± 0,0021 |  |
| 40 | RMSE | R² | Fstatistic | p_value |
|  | 0,0081 | 0,9663 | 0,0855 | 0,0675 |
|  | d | as | φdmin-1 |  |
|  | 1,5199 ± 0,3227 | 0,3262 ± 0,0311 | 0,0153 ± 0,0031 |  |

Table S2 - Fitted parameters of MDAR 2 for the different spatial velocities of the Ni/La-Al structured catalyst, at CH4:CO2= 4 ratio, in the deactivation curves.

| WHSV (L·h-1·gcat-1) | RMSE | R² | Fstatistic |  | p_value |
| --- | --- | --- | --- | --- | --- |
| 20 | 0,0057 | 0,9657 | 0,0705 |  | 0,0560 |
|  | d | ds | φdmin-1 | φsmin-1 |  |
|  | 0,8753 ± 0,2134 | 0,8752 ± 0,2133 | 96,4852 ± 39,2015 | 96,4797 ± 39,2010 |  |
| 30 | RMSE | R² | Fstatistic |  | p_value |
|  | 0,0077 | 0,9633 | 0,1241 |  | 0,0984 |
|  | d | ds | φdmin-1 | φsmin-1 |  |
|  | 0,8095 ± 0,3136 | 0,8094 ± 0,3134 | 90,6977 ± 42,8974 | 90,690 ± 42,8979 |  |
| 40 | RMSE | R² | Fstatistic |  | p_value |
|  | 0,0090 | 0,9556 | 0,0732 |  | 0,0581 |
|  | d | ds | φdmin-1 | φsmin-1 |  |
|  | 0,9754 ± 0,1785 | 0,9753 ± 0,1784 | 106,2632 ± 39,6489 | 106,256 ± 39,648 |  |