High temperature dielectric breakdown and energy storage properties of polyetherimide nanocomposites improved by hindering molecular motion

Lingyu Yang · Daomin Min* · Ziwei Gao · Liuqing Yang · Yuanwei Zhu · Wenfeng Liu *

State Key Laboratory of Electrical Insulation and Power Equipment, Xi’an Jiaotong University, Xi’an 710049, Shaanxi, China;

*Corresponding Author: forrestmin@foxmail.com (D. M.); liuwenfeng@xjtu.edu.cn (W. L.)

Declarations of interest: none

Fig S1	a Relationship between the logarithm of the Meyer-Neldel equation prefactor σ0 and activation energy EA. b Relationship between electrical conductivity of PEI PNCs and inverse of temperature at 100 kV/mm (dots are experimental results, lines are fitted results of the Meyer-Neldel equation). c Relationship between the electrical conductivity of PEI PNCs and the inverse of temperature at 100 kV/mm (dots are experimental results, lines are fitting results of the Arrhenius equation)

Fig S2	a Changes in glass transition temperatures and electrical conductivities. b Changes in glass transition temperatures and breakdown strength. c Changes in activation energies and breakdown strength

Fig S3	a Schematic diagram of the charge transport and molecular displacement modulated (CTMD) model. b Waveform diagram with a constant voltage applied. c Waveform diagram of an applied ramp voltage

Fig S4	Steady-state current density of a pure PEI, b PEI/Al2O3-1wt%, c PEI/Al2O3-3wt%, d PEI/Al2O3-5wt% and e PEI/Al2O3-7wt% under different electric fields at different temperatures (Dots are experimental results and lines are fitted curves for the hopping conductivity equation). (f) Changes in hopping distance of PEI PNCs with temperature

Fig S5	Distribution of internal temperature and molecular displacement of PEI/Al2O3-1wt% during step-up until breakdown at a 25°C, b 100°C and c 200°C

Fig S6	Distribution of internal temperature and molecular displacement of PEI/Al2O3-5wt% during step-up until breakdown at a 25°C, b 100°C and c 200°C

Fig S7	Distribution of internal temperature and molecular displacement of PEI/Al2O3-7wt% during step-up until breakdown at a 25°C, b 100°C and c 200°C

Fig S8	Experimental results of the Weibull distribution of breakdown strength for a pure PEI, b PEI/Al2O3-1wt%, c PEI/Al2O3-3wt%, d PEI/Al2O3-5wt% and e PEI/Al2O3-7wt% at different temperatures (f) Changes in Weibull shape parameters for PEI PNCs with temperature

Fig S9	Weibull distribution of breakdown strength with varying variance of a hopping potential, b hopping distance, c prefactor of molecular segment displacement, d power exponent and e characteristic temperature. f Changes in Weibull shape parameters with variance of random variables at 140°C

Underlying logic of charge transport and molecular displacement modulated (CTMD) model

1	Bipolar charge transport and heat transport processes

Under the applied electric field, the electron current density jin(e) and hole current density jin(h) injected by the electrodes into the dielectric are expressed as follows

where A is the Richardson constant; T is the temperature; uin(e) is the potential barrier at the cathode-dielectric interface; uin(h)is the potential barrier at the anode-dielectric interface; kB is the Boltzmann constant; usch is the Schottky barrier reduction; t is the time of applied electrical field and d is the thickness of the specimen The equation for the Schottky barrier reduction is usch=(eE/4πε0εr)1/2, where e is the electron charge; E is the electric field inside the dielectric; ε0 and εr are the vacuum permittivity and relative permittivity of the dielectric, respectively

The carrier mobility in the dielectric is obtained using a double-barrier hopping conduction transport model

where v(e) and v(h) are the electron and hole mobility; uhop(e) and uhop(h) are the hopping barriers of electrons and holes respectively; λhop(e) and λhop(h) are the average hopping distance of electrons and holes respectively; x represents the position in the dielectric; υ0 is the attempted escape frequency of carriers The carrier mobility is obtained by dividing the carrier mobility by the electric field, μ(e,h)=v(e,h)/E

The current density formed by carrier drift and diffusion is expressed as

where jC(e) and jC(h) are the conduction current density of electrons and holes, respectively; nM(e) and nM(h) are the electron and hole density, respectively; D(e) and D(h) are the diffusion rates of electrons and holes, respectively By Einstein's law we can obtain D(e,h)=μ(e,h)kBT/e

The charge conservation equation considering the charge recombination processes is expressed as

where RMe,Mh is the recombination coefficient between electrons and holes, RMe,Mh=e(μ(e)+μ(h))/ε0εr

As space charges accumulate in the dielectric, the potential and electric field can be calculated by the Poisson's equation

The relationship between electric field and potential is expressed as E=-, from which the electric field distribution in the dielectric can be calculated

The current density inside the dielectric increases dramatically at high electric fields and the high currents generate large joules heat, resulting in an increase in the internal temperature of the dielectric When the temperature gradient is generated inside the dielectric, the heat transfer occurs driven by a temperature gradient Using the Fourier heat conduction equation to describe the temperature change inside the dielectric

where ρ is the density of the dielectric; cM is the massic heat capacity of the dielectric; κ is the thermal conductivity of the dielectric

2	Breakdown process of Polyetherimide nanocomposites (PEI PNCs)

The molecular segment motion inside the PEI PNCs at high temperatures causes the distance of molecular chains to increase The distance of molecular chains λT is proportional to the linear expansion coefficient αf(L), the length of molecular chain LM, and the temperature T, expressed as

PEI PNCs may be destroyed when the temperature is above a critic temperature Tc The distance of molecular chains λc when damage occurs is proportional to the critic temperature Tc, expressed as:

Under the combined influence of electric field and temperature, the molecular chains of PEI PNCs undergo directional motion, resulting in an increase in the distance of molecular chains in the local areas Superimposing the distance of local molecular chains λE due to Coulomb forces with the distance of molecular chains λT due to heat, and assuming that the dielectric is broken down when the distance of molecular chains reaches the size at the critic temperature Tc, we obtain the breakdown criterion expressed as

Substituting equation  and equation  into equation , the expression for the distance of local molecular chains λE due to Coulomb forces at breakdown can be obtained as

The diffusion coefficient of molecular chains DMol is directly proportional to the temperature T and inversely proportional to the friction coefficient ξt between molecular chains, expressed as DMol=kBTξt The friction coefficient between molecular chains ξt reflects the strength of the intermolecular chain interactions in the polymer The stronger the intermolecular chain interactions, the higher the friction coefficient between molecular chains and the greater the energy required for the relative displacement of the molecular chains to occur Moreover, the relationship between the molecular mobility μMol under Coulomb forces and the diffusion coefficient of molecular chains DMol can be obtained from Einstien's equation, μMol=DMole/kBT This gives μMol=e/ξt This shows that the molecular mobility is independent of temperature The molecular mobility is mainly related to the friction coefficient between molecular chains or the interactions between molecular chains The stronger the intermolecular chain interactions, the higher the friction coefficient between molecular chains and the lower the molecular mobility

The product of the molecular mobility and the electric field under Coulomb forces is the rate of molecular chain motion The integration of the rate of molecular chain motion with respect to time obtains the molecular displacement, expressed as

Substituting equation  into the breakdown criterion equation , the breakdown criterion can be expressed as

In order to reduce the number of independent variables in the breakdown model, μMol/LM is defined as a new variable μ'Mol, representing the mobility of individual molecular segments This allows the breakdown criterion to be deformed as follows

It is assumed that the molecular mobility or individual molecular segment mobility is a power function of the electric field, μ'Mol=μ'Mol0Eβ where  is the exponent of the power function Substituting this into equation , the following breakdown criterion can be obtained:

A large amount of space charges will accumulate inside the dielectric under high electric fields, and distort the electric field This results in different displacements of the molecular segments at different locations The molecular segment displacements are large where the electric field is high, and small where the electric field is low Dielectric breakdown occurs at the maximum molecular segment displacement Therefore, dielectric breakdown occurs when the maximum molecular segment displacement is such that the criterion of equation  holds

3	Approximate analytical expression for the breakdown strength when the molecular mobility is independent of the electric field

The electric field E is equal to the applied voltage V divided by the thickness of the specimen d As it is a ramp voltage with a constant ramp rate, the ramp rate is kramp and the time of applied voltage is t The voltage on the specimen can be expressed as the ramp rate multiplied by the time of the applied voltage, which is V =krampt The molecular segment displacement is expressed as

The electric field can be expressed as E = krampt/d and by substituting the expression for the electric field into equation  we get:

Integrating both sides of equation  and considering the initial condition that the molecular segment displacements are 0 when no voltage is applied, we get:

Then substituting t=Ed/kramp into equation  we can obtain the relationship between the molecular segment displacements and the electric field

distance of individual molecular segments moving and the electric field

Substituting the distance expression  for the molecular segment displacements into the breakdown criterion equation  for the combined effect of electric field and heat, we get:

Expressing the macroscopic average electric field as V/d and considering the breakdown critical condition, the breakdown voltage expression can be obtained as

Without considering the distortion of the electric field caused by the space charges, the expression for the breakdown strength can be obtained as

The breakdown strength expression , derived from the pathway of breakdown due to the molecular segment displacements under the action of Coulomb forces, can uniformly explain the influencing mechanism of specimen thickness, temperature, ramp-up rate, nano-doping and pressure on the breakdown properties of PEI PNCs

- Equation  shows that the breakdown strength Eb is an inverse power function of the specimen thickness d, with a power exponent equal to -05 This is consistent with the experimental results that the breakdown strength is an inverse power function of the specimen thickness

- The breakdown strength Eb is positively correlated with the ramp-up rate kramp05 The faster the ramp-up rate, the higher the breakdown strength

- The higher the temperature T, the progressively lower the breakdown strength Eb, and the higher the temperature T, the faster the breakdown strength Eb decreases, which is in line with the experimental results seen now

- Substituting the molecular mobility expression into the breakdown strength expression , we get:

where ξt is the friction coefficient of individual molecular segments or the strength of the interactions of individual molecular segments by surrounding molecular chains, ξt=ξt/N The higher the ξt, the more difficult it is for molecular segments to move and the higher the breakdown strength Eb will be The main factors contributing to the increase in the ξt are the molecular weight and the interactions between the molecular chains Obviously, the higher the molecular weight, the more difficult it is for molecular segments to move and the higher the breakdown strength of the polymer The greater the intermolecular chain interactions, the greater the ξt and the higher the breakdown strength of the polymer probably

4	Analytic equation for breakdown strength when molecular mobility is a power function of electric field

Assuming that the molecular mobility or the individual molecular segment mobility is a power function of the electric field

where  is the exponent of the power function

The molecular segment displacements are expressed as

Substituting E= krampt/d into equation , we get:

Integrating both sides of equation  and considering the initial condition that the molecular segment displacements are 0 when no voltage is applied, we get:

Then substituting t=Ed/kramp into equation  we can obtain the relationship between the molecular segment displacements and the electric field

Combining the analytical equation  for the molecular segment displacements under Coulomb forces with the breakdown criterion equation , we get:

From equation , we can obtain the analytical formula for the breakdown strength when the molecular mobility is a power function of the electric field

The breakdown strength expression , derived from the pathway of breakdown due to the molecular segment displacements under the action of Coulomb forces, can uniformly explain the influencing mechanism of specimen thickness, temperature, ramp-up rate, nano-doping and pressure on the breakdown properties of PEI PNCs

- Equation  shows that the breakdown strength Eb is an inverse power function of the specimen thickness d, with a power exponent equal to -1/(+2) This is consistent with the experimental results that the breakdown strength is an inverse power function of the specimen thickness

- The breakdown strength Eb is positively correlated with the ramp-up rate kramp1/(+2) The faster the ramp-up rate, the higher the breakdown strength

- The higher the temperature T, the progressively lower the breakdown strength Eb, and the higher the temperature T, the faster the breakdown strength Eb decreases, which is in line with the experimental results seen now

- Assuming that the friction coefficient of individual molecular segments is an inverse power function of the electric field, ξt=ξt0E- Then Mol0=e/ξt0 can be obtained substituting Mol0=e/ξt0 into the breakdown strength expression , we get

An appropriate nanoparticle content can hinder the movement of molecular chains in PEI PNCs, leading to enhanced interactions between molecular chains or an increase in the friction coefficient between molecular chains ξt According to equation , the breakdown field strength and its temperature stability are improved The enhanced intermolecular chain interactions in the interface region also result in a reduction in the number of weakly bound molecular chain segments The enhanced intermolecular chain interactions in the interface regions also result in a reduction in the number of weakly bound molecular segments This reduces the probability of breakdown due to the slip of molecular segments, resulting in a larger shape parameter for the Weibull distribution