Supporting Information

A Highly Efficient Open-shell Singlet Luminescent Diradical with Strong Magnetoluminescence Properties

Alim Abdurahman,†[1]* Li Shen,†[2] Jingmin Wang,†[3] Meiling Niu,[3] Ping Li,[4] Qiming Peng,[3]* Jianpu Wang,[3] Geyu Lu[1]*

1 State Key Laboratory of Integrated Optoelectronics, College of Electronic Science and Engineering, Jilin University, Qianjin Avenue 2699, Changchun, 130012, P. R. China

2 College of Chemical Engineering and Environmental Chemistry, Weifang University, Weifang, 261061, P. R. China.

3 Key Laboratory of Flexible Electronics (KLOFE) & Institute of Advanced Materials (IAM), Jiangsu National Synergetic Innovation Center for Advanced Materials (SICAM), Nanjing Tech University (NanjingTech), 30 South Puzhu Road, Nanjing 211816, P. R. China.

4 Key Laboratory for Organic Electronics and Information Displays & Institute of Advanced Materials (IAM) National Synergistic Innovation Center for Advanced Materials (SICAM)

Nanjing University of Posts & Telecommunications, 9 Wenyuan Road, Nanjing, 210023, P. R. China

† These authors contributed equally to this work.

* Authors to whom correspondence should be addressed;

alim@jlu.edu.cn (Alim Abdurahman); iamqmpeng@njtech.edu.cn (Qiming Peng); Lugy@jlu.edu.cn (Geyu Lu)

Contents

S1. Theoretical calculations of radicals

S2. Material synthesis and characterisation

S3. Crystallographic data of DR1

S4. Magnetic susceptibility measurements of DR1

S5. Electron paramagnetic resonance (EPR) spectra of TTM, TTM-1Cz and DR1

S6. Summary of photophysical properties for TTM, TTM-1Cz and DR1 in different solvents

S7. The influence of doping concentration and temperature of DR1 (in PMMA) on photoluminescence

S8. Stabilitiy of TTM, TTM-1Cz and DR1

S9. Electroluminescence properties of DR1-based OLED

S10. ML properties of DR1 and TTM-1Cz.

S1. Theoretical calculations of radicals

Computational details

All these calculations were performed with the Gaussian 16 program package.[1] The geometries of all compounds were optimized as open-shell (OS) singlets by the spin- unrestricted broken-symmetry (BS) approach at the UB3LYP/6-31G**[2-3] theoretical level. This approach has been shown to provide reliable geometries and energies for singlet-state diradicals. Then these compounds were optimized as closed-shell (CS) singlets and thermally excited triplet (Tt) states at the (U)B3LYP/6-31G** level, respectively. All optimized geometries were confirmed to be local minima by vibrational analysis. The OS structures were shown to be the stable structures. ΔE(OS-CS) and ΔE(OS-Tt) were calculated as the energy differences between OS structure and CS structure, Tt structure, respectively.

Diradical character were determined using two different descriptors: (1) diradical character y0. It ranges from y0 = 0 (pure closed-shell) to y0 =1 (pure diradical), and calculated from the occupation numbers of natural orbitals using the spin-projected B3LYP/6-31G** level of theory as proposed by Yamaguchi.[4] The parameters are obtained by the following equation:

y0=1-2Ti1+Ti2 (1)

Where Ti represents the orbital overlap between the corresponding orbitals. It is expressed in the terms of the occupation numbers (ni) of the UB3LYP/6-31G** natural orbitals (UNO) as

Ti=nHONO-i-nLUNO+i2 (2)

and i= 0, 1, 2 …….. (2) the Fractional occupation number weighted density (FOD) analysis was used as a quantitate description of the open-shell singlet diradical character of these compounds. The number of hot electrons, NFOD were calculated at the FT-B3LYP/6-31G** level at a default electronic temperature (Tel) of 9000 K. The calculations were performed using the ORCA 5.0.3 program.[5]

Vertical electronic excitations were computed by using the time-dependent DFT (TD-DFT) approach. The excitation energies were calculated at UB3LYP/6-31G** level by using the OS and T1 geometries. In addition, the excitation characters were analysed with hole-electron analysis [6] by Multiwfn program,[7] and the corresponding results were visualized by VMD programs.[8]

Fig. S1. Frontier orbitals of previously reported luminescent diradical TTM-PhTTM9 in open-shell singlet (OS) ground state a) and thermally excited triplet (Tt) state b) calculated by DFT methods (UB3LYP/6-31G (d,p)).

Table S1. Diradical character y0, ΔES-T, ΔEOS-Tt and ΔEOS-CS of the four designed diradicals.

| Diradical | y0 | NFOD | ΔEOS-Tt (kcal mol-1) | ΔEOS-CS (kcal mol-1) |
| --- | --- | --- | --- | --- |
| DR1 | 0.947 | 3.50 | -0.022 | -20.39 |
| DR2 | 0.948 | 3.67 | -0.030 | -20.64 |
| DR3 | 0.972 | 3.67 | -0.008 | -21.58 |
| DR4 | 0.990 | 3.53 | 0.004 | -21.88 |

Fig. S2. Spin density distributions (isovalue 0.0015) (up panels), Frontier orbitals (down panels) of DR1 in open-shell singlet (OS) ground state a) and thermally excited triplet (Tt) state b) calculated by DFT methods (UB3LYP/6-31G (d,p)).

Fig. S3. Spin density distributions (isovalue 0.0015) (up panels), Frontier orbitals (down panels) of DR2 in open-shell singlet (OS) ground state a) and thermally excited triplet (Tt) state b) calculated by DFT methods (UB3LYP/6-31G (d,p)).

Fig. S4. Spin density distributions (isovalue 0.0015) (up panels), Frontier orbitals (down panels) of DR3 in open-shell singlet (OS) ground state a) and thermally excited triplet (Tt) state b) calculated by DFT methods (UB3LYP/6-31G (d,p)).

Fig. S5. Spin density distributions (isovalue 0.0015) (up panels), Frontier orbitals (down panels) of DR4 in open-shell singlet (OS) ground state a) and thermally excited triplet (Tt) state b) calculated by DFT methods (UB3LYP/6-31G (d,p)).

Fig. S6. Frontier orbitals of TTM (a) and TTM-1Cz (b) calculated by DFT methods (UB3LYP/6-31G (d,p)).

Table S2. Summary of selected calculated excitation energies, oscillator strength and contributions of major electronic transitions of mono-radical and diradicals.

|  | Transition | Wavelength (nm) | Energry/ (eV) | Osc.Strength () | Major Contribution |
| --- | --- | --- | --- | --- | --- |
| TTM | D0→D | 466.95 | 2.6552 | 0.0223 | 136 B →137 B |
| TTM-1Cz | D0→D | 662.12 | 1.8725 | 0.0830 | 171 B→172 B |
| DR1 | OS | 737.73 | 1.6806 | 0.0510 | 299 B→ 300 B |
|  |  | 604.00 | 2.0527 | 0.1380 | 299 A→ 300 A |
|  | Tt | 638.95 | 1.9404 | 0.1226 | 298 B→ 299 B |
| DR2 | OS | 636.30 | 1.9485 | 0.0008 | 319 B→ 320 B (or 319 A→ 320 A) |
|  |  | 628.03 | 1.9742 | 0.1939 | 319 A→ 320 A (or 319 B→ 320 B) |
|  | Tt | 574.89 | 2.1567 | 0.0009 | 318 B→ 319 B |
| DR3 | OS | 649.44 | 1.9091 | 0.0674 | 319 A→ 320 A (or 319 A→ 320 A) |
|  |  | 649.00 | 1.9104 | 0.0162 | 319 B→ 320 B (or 319 A→ 320 A) |
|  | Tt | 593.65 | 2.0885 | 0.1656 | 318 B→ 319 B |
| DR4 | OS | 709.25 | 1.7481 | 0.0006 | 299 B→ 300 B |
|  |  | 607.01 | 2.0425 | 0.0013 | 299 A→ 300 A |
|  | Tt | 620.22 | 1.9990 | 0.0730 | 298 B→ 299 B |

Fig. S7. Hole-electron analysis of the lower charge transfer state transition based on OS state of DR1-DR4 (isovalue = 0.001 a.u.).

Fig. S8. The fragment definition (up penals) and heat map of the second excited state transition based on OS state (down panels) of the four designed diradicals.

Table S3. The relevant index of low-lying charge transfer state of DR1-DR4 based on electron-hole analysis.

|  | DR1 | DR2 | DR3 | DR4 |
| --- | --- | --- | --- | --- |
| Sr(a.u.) | 0.518 | 0.870 | 0.832 | 0.099 |
| D(Å) | 7.812 | 0.461 | 2.091 | 9.425 |

S2. Materials synthesis and characterisation

General: All chemical agents and solvents, unless otherwise stated, were purchased from commercial suppliers and used directly without further purification. Tetrahydrofuran (THF) was distilled before used. Column chromatography was performed with silica gel (200-300 mesh).

The 1H nuclear magnetic resonance (NMR) spectra were recorded in (Methyl sulfoxide)-d6 (d6-DMSO) on a Bruker Avance-III 500 NMR spectrometer at ambient temperature. GC-MS mass spectra were recorded on a Thermo Fisher ITQ1100 mass spectrometer. MALDI-TOF mass spectra were recorded on a Bruker Autoflex speed TOF/TOF mass spectrometer with DCTB as a matrix. EPR spectra were recorded on a Bruker ELEXSYS-II E500 CW-EPR spectrometer. Thermal gravimetric analysis (TGA) curves were obtained on the Pyris1 TGA thermal analysis system at a heating rate of 20°C min−1 in a nitrogen atmosphere. Elemental analysis was conducted by an Elementar vario MICRO cube instrument. Ultraviolet-visible (UV-Vis) and photoluminescence (PL) spectra of the radicals were recorded on a Shimadzu UV-2550 spectrophotometer and a Shimadzu 5301PC spectrophotometer. Intensity of luminescence at 654 nm (for DR1), 564 nm (for TTM) and 628 nm (for TTM-1Cz) were monitored exciting at 370 nm light (excitation slit was 20 nm, and shutter control was off). The relative PLQYs were measured using a Shimadzu UV-2550 spectrophotometer and Edinburgh fluorescence spectrometer (FLS980). The fluorescence lifetimes were measured with FLS980.

Single crystal X-ray diffraction data of DR1 was collected using a synchrotron X-ray source at the Shanghai Synchrotron Radiation Facility. The crystal structure was determined by direct methods, and further refined by the full matrix least squares method of F2 using the SHELX-97 and Olex-2.

Magnetic measurements were performed on a Quantum Design 6.5 Tesla SQUID-VSM system with a temperature range of 2 to 300 K and an applied field of 1000 Oe. Powder sample of DR1 with a weight of 5-10 mg was sealed in a plastic capsule. Magnetic moment was measured in the temperature range of 2 to 300 K. After correction of diamagnetic contributions from the sample, using tabulated constants, sample holder and paramagnetic contamination, the magnetic data were fitted with Bleaney-Bowers equation.[10]

The temperature-dependent PL spectra of the radicals were measured using a spectrometer (Ocean Optics QE65 Pro) and a Spectromag PT liquid helium free superconducting magneto-optical system (Oxford Instuments NanoScience) was used to provide different temperatures with 2~300 K and magnetic fields from 0 to 7 T.

The intermediate 2(HTTM), mono-radical TTM and TTM-1Cz are prepared according to our previous report. [11, 12]

Synthesis of 3. Under argon atmosphere, HTTM (1.0 g, 1.8 mmol), 3-(4,4,5,5-tetraMethyl-1,3,2-dioxaborolan-2-yl)-carbazole (0.52 g, 1.8 mmol) and Pd(PPh3)4 (0.104 g, 0.09 mmol) were mixed in a 100 ml round-bottom flask containing toluene (12 ml), K3PO4 aqueous solution (8 ml, 2 M), and ethanol (4 ml), the mixture was refluxed at 90℃ for 48 h. After the reaction mixture cooling to room temperature, the mixture was extracted with dichloromethane. The organic layer was dried over anhydrous MgSO4. The crude product was purified by silica gel column chromatography (dichloromethane: petroleum =1:4) to obtain 3 as white powder with 44% yield. GC-MS (m/z): [M]+ Calcd for C31H15Cl8N：685.07, Found, 685.33. 1H  NMR (500 MHz, DMSO) δ 11.42 (s, 1H), 8.65 (d, J = 7.9 Hz, 1H), 8.26 (d, J = 7.9 Hz,1H), 7.99 (d, J = 2.0 Hz, 1H), 7.86-7.78 (m, 4H), 7.62 (dd, J = 4.4, 2.2 Hz, 2H), 7.55 (d, J=8.5 Hz,1H), 7.51 (d, J = 8.1 Hz,1H), 7.44-7.39 (m, 1H), 7.20 (t, J = 7.4 Hz, 1H), 6.73 (s, 1H).

Synthesis of 4. A mixture of TTM (0.50 g, 0.90 mmol), 3 (0.60 g, 0.90 mmol), anhydrous Cs2CO3 (0.90 g, 2.80 mmol) and DMF (30 ml) was stirred at 160℃ for 12 h under argon atmosphere and dark conditions. After the reaction mixture cooled to room temperature, it was poured into (1 M) hydrochloric acid solution; the precipitate was filtered and washed with water three times. The crude product was dissolved in dichloromethane and extracted with water and dichloromethane. The organic layer was dried over MgSO4, and evaporated under vacuum. The crude product was purified by silica gel column chromatography (dichloromethane: petroleum =1:3) to obtain 4 with 40% yield. MALDI-TOF (m/z): [M] Calcd for C50H21Cl16N:1202.93; Found, 1202.11. 1H NMR (500 MHz, DMSO) δ 8.81 (s, 1H), 8.41 (d, J = 7.8 Hz, 1H), 8.01 (d, J = 13.7 Hz, 2H), 7.93 (d, J = 9.5 Hz, 1H), 7.84 (dd, J = 18.8, 7.9 Hz, 5H), 7.78 (s, 1H), 7.68 (s, 1H), 7.66 – 7.61 (m, 3H), 7.53 (d, J = 7.5 Hz, 1H), 7.48 (d, J = 8.7 Hz, 1H), 7.44 (d, J = 8.1 Hz, 1H), 7.40 – 7.37 (m, 1H), 6.82 (s, 1H), 6.74 (s, 1H).

Synthesis of DR1. Under argon atmosphere and in the dark, the KOtBu (0.31 g, 2.8 mmol) was added to the solution of 4 (0.30 g, 0.25 mmol) in dry THF and the solution acquired a light red colour. The solution was stirred for 12 h at room temperature, and then the 2,3,5,6-tetrachloro-p-benzoquinone (0.76 g, 3.1 mmol) was added. The solution was stirred for another 3 h. after the reaction finished, the solvent was removed under vacuum and further purified by silica gel column chromatography (dichloromethane: petroleum =1:2) to obtain DR1 as deep green solid 0.18g (61%). MALDI-TOF (m/z): [M] Calculated for C50H19Cl16N:1200.91; Found, 1200.29. Elem. Anal. Calculated for C50H19Cl16N: C 50.01, H 1.59, N 1.17. Found, C 50.16, H 1.76, N 1.21.

S3. Crystallographic data of DR1

Table S4 X-Ray Crystallographic Data of DR1

| CCDC | 2252807 |
| --- | --- |
| Identification code Empirical formula | DR1 C50H19Cl16N |
| Formula weight | 1200.86 |
| Temperature/K | 273.15 |
| Crystal system | monoclinic |
| Space group | P21/c |
| a/Å | 25.3440(16) |
| b/Å | 8.4097(5) |
| c/Å | 26.7278(16) |
| α/° | 90 |
| β/° | 108.058(2) |
| γ/° | 90 |
| Volume/Å3 | 5416.0(6) |
| Z | 4 |
| ρcalcg/cm3 | 1.473 |
| μ/mm-1 | 0.778 |
| F(000) | 2392.0 |
| Crystal size/mm3 | 0.2 × 0.05 × 0.05 |
| Radiation | Synchrotron (λ = 0.68878) |
| 2Θ range for data collection/° | 3.936 to 46.796 |
| Index ranges | -29<=h<=29, -9<=k<=9, -30<=l<=30 |
| Reflections collected | 49925 |
| Independent reflections | 8638 [Rint= 0.0979, Rsigma= 0.0680] |
| Data/restraints/parameters | 8638/3450/656 |
| Goodness-of-fit on F2 | 1.054 |
| Final R indexes [I>=2σ (I)] | R1 = 0.1400, wR2 = 0.3328 |
| Final R indexes [all data] | R1= 0.1516, wR2 = 0.3381 |
| Largest diff. peak/hole / e Å-3 | 1.70/-1.21 |

S4. Magnetic susceptibility measurements of DR1

Fig. S9 m T - T curve (circle) in the SQUID measurements for the powder of DR1 and the fitting plot obtained by the Bleaney-Bowers equation (red line).

S5. Electron paramagnetic resonance (EPR) spectra of radicals

Fig. S10. EPR spectra of TTM, TTM-1Cz, and DR1 in CH2Cl2 (10-4 M) at 298 K.

S6. Summary of photophysical properties for TTM, TTM-1Cz and DR1 in different solvents

Fig. S11. Normalised absorption, PL and transient PL decay spectra (excitation at 375 nm) of TTM (a, d, g), TTM-1Cz (b, e, h) and DR1 (c, f, i) in various solvents (10-5 M) at room temperature.

Table S5. Photophysical properties of TTM, TTM-1Cz and DR1 in various solvents.

| Radical | Solvent | λabs (nm) | λPL (nm) |  (ns) | PLQY (%) | kr (×107 s-1) | knr (×107 s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Cyclohexane | 540 | 564 | 5.6 | 2.0 | 0.35 | 17.5 |
|  | p-Xylene | 543 | 567 | 5.7 | 2.4 | 0.42 | 17.1 |
|  | Toluene | 542 | 565 | 5.8 | 2.5 | 0.43 | 16.8 |
|  | Butyl ether | 541 | 565 | 5.9 | 2.4 | 0.41 | 16.5 |
| TTM | Chloroform | 541 | 566 | 6.0 | 2.6 | 0.43 | 16.2 |
|  | Tetrahyrofuran | 541 | 569 | 6.0 | 1.8 | 0.33 | 16.3 |
|  | Dichloromethane | 542 | 568 | 6.3 | 2.0 | 0.29 | 15.6 |
|  | Cyclohexane | 603 | 628 | 41.3 | 53.0 | 1.28 | 1.13 |
|  | p-Xylene | 609 | 670 | 28.7 | 23.0 | 0.80 | 2.68 |
|  | Toluene | 609 | 673 | 25.4 | 18.5 | 0.73 | 3.21 |
|  | Butyl ether | 602 | 663 | 26.9 | 23.0 | 0.85 | 2.86 |
| TTM-1Cz | Chloroform | 600 | 687 | 13.2 | 5.0 | 0.38 | 7.20 |
|  | Tetrahyrofuran | 603 | 735 | 1.3 | - | - | - |
|  | Dichloromethane | 599 | 728 | 1.6 | - | 1.28 | 1.13 |
|  | Cyclohexane | 600 | 654 | 10.6 | 16.0 | 1.51 | 7.92 |
|  | p-Xylene | 610 | 670 | 12.3 | 22.0 | 1.79 | 6.34 |
|  | Toluene | 610 | 672 | 12.7 | 25.0 | 1.97 | 5.91 |
| DR1 | Butyl ether | 602 | 665 | 12.1 | 20.0 | 1.65 | 6.61 |
|  | Chloroform | 602 | 675 | 12.5 | 19.0 | 1.52 | 6.48 |
|  | Tetrahyrofuran | 609 | 705 | 3.9 | 2.6 | 0.66 | 2.49 |
|  | Dichloromethane | 602 | 694 | 2.6 | 4.2 | 0.16 | 3.68 |

The radiative rate constants (kr) and non-radiative rate constants (knr) of radicals were calculated using basic photophysical equations (1) and (2)

PLQY= kr/ (kr +knr)             (1)

=1/ (kr +knr)                  (2)

S7. The influence of doping concentration and temperature of DR1 (in PMMA) on photoluminescence

Fig. S12. PL spectra of PMMA film with Different DR1 concentrations.

Table S6 The Emission band and PLQYs of PMMA film with different DR1 concentrations.

| Wt.% | 0.1 | 0.5 | 2 | 10 | 20 | 30 |
| --- | --- | --- | --- | --- | --- | --- |
| Emission band (nm) | 671 | 673 | 680 | 689 | 690 | 689 |
| PLQY (%) | 5.2 | 14.1 | 13.3 | 1.2 | 0.24 | 0.12 |

Fig. S13. Temperature-dependent PL of DR1 (0.5 wt.%) doped in PMMA film.

Fig. S14. Temperature-dependent PL of TTM-1Cz (0.5 wt.%) doped in PMMA film.

Fig. S15. Temperature-dependent PL of DR1 (20 wt.%) doped in PMMA film.

S8. Stablities of TTM, TTM-1Cz and DR1

Fig. S16. (a) TAG curve of DR1 under nitrogen flow. (b) Plots showing the PL intensity decay of radicals in cyclohexane under 375 nm continuous photoexcitation (Emission intensities are normalized).

Table S7. RSEs calculations of TTM, TTM-1Cz and DR1.

| Molecule | H(R)/ a.u. | H(H▪)/a.u. | H(R-H)/ a.u. | BDE/kJ mol-1 | RSE/kJ mol-1 |
| --- | --- | --- | --- | --- | --- |
| TTM | -4869.136 | -0.498 | -4869.752 | 310.617 | 0.000 |
| TTM-1Cz | -4925.651 | -0.498 | -4926.267 | 309.872 | 0.746 |
| DR1-OS | -9334.013 | -0.498 | -9335.245 | 619.836 | 1.399 |
| DR1-Tt | -9334.013 | -0.498 | -9335.245 | 619.935 | 1.300 |

*R represents the corresponding radical, R-H represents the precursor of the radical, and H▪ represents the hydrogen radical.

S9. Electroluminescence properties of DR1-based OLED

Fig. S17. Optoelectronic properties of the OLED device with DR1 as the emitter. (a) Device structure diagram (b) EL spectra. (c) Radiance–voltage curves for the DR1 OLEDs. (d) EQE-current density.

Solution-processing device fabrication:

Indium tin-oxide (ITO; WF ∼ 4.8 eV) coated glass substrates were subsequently cleaned by sonication in acetone and 2-propanol for 10 minutes, followed by plasma 𝑂2 treatment for 10 minutes. PEDOT: PSS (Clevios CH4083, LumTech Taiwan) was spin-casted on top of the ITO under ambient conditions and annealed on a hot plate at 150 °C for 10 minutes, forming a 40 nm-thick film. The substrates were then transferred to a nitrogen-filled glovebox to conduct the following solution processes 2. Poly(9-vinylcarbazone) (PVK, Sigma-Aldrich) as the hole injection layer (HIL) was spin-casted onto the PEDOT: PSS layer at the concentration of 15 mg/ml in chlorobenzene (Sigma-Aldrich) followed with an annealing process for 20 min at 120°C. The 40 nm-thick emitting layer (EML) of TPBi (Xi’an p-OLED Corp) doped with 0.5 wt.% of DR1 in chlorobenzene (20 mg/ml) was spin-coated on top of the PVK layer and baked on a hot plate at 90 °C for 10 min to remove any solvent present. The samples were then transferred to a vacuum deposition system. The 60 nm-thick electron-transporting layer (ETL) (B3PYMPM, Xi’an p-OLED Corp.), 1 nm-thick LiF (99.99%, Sigma-Aldrich) and 100 nm-thick aluminium were subsequently deposited by thermal evaporation under high vacuum (< 3×10−7 mbar)2.

S10. Magneto-optical properties of DR1 and TTM-1Cz.

Fig. S18. The transient PL decay spectra of TTM-1Cz (0.5 wt%) doped in PMMA film with and without a magnetic field of 7 T at 2 K.

Fig. S19. MLs of TTM-1Cz (0.5 wt%) doped in PMMA film in different temperature. (a) 8 K, (b) 20 K, (c) 40 K and (d) 100 K.

Fig. S20. MLs of DR1(0.5 wt%) doped in PMMA film in different temperature. (a) 8 K, (b) 20 K, (c) 40 K and (d) 100 K.

Fig. S21 Temperature dependent ML of DR1 (20 wt.%) doped in PMMA film at 690 nm.

Fig. S22 Temperature dependent ML of DR1 (20 wt.%) doped in PMMA film at 820 nm.

References

[1] M. J. Frisch, G. W. Trucks, H. B. Schlegel, G. E. Scuseria,  M. A. Robb, J. R. Cheeseman, G. Scalmani, V. Barone,  G. A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A. V. Marenich,  J. Bloino, B. G. Janesko, R. Gomperts, B. Mennucci, H. P. Hratchian,  J. V. Ortiz, A. F. Izmaylov, J. L. Sonnenberg, D. Williams-Young,  F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone,  T. Henderson, D. Ranasinghe, V. G. Zakrzewski, J. Gao, N. Rega,  G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda,  J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai,  T. Vreven, K. Throssell, J. A. Montgomery, Jr., J. E. Peralta,  F. Ogliaro, M. J. Bearpark, J. J. Heyd, E. N. Brothers, K. N. Kudin,  V. N. Staroverov, T. A. Keith, R. Kobayashi, J. Normand, K. Raghavachari, A. P. Rendell, J. C. Burant, S. S. Iyengar, J. Tomasi, M. Cossi, J. M. Millam, M. Klene, C. Adamo, R. Cammi,  J. W. Ochterski, R. L. Martin, K. Morokuma, O. Farkas, J. B. Foresman, and D. J. Fox, Gaussian 16, Revision C.02, Wallingford CT, 2019.

[2] Stephens P. J.; Devlin, F.J.; Chabalowski, C.F. and Frisch M. J., J. Phys. Chem, 1994, 98: 11623.

[3] Frisch, M. J.; Pople, J. A.; Binkley, J. S., J. Chem. Phys. 1984, 80, 3265-3269.

[4] Yamaguchi, K., Chem. Phys. Lett., 1975, 33, 330–335.

[5] Neese, F., The ORCA program system. WIRES Comput. Mol. Sci. 2012, 2, 73-78.

[6] Liu Z., Lu T., Chen Q., Carbon, 2020, 165, 461-467.

[7] Lu, T.; Chen, F., J. Comput. Chem. 2012, 33, 580-592.

[8] Humphrey, W., Dalke, A. and Schulten, K., J. Molec. Graphics. 1996, 14, 33-38.

[9] Abdurahman, A.; Wang, J.; Zhao, Y.; Li, P.; Shen, L.; Peng, Q., Angew. Chem., Int. Ed. 2023, 62, e202300772.

[10] Bleaney, B.; Bowers, K., Proc. R. Soc. London, Ser. A 1952, 214, 451− 465

[11] Peng, Q.; Obolda, A.; Zhang, M.; Li, F., Angew.Chem.Int. Ed. 2015, 54, 7091-7095;

[12] Abdurahman, A.; Hele, T. J. H.; Gu, Q.; Zhang. J.; Peng, Q.; Zhang, M.; Friend, R. H.; Li, F.; Evans, E. W., Nat. Mater. 2020, 19, 1224-1229.