Multispecies-Coadsorption-Induced Rapid Preparation of Graphene Glass Fiber Fabric and Applications in Flexible Pressure Sensor Based on the Hierarchical Conductive Configuration

Kun Wang1,2,6, Xiucai Sun1,2,6, Shuting Cheng2,3,6, Yi Cheng1, Kewen Huang1,2, Ruojuan Liu1,2, Hao Yuan1,2, Wenjuan Li1,2, Fushun Liang1,2, Yuyao Yang1,2, Fan Yang1,2, Kangyi Zheng2,4, Zhiwei Liang2,5, Ce Tu2, Mengxiong Liu1,2, Mingyang Ma1,2, Yunsong Ge1,2, Muqiang Jian1,2, Wanjian Yin2,4, Yue Qi2*, Zhongfan Liu1,2*

- Centre for Nanochemistry, Beijing Science and Engineering Centre for Nanocarbons, Beijing National Laboratory for Molecular Sciences, College of Chemistry and Molecular Engineering, Peking University, Beijing 100871, China.

- Beijing Graphene Institute (BGI), Beijing 100095, China.

- State Key Laboratory of Heavy Oil Processing, College of Science, China University of Petroleum, Beijing 102249, China.

- College of Energy, Soochow Institute for Energy and Materials Innovations (SIEMIS), Jiangsu Provincial Key Laboratory for Advanced Carbon Materials and Wearable Energy Technologies, Soochow University, Suzhou 215006, China.

- Guangdong Provincial Key Laboratory of Quantum Engineering and Quantum Materials, School of Physics, South China Normal University, Guangzhou 510006, China

- These authors contributed equally: Kun Wang, Xiucai Sun, Shuting Cheng.

*   Correspondence: zfliu@pku.edu.cn; qiyue@bgi-graphene.com

# This PDF file includes:

# Supplementary Methods

Supplementary Figs. 1 to 12

Supplementary Reference

# Supplementary Methods

# DFT computational details

The DFT calculations are performed using the Vienna Ab initio Simulation Package (VASP) software1. The projector augmented wave (PAW) method was used to describe the interactions between the core and valence electrons. The Perdew-Burke-Ernzerhof (PBE) form involving the generalized gradient approximation (GGA) functional was used to describe the exchange correlation potential2. The electron wave functions were expanded in a plane wave basis set with a kinetic energy cutoff of 450 eV, the Monkhorst-Pack scheme k-point grids were set to 2×2×1. A vacuum layer of 15 Å is added perpendicular to the sheet to avoid artificial interaction between periodic images. All the structures are relaxed until the residual forces on the atoms have declined to less than 0.05 eV Å−1, and the convergence criterion for the total energy is set to 1 × 10−4 eV. For the calculation of the atomic dipole moments, with consideration of periodic boundary conditions, was accomplished by the application of the recently developed density-derived electrostatic and chemical (DDEC6) methods3. For transition state calculations, the climbing image nudged elastic band (CI-NEB) method was used to determine the energy barriers of various kinetic processes4. The transition states during each elementary reaction were verified by transition state imaginary frequency calculations.

The stability of hydrocarbon species adsorption geometry was evaluated by the adsorption energy (Eads), which is defined as

Eads = Etot-Esub- ECHx                                                      (1)

where Etot and Esub are the total energies of the SiO2(0001) substrate with and without adsorbed hydrocarbon species, ECHx is the energy of a hydrocarbon molecule.

During the various elementary reaction calculations and transition state searching processes, the reaction barrier Ea is calculated as

Ea = ETS-EIS                                                             (2)

where EIS and ETS represent the energies of the initial state (IS) and transition state (TS), respectively.

Considering the weak absorption on insulating surfaces, the lifetime of a species on a surface can be estimated by

τ = τ0exp(Eb/kBT)                                                        (3)

where τ0 = h/kBT is the prefactor and h and kB are the Plank and Boltzmann constants, respectively.

Supplementary Fig. 1 | SEM images of original GFF (a) and GGFF obtained after the high-temperature (~1100 °C) graphene CVD growing process (b). The structure of the fiber was well maintained after the high-temperature treatment.

Supplementary Fig. 2 | Current-voltage curves of GGFFs with growth time of (a) 15 s and (b) 30 s, showing open-circuit (corresponding to period I in Fig. 2) and connected-circuit (corresponding to period II in Fig. 2) characteristics, respectively.

Supplementary Fig. 3 | Growth rates of graphene grown with dichloromethane and methane at the different H2/CH2Cl2 or H2/CH4 ratios. The growth rates of graphene on GFF in the dichloromethane CVD system kept at ~3 orders of magnitude higher that of methane.

Supplementary Fig. 4 | Comparison of Raman spectra for dichloromethane- and methane-grown graphene obtained with the same growth rate. In contrast to the characteristic Raman 2D band (~2,680 cm−1) for dichloromethane-grown graphene, the Raman 2D band of methane-grown graphene is nearly negligible.

Supplementary Fig. 5 | DFT calculated bond lengths and overlap populations of (a) C−H in methane molecule and (b) C−H and C−Cl in dichloromethane molecule. The overlap population between two atoms provides a measure of the extent of electron density overlap between their respective atomic orbitals, indicating the strength of the bond between those atoms.

Supplementary Fig. 6 | Kinetic calculations of dichloromethane and methane pyrolysis. a, Energy barriers Ea (in eV) and possible routes for dichloromethane pyrolysis in gas phase.The black filled arrows indicate the main decomposition route. b, Energy barrier of CH4 dehydrogenation processes in gas phase.

Supplementary Fig. 7 | Calculated partial pressure of the decomposition products of dichloromethane as a function of temperature. The reaction is assumed under a thermodynamic equilibrium, and P(CH2Cl2) = 2.5  10−4 bar, P(H2) = 2.0  10−3 bar. The typical graphene growth temperature of ~1100 °C is marked with grey line.

Supplementary Fig. 8 | Calculation model of the GFF substrate. a, Schematic of the atomic configurations for SiO2(0001) surfaces terminated with different elements. b, Stable configurations of O1-, O2-, and Si-terminated surface structures with or without H passivation. c, Comparisons of the surface energy corrosponding to the six configurations in (b), where Si-terminated SiO2(0001) without H passivation (marked by the red box in (b)) is proved to be the most stable structure with the lowest surface energy.

Supplementary Fig. 9 | Stable configurations and adsorpstion energies (Eads) of CH2 adsorbed on SiO2(0001) surface (a) without and (b) with Cl coadsorption. Without Cl coadsorption, the adsorption energy of CH2 is ~−1.24 eV for Si site and ~1.40 eV for O site, revealing the nonactivity of O site for CH2 adsorption. With Cl coadsorption on Si site, the adsorption energy of CH2 decreases from ~−1.24 eV to ~−1.26 eV for Si site and from ~1.40 eV to ~−0.63 eV for adjacent non-bonding O site. The significant decrease of adsorpstion energies on O site indicates that CH2 adsorption is greatly enhanced and the nonactive O site is thus activated.

Supplementary Fig. 10 | Energy profiles and the corresponding structure evolution during the dehydrogenation kinetics of thegrowing zigzag edges of graphene domain, where (H-)Gr represents that the frontier edge of graphene is terminated by H. The H atoms at graphene edges are removed by CH2 species in the gas phase via CH2 + H-Gr → CH3 + Gr reaction. The high reaction energy barrier of ~2.06 eV severely limits the expansion of graphene edges.

Supplementary Fig. 11 | Schematic of the GGFF flexible pressure sensor, where GGFF is encapsulated by polypropylene films.

Supplementary Fig. 12 | ΔR/R0 of GGFF pressure sensor at different finger bending angles, exhibiting a rapid relative resistance variations with the good repeatability and stability.

# Supplementary References

1.	Kresse, G. & Joubert, D. From ultrasoft pseudopotentials to the projector augmented-wave method. Phys. Rev. B 59, 1758–1775 (1999).

2.	Perdew, J. P., Burke, K. & Ernzerhof, M. Generalized gradient approximation made simple. Phys. Rev. Lett. 77, 3865–3868 (1996).

3.	Limas, N. & Manz, T. A. Introducing DDEC6 atomic population analysis: part 2. Computed results for a wide range of periodic and nonperiodic materials. RSC Adv. 6, 45727–45747 (2016).

4.	Mills, G., Jonsson, H. & Schenter, G. K. Reversible work transition state theory: application to dissociative adsorption of hydrogen. Surf. Sci. 324, 305–337 (1995).