Molecularly imprinted polymers with ionic liquid as the functional monomer for selective solid-phase extraction of gastrodin.

Congcong Zhaoa, Jin Lib and Zhenyu Zuo*a,c

Congcong Zhao, Email:zhaocongcong9803@163.com；

Jin Li, Email: 2051014@sntcm.edu.cn；

Zhenyu Zuo, Email: zuozhenyu666@sina.cn；

a Department of Pharmacy, Shaanxi University of Chinese Medicine, Xi’an, 712046, China;

b Northwestern Polytechnical University, Xi’an 712072, China;

c Shaanxi Key Laboratory of Basic and New Herbal Medicament Research, Xi'an 712046, China);

*Corresponding author: Zhenyu Zuo, Email: zuozhenyu666@sina.cn.

Fig.3 Synthesis of dehydroabietic acid [2-(acryloyloxy)ethyl] ester (DAAEE).

Fig.4 Synthesis of [COOHvimBr] ionic liquid.

Fig.5 Synthesis of [C14VIM+] [Br-] ionic liquid.

Fig. S1 1H-NMR of DAAEE.

1H-NMR(400MHz;CDCl3);δ(ppm)=7.10(d,1H),6.93(d,1H),6.80(s,1H),6.39-6.29 (m,1H),6.09-5.99(m,1H),5.77(1H,dd),4.32-4.22(m,4H),2.81-2.69(m,3H),2.26-2.13(m,2H), 1.73-1.65 (m,4H), 1.63 (s,2H), 1.57 (d,1H), 1.21-1.13 (m,12H).

Fig. S2 1H-NMR of [COOHvimBr].

1HNMR(400MHz;D2O-d6;MeSi4);δ(ppm)=2.9(t,2H),4.44(t,2H),5.34(d,1H),5.74(d, 1H),7.07(m,1H),7.58(s,1H),7.71(s, 1H),9.05(s,1H).

Fig. S3 1H-NMR of [C14VIM+] [Br-].

1HNMR(400MHz;D2O);δ(ppm)=7.85(s,1H),7.65(s,1H),7.15(s,1H),5.85(d,1H), 5.45(s,1H), 4.25(s,2H), 1.75(s,2H), 1.15(s,23H),0.80(s,3H).

a                                 b

Fig.7 binding energy of functional monomer and GAS(a) and molar ratio of functional monomer to template molecule(b).

Fig.8 The Ultraviolet and visible spectrophotometry of different functional monomers (a) and GAS in ethanol with addition of different concentrations of [C14VIM＋][Br-] (b).

Fig.9 Interaction between [C14VIM+] [Br-] and GAS.

Fig.10 The FT-IR spectrum of MIP (a), [C14VIM+] [Br-](b), MIP after the adsorption of GAS(c), GAS(d).

Fig.11 The FT-IR spectrum of silica gel(a), modified silica gel (b)and SNIPs(c).

a

b

Fig.14 EDS energy spectrum of MIPs(a)and SMIPs(b).

Fig.17 Adsorption kinetics curves of MIPs and NIPs.

Tab. S1 simulation parameters of pseudo-first-order dynamics and

pseudo-second- order dynamics

|  | Qe(exp) (mg/g) | the pseudo-first-order model |  |  | the pseudo- second -order model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | R12 | K1 (min-1) | lnQe (mg/g) | R22 | K2(g·mg-1·min-1) | lnQe (mg/g) |
| MIP | 151.8424 | 0.835 | 0.0222 | 5.6032 | 0.5894 | -0.0042 | 0.3204 |
| NIP | 120.3517 | 0.9065 | 0.0239 | 5.0973 | 0.1468 | -0.0016 | 0.9631 |

Fig. S4 The pseudo-first-order kinetic model curve of MIPs.

Table S2 Recoveries of GAS at different spiked levels in samples(n=3)

| Spiked levels(%) | Recovery (%) | Mean recovery (%) | RSD (%) |
| --- | --- | --- | --- |
| 80% | 97.75 | 0.99092 | 2.23 |
|  | 101.64 |  |  |
|  | 97.89 |  |  |
| 100% | 102.15 | 1.004249333 | 1.53 |
|  | 99.88 |  |  |
|  | 99.24 |  |  |
| 120% | 103.43 | 1.001487667 | 2.88 |
|  | 99.03 |  |  |
|  | 97.98 |  |  |

Fig.20 HPLC spectrum of GAS standard (a), Gastrodia elata root extracts before percolating through SPE column (b), methanol acetic acid eluent (c), methanol eluent (d), 70% methanol eluent (e), ethanol eluent (f), 50% ethanol eluent (g), 70% ethanol eluent (h), SMIPs-SPE-70% ethanol eluent (I).