TEMPO Oxidation for High Cellulose Content Biomass: A Study on Palm Oil Empty Fruit Bunch Fibers

Andrea P. Martínez-Ramírez1 0000-0002-5375-1399, Sergio A Rincón-Ortiz2 0000-0001-6494-4762, Víctor G. Baldovino-Medrano2 0000-0003-3227-0251, Cristian Blanco-Tirado1 0000-0002-3650-5487, Marianny Y. Combariza1* 0000-0002-6907-4759.

1Escuela de Química, Universidad Industrial de Santander, Bucaramanga – Colombia, 680002, 2Laboratorio de Ciencia de Superficies (#SurfLab-UIS), Parque Tecnológico de Guatiguará, Universidad Industrial de Santander, Piedecuesta – Colombia,681011.

*Corresponding author: marianny@uis.edu.co (Marianny Y. Combariza).

SUPPORTING INFORMATION

Table S1. Multilevel Factorial Design 24

| No. Experiments | Identification samples | Experimental parameters |  |
| --- | --- | --- | --- |
|  |  | Reaction time [min] | Cellulose:NaClO molar ratio |
| 1 | TOCN 30-1:1 | 30 | 1:1 |
| 2 | TOCN 30-1:5 | 30 | 1:5 |
| 3 | TOCN 30-1:8 | 30 | 1:8 |
| 4 | TOCN 30-1:10 | 30 | 1:10 |
| 5 | TOCN 60-1:1 | 60 | 1:1 |
| 6 | TOCN 60-1:5 | 60 | 1:5 |
| 7 | TOCN 60-1:8 | 60 | 1:8 |
| 8 | TOCN 60-1:10 | 60 | 1:10 |
| 9 | TOCN 90-1:1 | 90 | 1:1 |
| 10 | TOCN 90-1:5 | 90 | 1:5 |
| 11 | TOCN 90-1:8 | 90 | 1:8 |
| 12 | TOCN 90-1:10 | 90 | 1:10 |
| 13 | TOCN 120-1:1 | 120 | 1:1 |
| 14 | TOCN 120-1:5 | 120 | 1:5 |
| 15 | TOCN 120-1:8 | 120 | 1:8 |
| 16 | TOCN 120-1:10 | 120 | 1:10 |

Figure S1. Conductimetric titration graphs of oxidized cellulose suspensions

Figure S2. Statistical analysis of charge density a) Pareto chart, b) Main effects plot, c) Estimated response surface, and d) Interaction plot

Figure S3. Statistical analysis of oxidation yield [%] a) Pareto chart, b) Main effects plot, c) Estimated response surface, and d) Interaction plot

Figure S4. Statistical analysis of size distribution a) Pareto chart, b) Main effects plot, c) Estimated response surface, and d) Interaction plot

Figure S5. Statistical analysis of Z potential a) Pareto chart, b) Main effects plot, c) Estimated response surface, and d) Interaction plot

Table S2. Signal assignment infrared spectroscopy

| Wave number [cm-1] | Functional group | Reference |
| --- | --- | --- |
| 1733 | C=O stretch of acetyl and hemicellulose | Kaffashsaie et al., 2021 |
| 1602 | Stretching C=O in carboxylic acids with sodium | (Chuensangjun et al., 2019; C. F. Huang et al., 2015)(Chuensangjun et al., 2019; C. F. Huang et al., 2015)(Chuensangjun et al., 2019; C. F. Huang et al., 2015) |
| 1317 | Stretch flexion CH2 in cellulose | (Traoré et al., 2018)(Traoré et al., 2018)(Traoré et al., 2018) |
| 1230 | Asymmetric axial deformation =C-O- in the ether, ester, and phenol group of lignin |  |
| 1164 | Asymmetrical C-O-C stretch of the pyranose ring | (Fahma et al., 2020)(Fahma et al., 2020)(Fahma et al., 2020) |
| 1109 | C-O-C stretch of cellulose | (Traoré et al., 2018)(Traoré et al., 2018)(Traoré et al., 2018) |
| 1030 | Cellulose C-O and C-H stretching vibrations | (Fahma et al., 2010, 2020)(Fahma et al., 2010, 2020)(Fahma et al., 2010, 2020) |
| 900 | specific C-H anomeric vibration for β-glycosides |  |

Figure S6 a. Spectra XPS (EFB, EFB-AHP, TOCN 30-1:8, TOCN 60-1:8, TOCN 90-1:8 and TOCN 120-1:8)

Figure S6 b. Spectra XPS (EBF-TOCN, TOCN 120-1:1, TOCN 120-1:5, and TOCN 120-1:10)

Table S3. General spectra and the positions and values of FWHM

| Atom |  | XPS data | EFB | EFB-AHP | EFB-TOCN | TOCN 30-1:8 | TOCN 60-1:8 | TOCN 90-1:8 | TOCN 120-1:8 | TOCN 120-1:1 | TOCN 120-1:5 | TOCN 120-1:10 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C | C-H | Position [eV] | 284.8 | 284.8 | 284.8 | 284.8 | 284.8 | 284.8 | 284.8 | 284.8 | 284.8 | 284.8 |
|  |  | FWHM | 2.37 | 1.91 | 1.28 | 1.30 | 1.35 | 1.26 | 1.20 | 1.30 | 1.14 | 1.21 |
|  | C-C-O | Position [eV] | - | 286.8 | 286.5 | 286.5 | 286.5 | 286.5 | 286.4 | 286.5 | 286.5 | 286.4 |
|  |  | FWHM | - | 1.91 | 1.28 | 1.30 | 1.35 | 1.26 | 1.20 | 1.30 | 1.14 | 1.21 |
|  | O-C-O | Position [eV] | 287.9 | 288.6 | 288.2 | 287.9 | 288.1 | 288.0 | 288.3 | 287.9 | 287.9 | 287.7 |
|  |  | FWHM | 2.37 | 1.55 | 1.28 | 1.30 | 1.35 | 1.26 | 1.20 | 1.30 | 1.14 | 1.21 |
|  | C-COO- | Position [eV] | - | - | 289.5 | 288.8 | 289.4 | 289.3 | 289.5 | 289.0 | 288.7 | 288.6 |
|  |  | FWHM | - | - | 1.28 | 1.30 | 1.35 | 1.26 | 1.20 | 1.30 | 1.14 | 1.21 |
| O |  | Position [eV] | 532.5 | 532.6 | 532.3 | 532.9 | 532.7 | 532.8 | 531.9 | 533.0 | 532.9 | 532.8 |
|  |  | FWHM | 2.90 | 2.52 | 2.43 | 1.99 | 2.4 | 2.17 | 2.15 | 1.88 | 1.81 | 1.90 |
| Ca | 3/2 | Position [eV] | 347.5 | 347.2 | 347.3 | 347.5 | 347.3 | 347.3 | 347.3 | 347.4 | 347.39 | 347.3 |
|  |  | FWHM | 2.32 | 1.94 | 1.48 | 1.48 | 1.57 | 1.54 | 1.44 | 1.5 | 1.46 | 1.77 |
|  | 1/2 | Position [eV] | 351.1 | 350.9 | 350.9 | 351.1 | 350.9 | 350.9 | 350.9 | 351.0 | 351.0 | 350.9 |
|  |  | FWHM | 2.20 | 1.95 | 1.56 | 1.59 | 1.56 | 1.55 | 1.52 | 1.50 | 1.50 | 1.83 |
| Si |  | Position [eV] | 101.9 | - | - | 101.9 | 101.9 | - | 101.9 | - | - | - |
|  |  | FWHM | 1.94 | - | - | 1.36 | 1.42 | - | 0.98 | - | - | - |
| Na |  | Position [eV] | - | - | 1073.9 | 1072.9 | 1073.8 | 1073.7 | 1072.2 | 1074.3 | 1072.6 | 1072.1 |
|  |  | FWHM | - | - | 1.83 | 2.18 | 2.74 | 2.39 | 2.25 | 1.63 | 1.68 | 2.22 |
| Cl | 3/2 | Position [eV] | - | - | 198.4 | - | - | 198.8 | - | 197.8 | 198.2 | 198.2 |
|  |  | FWHM | - | - | 1.87 | - | - | 2.49 | - | 1.56 | 2.31 | 2.12 |
|  | 1/2 | Position [eV] | - | - | 200.02 | - | - | 200.4 | - | 199.4 | 199.8 | 199.8 |
|  |  | FWHM | - | - | 1.28 | - | - | 1.84 | - | 1.43 | 2.09 | 0.98 |
| N |  | Position [eV] | - | - | 398.7 | 399.9 | - | 398.7 | 398.3 | 400.0 | 399.8 | 399.9 |
|  |  | FWHM | - | - | 0.78 | 1.50 | - | 0.50 | 0.1 | 2.34 | 2.50 | 1.83 |

Parity Plot

The parity plot was performed with the experimental data obtained in the C 1S spectra, focusing on the atomic percentages obtained for the signals C-C-O, O-C-O/C= O and C-COO-. The contributions were then summed and divided by the corresponding ratio for AHP-EFB 5/6 and 1/6 for C-C-O and O-C-O and for oxidised cellulose TOCN 4/6, 1/6 and 1/6 for C-C-O, O-C-O/C= O and C-COO- respectively. Table S4 presents the data obtained for EFB-AHP and EFB-TOCN.

Table S4. Theorical value parity plot

|  | C 1s | Experimental | Ratio | Operation | Theoretical |
| --- | --- | --- | --- | --- | --- |
| EFB-AHP | C-C-O | 16.84 | 5/6 | (20.74/(5/6) | 17.28 |
|  | O-C-O | 3.90 | 1/6 | (20.74)/(1/6) | 3.46 |
|  | C-COO- | 0.00 | - | - | - |
|  | Total Carbon | 20.74 | - | - | - |
| EFB-TOCN | C-C-O | 18.15 | 4/6 | (28.63) /(4/6) | 19.09 |
|  | O-C-O | 6.60 | 1/6 | (28.63) /(1/6) | 4.77 |
|  | C-COO- | 3.88 | 1/6 | (28.63) /(1/6) | 4.77 |
|  | Total Carbon | 28.63 | - | - | - |