Supporting information

Two-step modification of sepiolite (SDS/isep) and its performance for remediation of Pb contaminated water

1Yiming Gu, 1*Huixia Feng, 2Bin Wang, 3Liang Zhang, 1Sijie Liang, 1Nali Chen, 1Lin Tan

1School of Petrochemical Technology, Lanzhou University of Technology, Lanzhou, P.R. China

2School of Materials Science and Engineering, Southwest Jiaotong University, Chengdu, P.R. China

3Department of Machine Intelligence and Systems Engineering Faculty of Systems Engineering, Akita Prefectural University, Akita, Japan

* Corresponding author at: College of Petrochemical Engineering, Lanzhou University of Science and Technology, Lanzhou, 730050, China.

E-mail address: fenghx@lut.edu.cn (H. Feng).

Fig. S1. (a) SEM micrographs of natural sepiolite; (b), SEM micrographs of isep.

Fig. S2. (a) N2 adsorption-desorption isotherms and BJH pores of the natural sepiolite.; (b), N2 adsorption-desorption isotherms and BJH pores of the isep.

Fig. S3. TGA/DTG curve of SDS/isep

Table S1 XRD indexes of natural sepiolite and as@sep adsorbents.

| hkl | natural sepiolite |  |  | isep |  |  | SDS/isep |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 2θ(°) | Height | d(Å) | 2θ(°) | Height | d(Å) | 2θ(°) | Height | d(Å) |
| (110) | 7.291 | 19438 | 12.114 | 7.341 | 30678 | 11.953 | 7.370 | 14173 | 11.985 |
| (060) | 19.897 | 3557 | 4.459 | 19.703 | 3041 | 4.487 | 19.697 | 2035 | 4.503 |
| (031) | 20.646 | 5498 | 4.298 | 20.626 | 4870 | 4.301 | 20.625 | 3398 | 4.302 |
| (221) | 22.461 | 3548 | 3.955 | 23.767 | 3230 | 3.953 | 23.862 | 1955 | 3.740 |
| (400) | 26.654 | 3978 | 3.342 | 26.731 | 3291 | 3.335 | 26.586 | 1903 | 3.350 |
| (191) | 35.275 | 4541 | 2.542 | 35.012 | 3834 | 2.553 | 35.028 | 2135 | 2.559 |

Table S2 Sepcific surface area and pore characters of sepiolite and as@sep.

| Sample | Sepcific surface | Pore volume | Pore size |
| --- | --- | --- | --- |
| natural sepiolite | 143.7 m2/g | 0.61 cm3/g | 17.1 nm |
| isep | 184.4 m2/g | 0.51 cm3/g | 10.9 nm |
| SDS/isep | 104.4 m2/g | 0.57 cm3/g | 21.9 nm |

Table S3 The cation exchange capacity of three absorbents

| Sample | Cation exchange capacity |
| --- | --- |
| natural sepiolite | 61.6 cmol/kg |
| isep | 66.8 cmol/kg |
| SDS/isep | 68.8 cmol/kg |