Fabrication of Fluorescent PMMA-Carbon Nanodots Optical Films and their Feasibility in Improving Solar Cells Efficiency using Low-Cost Sustainable Materials

Marco C. P. Soares1,*,+, Michele Cacioppo2,†,*,+, Francesco Amato2,‡,*,+, Thiago D. Cabral1, Marcelo N. P. Carreño3, Inés Pereyra3, Carlos A. S. Ramos3, Manuel Cid3, Gilson S. Goveia4, José F. D. Chubaci4, Eric Fujiwara1, Maurizio Prato2,5,6, Julio R. Bartoli1,7,*

1Laboratory of Photonic Materials and Devices, School of Mechanical Engineering, University of Campinas, Campinas, SP, Brazil

2Carbon Nanotechnology Group, Department of Chemical and Pharmaceutical Sciences, University of Trieste, Trieste, Italy

3Laboratory of Microelectronics, Polytechnic School, University of São Paulo, SP, Brazil (LME/EPUSP)

4Institute of Physics, University of São Paulo, SP, Brazil

5Center for Cooperative Research in Biomaterials (CIC biomaGUNE), Basque Research and Technology Alliance (BRTA), Paseo de Miramón 182, 20014, Donostia San Sebastián (Spain)

6Basque Foundation for Science, Ikerbasque, 48013 Bilbao, Spain

7School of Chemical Engineering, University of Campinas, Campinas, SP, Brazil

†Present address: Department of Biological, Chemical and Pharmaceutical Sciences and Technologies (STEBICEF), University of Palermo, Viale delle Scienze Ed. 17, 90128 Palermo, Italy

‡Present Address: Department of Chemistry, University of Rome “La Sapienza”, Rome, Italy

*Corresponding authors: marcosoares.feq@gmail.com (M.C.P.S); michelecacioppo@gmail.com (M.C.); amatofrancesco89@libero.it (F.A.); bartoli@unicamp.br (J.R.B.)

+These authors contributed equally to this work.

Supporting Information

Contents

Figure SI 1. Lyophilized α-CDs (5 wt%) dispersed in a mixture comprised of chloroform and methanol (proportion of 2:1 (v/v)) observed under: a. daylight; b. UV light (λ = 365 nm).	2

Figure SI 2. PMMA-NCNDs (5 wt%) solution (before casting) observed under: a. daylight; b. UV light (λ = 365 nm).	2

Figure SI 3. PMMA-NCNDs (5 wt%) films on the Petri dishes after drop casting: a. frontal aspect, under daylight; b. side aspect, under daylight; c. frontal aspect, under UV light (λ = 365 nm); d. side aspect, under UV light (λ = 365 nm).	3

Figure SI 4. a. Silicon solar cell; b. bench for photovoltaic measurements; c. PMMA-NCNDs (0.5 wt%) optical film positioned on the solar cell; d. Measurements of I × V curve and obtention of photovoltaic parameters with Lab Tracer 2.0 software.	4

Figure SI 5. PMMA-α-CDs (5 wt%) solution (before casting) observed under: a. daylight; b. UV light (λ = 365 nm).	4

Figure SI 6. Photoluminescence spectra obtained for PMMA-α-CDs (5 wt%) optical films when reducing the excitation and emission slits from 5 to 2.5 nm. The collected intensities considerably decreased, allowing the observation of the spectra with no saturation.	5

Figure SI 7. Different optical films obtained when observed under: a. daylight; b. UV light (λ = 365 nm).	5

Figure SI 8. Absorbances obtained for the different optical films.	6

Figure SI 9. Transmittances obtained for the different optical films.	7

Figure SI 1. Lyophilized α-CDs (5 wt%) dispersed in a mixture comprised of chloroform and methanol (proportion of 2:1 (v/v)) observed under: a. daylight; b. UV light (λ = 365 nm).

Figure SI 2. PMMA-NCNDs (5 wt%) solution (before casting) observed under: a. daylight; b. UV light (λ = 365 nm).

Figure SI 3. PMMA-NCNDs (5 wt%) films on the Petri dishes after drop casting: a. frontal aspect, under daylight; b. side aspect, under daylight; c. frontal aspect, under UV light (λ = 365 nm); d. side aspect, under UV light (λ = 365 nm).

Figure SI 4. a. Silicon solar cell; b. bench for photovoltaic measurements; c. PMMA-NCNDs (0.5 wt%) optical film positioned on the solar cell; d. Measurements of I × V curve and obtention of photovoltaic parameters with Lab Tracer 2.0 software.

Figure SI 5. PMMA-α-CDs (5 wt%) solution (before casting) observed under: a. daylight; b. UV light (λ = 365 nm).

Figure SI 6. Photoluminescence spectra obtained for PMMA-α-CDs (5 wt%) optical films when reducing the excitation and emission slits from 5 to 2.5 nm. The collected intensities considerably decreased, allowing the observation of the spectra with no saturation.

Figure SI 7. Different optical films obtained when observed under: a. daylight; b. UV light (λ = 365 nm).

Figure SI 8. Absorbances obtained for the different optical films.

Figure SI 9. Transmittances obtained for the different optical films.