Supplementary information

Iron alloying improved electrocatalytic activity in dye-sensitized solar cells with Cu2Cu1-xFexSnS4 counter electrodes

K.P. Lia, Z.Z. Liua, C. Wanga, Y.Q. Zhanga, Z.Q. Zhaoa, X.B. Yangb, B. Zhoua, Z.X. Xiea, Z.Q. Duana, and Y.M. Hua, *

a College of Engineering, Dali University, Dali, 671003, China

b Faculty of Material Science and Engineering, Kunming University of Science and Technology, Kunming, 650093, China

1. XRD pattern of the samples

1.1 XRD peaks shift of CCFTS powder

Figure S1 Amplified characteristic peaks of the CCFTS powder

1.2 Peak analyses for FT-4

Figure S2 Lorentz fitting for the peaks located at 25.5~29.5° of FT-4

The peak is composed of two peaks, corresponding to orthogonal CTS (the peak at 27.90°) and tetragonal CFTS (JCPDS No. 97-009-0827) (the peak at 28.18°), respectively, indicating CFTS phase was generated during the annealing.

2. Morphology and composition

2.1 Morphology

Figure S3 HRTEM images of F-3 under different magnifications

Figure S4 Profile image of FT-3

2.2 Composition

Table S1 EDS results of the CCFTS precursor powder

| Samples | Cu At% | Sn At% | S At% | Fe At% | Chemical formula |
| --- | --- | --- | --- | --- | --- |
| F-0 | 31.47 | 13.36 | 55.17 | - | Cu2.52Sn1.07S4.41 |
| F-1 | 33.24 | 13.82 | 51.39 | 1.55 | Cu2.66Fe0.12Sn1.11S4.11 |
| F-2 | 31.78 | 13.92 | 52.45 | 1.85 | Cu2.54Fe0.15Sn1.11S4.20 |
| F-3 | 31.31 | 13.36 | 53.07 | 2.26 | Cu2.50Fe0.18Sn1.07S4.25 |
| F-4 | 30.25 | 13.96 | 53.46 | 2.33 | Cu2.42Fe0.19Sn1.11S4.28 |

Table S2 EDS results of the CCFTS CEs

| CE | Cu At% | Sn At% | S At% | Fe At% | Chemical formula |
| --- | --- | --- | --- | --- | --- |
| FT-0 | 36.92 | 14.37 | 48.71 | - | Cu2.95Sn1.15S3.90 |
| FT-1 | 35.04 | 15.38 | 48.73 | 0.85 | Cu2.80Fe0.07Sn1.23S3.90 |
| FT-2 | 32.12 | 17.08 | 48.81 | 1.99 | Cu2.57Fe0.16Sn1.37S3.90 |
| FT-3 | 30.43 | 15.27 | 52.65 | 1.65 | Cu2.44Fe0.13Sn1.22S4.21 |
| FT-4 | 33.48 | 16.41 | 47.27 | 2.84 | Cu2.68Fe0.23Sn1.31S3.78 |

3. Optical bandgaps

Figure S5 Bandgaps of the CCFTS precursor powder (a) and CEs (b)

4. The top of the valence band

Figure S6 The top of the valence band (EVB,XPS) of FT-0, FT-3 and FT-4