Supplemental Material for “Unravelling Ultralow Thermal Conductivity in Double Perovskite Cs2AgBiBr6: Dominant Wave-like Phonon Tunnelling, Strong Quartic Anharmonicity and Lattice Instability”

Jiongzhi Zheng 1,2, Changpeng Lin 3,4, Chongjia Lin1, Geoffroy Hautier2, Ruiqiang Guo5,, Baoling Huang 1,6,7,

1Department of Mechanical and Aerospace Engineering, The Hong Kong University of Science and Technology, Clear Water Bay, Kowloon, Hong Kong

2Thayer School of Engineering, Dartmouth College, Hanover, New Hampshire, 03755, USA

3Theory and Simulation of Materials (THEOS), Ecole Polytechnique Federale de Lausanne, CH-1015 Lausanne, Switzerland

4National Centre for Computational Design and Discovery of Novel Materials (MARVEL),

Ecole Polytechnique Federale de Lausanne, CH-1015 Lausanne, Switzerland

5Thermal Science Research Center, Shandong Institute of Advanced Technology, Jinan, Shandong Province, 250103, China

6HKUST Foshan Research Institute for Smart Manufacturing, Hong Kong University of Science and Technology, Clear Water Bay, Kowloon, Hong Kong, China

7HKUST Shenzhen-Hong Kong Collaborative Innovation Research Institute, Futian, Shenzhen 518055, China

Contents

I.	Atomic participation ratio projected on the phonon dispersions	2

II.	Calculated atomic displacement parameters	2

III.	Harmonic and anharmonic phonon dispersions and atom-decomposed partial and total phonon density of states	4

IV.	Comparison of the experimentally measured and theoretically calculated phonon energies	5

V.	Calculated room temperature phonon dispersion in comparison with Raman results	6

VI.	Calculated phonon group velocity	6

VII.	Comparison of the experimentally measured and theoretically calculated specific heat	6

VIII.	Calculated phonon scattering rates with neglecting modes	7

IX.	Calculated spectral and cumulative phonon thermal conductivity	7

X.	Calculated phonon scattering rates	8

XI.	Mode grȕneisen parameters projected onto the phonon dispersions	8

XII.	Calculated participation ratio projected onto the phonon bands	9

XIII.	Calculated phonon mean free paths	9

- Atomic participation ratio projected on the phonon dispersions

Fig. S1. The color-coded atomic participation ratio (APR) of double perovskite Cs2AgBiBr6 projected onto the phonon bands at finite temperatures. (a) Br atom at T = 0 K. (b) Cs atom at T = 300 K. (c) Bi atom at T = 500 K. (d) Ag atom at T = 700 K.

- Calculated atomic displacement parameters

Fig. S2. Comparison of atomic displacement parameters calculated using the SCP and SCPB methods, respectively.

- Harmonic and anharmonic phonon dispersions and atom-decomposed partial and total phonon density of states

Fig. S3. Calculated harmonic phonon dispersion at T = 0 K in comparison with the anharmonic phonon dispersions calculated at finite temperatures (100 K-700 K). Atom-decomposed partial and total phonon densities of states at T = 0 (HA), 300, and 700 K are shown on the right panel.

- Comparison of the experimentally measured and theoretically calculated phonon energies

Fig. S4. Calculated room temperature phonon dispersions along the G-K line using SCP and SCPB methods, respectively, compared with experimental data  [1].

- Calculated room temperature phonon dispersion in comparison with Raman results

Fig. S5. Phonon dispersions calculated using SCPB approximation in comparison with Raman results [2].

- Calculated phonon group velocity

Fig. S6. (a) Comparison of group velocity at T = 300 K calculated using the SCP and SCPB methods, respectively. (b) The same as (a), but T = 700 K.

- Comparison of the experimentally measured and theoretically calculated specific heat

Fig. S7. Calculated temperature-dependent specific heat using SCP and SCPB methods, in comparison with experimental results  [3].

- Calculated phonon scattering rates with neglecting modes

Fig. S8. (a) Comparison of phonon scattering rates at T = 300 K calculated with the original phonon dispersions and those neglecting Br-dominated soft modes (including 4th, 5th, and 6th phonon bands). (b) The same as (a), but with those neglecting Cs-dominated soft modes (including 7th, 8th, and 9th phonon bands).

- Calculated spectral and cumulative phonon thermal conductivity

Fig. S9. Comparison of spectral and cumulative thermal conductivity at T = 300 K calculated using phonon dispersions with neglecting Br- or Cs-dominated modes, respectively.

- Calculated phonon scattering rates

Fig. S10. Comparison of phonon scattering rates calculated using the SCPB+3ph model at T = 200, 300 and 700 K, respectively.

- Mode grȕneisen parameters projected onto the phonon dispersions

Fig. S11. Calculated mode gruneisen parameter projected onto the phonon dispersions at room temperature.

- Calculated participation ratio projected onto the phonon bands

Fig. S12. Calculated participation ratio projected onto the phonon dispersions along high-symmetry paths in the Brillouin zone at room temperature.

- Calculated phonon mean free paths

Fig. S13. (a) Comparison of phonon mean free paths at T = 300 K calculated using three different levels of thermal transport theory, i.e., SCP+3ph, SCPB+3ph and SCPB+3,4ph models, respectively. (b) The same as (a), but T = 700 K.

References

[1] X. He, M. Krogstad, M. K. Gupta, T. Lanigan-Atkins, C. Mao, F. Ye, Y. Liu, T. Hong, S. Chi, and H. Wei, arXiv preprint arXiv:2112.04717 (2021).

[2] J. A. Steele, P. Puech, M. Keshavarz, R. Yang, S. Banerjee, E. Debroye, C. W. Kim, H. Yuan, N. H. Heo, and J. Vanacken, ACS nano 12, 8081 (2018).

[3] A. Cohen, T. M. Brenner, J. Klarbring, R. Sharma, D. H. Fabini, R. Korobko, P. K. Nayak, O. Hellman, and O. Yaffe, Adv Mater 34, 2107932 (2022).

stylefix

ruiqiang.guo@iat.cn

mebhuang@ust.hk