Cation exchange strategy to construct a targeting nanoprobe for enhanced positive MR imaging capability

Siyu Chen1, Haitao Sun4 ,Yingyan Zheng5, Qian Chen3, Yu Luo*2, Hangrong Chen*3 and Quan Zhou*1

1Department of Radiology, Third Affiliated Hospital of Southern Medical University (Academy of Orthopedics Guangdong Province), Southern Medical University, Guangzhou, Guangdong 510630, P. R. China

2School of Chemical Science and Engineering, Tongji University, 1239 Siping Road, Shanghai 200092, P. R. China

3Country State Key Laboratory of High-Performance Ceramics and Superfine Microstructure, Shanghai Institute of Ceramics, Chinese Academy of Sciences, 1295 Ding-Xi Road, Shanghai 200050, P. R. China

4Shanghai Institute of Medical Imaging, Department of Interventional Radiology, Zhongshan Hospital, Fudan University, No. 180 Fenglin Road, Xuhui District, Shanghai 200032, P. R. China

5Department of Radiology, Huashan Hospital, Fudan University, 12 Middle Wulumuqi Road, Jingan District, Shanghai, 200040, P. R. China

Corresponding Author

*E-mail: yuluo@tongji.edu.cn (Y.L.).

*E-mail: hrchen@mail.sic.ac.cn (H. C.).

*E-mail: zhouquan3777@smu.edu.cn (Q. Z.).

Figure S1. SEM element line scanning analysis of TUG.

Figure S2. (a) Photo of TUG dispersed in deionized water, PBS, and serum contained medium for 3 months (inset) and hydrated particle sizes of the TUG dispersed in deionized water, PBS, and serum contained medium for 7 days. (b) Zeta potentials of the TUG dispersed in water, PBS, and medium for 7 days.

Figure S3. MRI imaging of TUG aqueous solution at different Gd concentrations (0.6, 1.2, 2.4, 4.8, 9.6 mM) taken by 3.0 T clinical MR imaging system under the following parameters: FOV = 60 × 60 mm; matrix = 256 × 256; section thickness = 2 mm; TR =1200 ms; TE = 17 ms.

Figure S4. In vivo blood circulation time of TUG and UG. The healthy Balb/c mice were injected with TUG and UG (1 mg/mL, 250 μL) and then 10 μL blood were taken from tail vein at the fixed time points (0 min, 5 min, 30 min, 1 h, 2 h, 4 h, 8 h, 12 h, 24 h) and sent for ICP-OES.

Figure S5. Hematological assay of healthy Balb/c mice after intravenous injection of TUG (15 mg.kg−1) for 14 days. The mice without treatment was used as control.

Figure S6. Representative MRI gray images of tumors. (a) MRI images of subcutaneous tumor in Balb/c nude mice after injection of TUG and Gd-DTPA; (b) MRI images of tumor in situ in Balb/c nude mice after injection of TUG and Gd-DTPA