| Table S1 Average colony diameters (mm) of wood decay fungi grown on media containing 4 mg/mL of thermally modified poplar and spruce wood extracts at different temperatures (mm) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Fungus | Extract | Temperature (°C) | Colony diameters (mm)a |  |  |  |
|  |  |  | 6 days | 8 days | 14 days | 21 days |
| White-rot fungi T. versicolor | Control | － | 60.0 | 60.0 | 60.0 | 60.0 |
|  | Ethanol | － | 60.0 | 60.0 | 60.0 | 60.0 |
|  | TMP extract | 180 | 21.7±1.9 | 31.1±1.4 | 60.0 | 60.0 |
|  |  | 200 | 19.4±0.7 | 31.9±1.1 | 60.0 | 60 |
|  |  | 220 | 25.3±3.8 | 34.9±6.6 | 60.0 | 60 |
|  | TMS extract | 180 | 20.2±4.7 | 32.1±5.5 | 60.0 | 60 |
|  |  | 200 | 36.6±2.4 | 60.0 | 60.0 | 60.0 |
|  |  | 220 | 29.5±1.0 | 50.8±1.2 | 60.0 | 60.0 |
| Brown-rot fungi G. trabeum | Control | － | 38.3±2.0 | 60.0 | 60.0 | 60.0 |
|  | Ethanol | － | 36.5±0.8 | 60.0 | 60.0 | 60.0 |
|  | TMP extract | 180 | 16.9±0.6 | 16.6±1.4 | 30.1±4.4 | 45.6±3.7 |
|  |  | 200 | 24.7±3.4 | 25.7±4.7 | 50.3±2.5 | 60.0 |
|  |  | 220 | 24.1±1.4 | 25.5±0.5 | 60.0 | 60.0 |
|  | TMS extract | 180 | 13.5±0.3 | 22.9±1.5 | 47.7±11.8 | 60.0 |
|  |  | 200 | 13.4±0.9 | 31.1±2.8 | 60.0 | 60.0 |
|  |  | 220 | 16.1±0.9 | 31.9±1.6 | 51.9±7.7 | 60.0 |
| a The initial diameter of the fungal inoculum was 4.4 mm; The diameter of the petri dish was 60 mm; Values represent means of 3 replicates/fraction/ fungus |  |  |  |  |  |  |