	Table S1 Average colony diameters (mm) of wood decay fungi grown on media containing 4 mg/mL of thermally modified poplar and spruce wood extracts at different temperatures (mm)

	Fungus
	Extract
	Temperature (°C)
	Colony diameters (mm)a

	
	
	
	6 days
	8 days
	14 days
	21 days

	White-rot fungi
T. versicolor
	Control
	－
	60.0
	60.0
	60.0
	60.0

	
	Ethanol
	－
	60.0
	60.0
	60.0
	60.0

	
	TMP extract
	180
	21.7±1.9
	31.1±1.4
	60.0
	60.0

	
	
	200
	19.4±0.7
	31.9±1.1
	60.0
	60

	
	
	220
	25.3±3.8
	34.9±6.6
	60.0
	60

	
	TMS extract
	180
	20.2±4.7
	32.1±5.5
	60.0
	60

	
	
	200
	36.6±2.4
	60.0
	60.0
	60.0

	
	
	220
	29.5±1.0
	50.8±1.2
	60.0
	60.0

	Brown-rot fungi 
G. trabeum
	Control
	－
	38.3±2.0
	60.0
	60.0
	60.0

	
	Ethanol
	－
	36.5±0.8
	60.0
	60.0
	60.0

	
	TMP extract
	180
	16.9±0.6
	16.6±1.4
	30.1±4.4
	45.6±3.7

	
	
	200
	24.7±3.4
	25.7±4.7
	50.3±2.5
	60.0

	
	
	220
	24.1±1.4
	25.5±0.5
	60.0
	60.0

	
	TMS extract
	180
	13.5±0.3
	22.9±1.5
	47.7±11.8
	60.0

	
	
	200
	13.4±0.9
	31.1±2.8
	60.0
	60.0

	
	
	220
	16.1±0.9
	31.9±1.6
	51.9±7.7
	60.0

	a The initial diameter of the fungal inoculum was 4.4 mm; The diameter of the petri dish was 60 mm; Values represent means of 3 replicates/fraction/ fungus



