	Table S2 Compounds identified in acetone extracts of un-treated wood and 
their relative content (%)

	Poplar wood extract
	Spruce wood extract

	Rt/min
	Compounds
	Area%
	Rt/min
	Compounds
	Area%

	22.7
	4H-1-Benzopyran-4-one, 2,3-dihydro-5-hydroxy-2-(4-hydroxyphenyl)-7-methoxy-, (S)-
	23.4
	18.7
	4'-Methoxy-2-hydroxystilbene
	25.1

	23.6
	Naringenin
	9.8
	19.3
	2-(4-Methylphenyl)benzoic acid
	8.9

	22.2
	Benzeneacetic acid,4-hydroxy-, ethyl ester
	4.02
	20.6
	15-Hydroxydehydroabietic acid, methyl ester
	3.0

	18.7
	ç-Sitosterol
	3.2
	3.0
	2-Pentanone,4-hydroxy-4-methyl-
	2.4

	23.1
	Phenol, 2,4- bis(1,1-dimethylethyl)-,phosphite (3:1)
	2.7
	21.5
	10,11-Dihydro-10-hydroxy-2,3-dimethoxydibenz(b,f)oxepin*
	1.9

	2.9
	2-Pentanone, 4-hydroxy-4-methyl-
	2.7
	19.6
	Phenol, 2,2'-methylenebis[6-(1,1-dimethylethyl)-4-methyl-
	1.6

	4.1
	Glycerin
	1.6
	19.0
	Methyl dehydroabietate
	1.3

	19.5
	2,2'-methylenebis[6-(1,1-dimethylethyl)-4-methyl- Phenol
	1.6
	9.7
	2,4-Di-tert-butylphenol
	1.3

	9.3
	9-Oxononanoic acid
	1.3
	20.2
	4H-1-Benzopyran-4-one, 2,3-dihydro-5,7-dihydroxy-2-phenyl-, (S)-
	1.1

	7.3
	Salicyl alcohol
	1.0
	4.1
	Hexanoic acid
	1.0



