Supplementary material

| Table S1 Average colony diameters (mm) of wood decay fungi grown on media containing 4 mg/mL of thermally modified poplar and spruce wood extracts at different temperatures (mm) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Fungus | Extract | Temperature (°C) | Colony diameters (mm)a |  |  |  |
|  |  |  | 6 days | 8 days | 14 days | 21 days |
| White-rot fungi T. versicolor | Control | － | 60.0 | 60.0 | 60.0 | 60.0 |
|  | Ethanol | － | 60.0 | 60.0 | 60.0 | 60.0 |
|  | TMP extract | 180 | 21.7±1.9 | 31.1±1.4 | 60.0 | 60.0 |
|  |  | 200 | 19.4±0.7 | 31.9±1.1 | 60.0 | 60 |
|  |  | 220 | 25.3±3.8 | 34.9±6.6 | 60.0 | 60 |
|  | TMS extract | 180 | 20.2±4.7 | 32.1±5.5 | 60.0 | 60 |
|  |  | 200 | 36.6±2.4 | 60.0 | 60.0 | 60.0 |
|  |  | 220 | 29.5±1.0 | 50.8±1.2 | 60.0 | 60.0 |
| Brown-rot fungi G. trabeum | Control | － | 38.3±2.0 | 60.0 | 60.0 | 60.0 |
|  | Ethanol | － | 36.5±0.8 | 60.0 | 60.0 | 60.0 |
|  | TMP extract | 180 | 16.9±0.6 | 16.6±1.4 | 30.1±4.4 | 45.6±3.7 |
|  |  | 200 | 24.7±3.4 | 25.7±4.7 | 50.3±2.5 | 60.0 |
|  |  | 220 | 24.1±1.4 | 25.5±0.5 | 60.0 | 60.0 |
|  | TMS extract | 180 | 13.5±0.3 | 22.9±1.5 | 47.7±11.8 | 60.0 |
|  |  | 200 | 13.4±0.9 | 31.1±2.8 | 60.0 | 60.0 |
|  |  | 220 | 16.1±0.9 | 31.9±1.6 | 51.9±7.7 | 60.0 |
| a The initial diameter of the fungal inoculum was 4.4 mm; The diameter of the petri dish was 60 mm; Values represent means of 3 replicates/fraction/ fungus |  |  |  |  |  |  |

| Table S2 Compounds identified in acetone extracts of un-treated wood and their relative content (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Poplar wood extract |  |  | Spruce wood extract |  |  |
| Rt/min | Compounds | Area% | Rt/min | Compounds | Area% |
| 22.7 | 4H-1-Benzopyran-4-one, 2,3-dihydro-5-hydroxy-2-(4-hydroxyphenyl)-7-methoxy-, (S)- | 23.4 | 18.7 | 4'-Methoxy-2-hydroxystilbene | 25.1 |
| 23.6 | Naringenin | 9.8 | 19.3 | 2-(4-Methylphenyl)benzoic acid | 8.9 |
| 22.2 | Benzeneacetic acid,4-hydroxy-, ethyl ester | 4.02 | 20.6 | 15-Hydroxydehydroabietic acid, methyl ester | 3.0 |
| 18.7 | ç-Sitosterol | 3.2 | 3.0 | 2-Pentanone,4-hydroxy-4-methyl- | 2.4 |
| 23.1 | Phenol, 2,4- bis(1,1-dimethylethyl)-,phosphite (3:1) | 2.7 | 21.5 | 10,11-Dihydro-10-hydroxy-2,3-dimethoxydibenz(b,f)oxepin* | 1.9 |
| 2.9 | 2-Pentanone, 4-hydroxy-4-methyl- | 2.7 | 19.6 | Phenol, 2,2'-methylenebis[6-(1,1-dimethylethyl)-4-methyl- | 1.6 |
| 4.1 | Glycerin | 1.6 | 19.0 | Methyl dehydroabietate | 1.3 |
| 19.5 | 2,2'-methylenebis[6-(1,1-dimethylethyl)-4-methyl- Phenol | 1.6 | 9.7 | 2,4-Di-tert-butylphenol | 1.3 |
| 9.3 | 9-Oxononanoic acid | 1.3 | 20.2 | 4H-1-Benzopyran-4-one, 2,3-dihydro-5,7-dihydroxy-2-phenyl-, (S)- | 1.1 |
| 7.3 | Salicyl alcohol | 1.0 | 4.1 | Hexanoic acid | 1.0 |