Supplementary material

	Table S1 Average colony diameters (mm) of wood decay fungi grown on media containing 4 mg/mL of thermally modified poplar and spruce wood extracts at different temperatures (mm)

	Fungus
	Extract
	Temperature (°C)
	Colony diameters (mm)a

	
	
	
	6 days
	8 days
	14 days
	21 days

	White-rot fungi
T. versicolor
	Control
	－
	60.0
	60.0
	60.0
	60.0

	
	Ethanol
	－
	60.0
	60.0
	60.0
	60.0

	
	TMP extract
	180
	21.7±1.9
	31.1±1.4
	60.0
	60.0

	
	
	200
	19.4±0.7
	31.9±1.1
	60.0
	60

	
	
	220
	25.3±3.8
	34.9±6.6
	60.0
	60

	
	TMS extract
	180
	20.2±4.7
	32.1±5.5
	60.0
	60

	
	
	200
	36.6±2.4
	60.0
	60.0
	60.0

	
	
	220
	29.5±1.0
	50.8±1.2
	60.0
	60.0

	Brown-rot fungi 
G. trabeum
	Control
	－
	38.3±2.0
	60.0
	60.0
	60.0

	
	Ethanol
	－
	36.5±0.8
	60.0
	60.0
	60.0

	
	TMP extract
	180
	16.9±0.6
	16.6±1.4
	30.1±4.4
	45.6±3.7

	
	
	200
	24.7±3.4
	25.7±4.7
	50.3±2.5
	60.0

	
	
	220
	24.1±1.4
	25.5±0.5
	60.0
	60.0

	
	TMS extract
	180
	13.5±0.3
	22.9±1.5
	47.7±11.8
	60.0

	
	
	200
	13.4±0.9
	31.1±2.8
	60.0
	60.0

	
	
	220
	16.1±0.9
	31.9±1.6
	51.9±7.7
	60.0

	a The initial diameter of the fungal inoculum was 4.4 mm; The diameter of the petri dish was 60 mm; Values represent means of 3 replicates/fraction/ fungus




	Table S2 Compounds identified in acetone extracts of un-treated wood and 
their relative content (%)

	Poplar wood extract
	Spruce wood extract

	Rt/min
	Compounds
	Area%
	Rt/min
	Compounds
	Area%

	22.7
	4H-1-Benzopyran-4-one, 2,3-dihydro-5-hydroxy-2-(4-hydroxyphenyl)-7-methoxy-, (S)-
	23.4
	18.7
	4'-Methoxy-2-hydroxystilbene
	25.1

	23.6
	Naringenin
	9.8
	19.3
	2-(4-Methylphenyl)benzoic acid
	8.9

	22.2
	Benzeneacetic acid,4-hydroxy-, ethyl ester
	4.02
	20.6
	15-Hydroxydehydroabietic acid, methyl ester
	3.0

	18.7
	ç-Sitosterol
	3.2
	3.0
	2-Pentanone,4-hydroxy-4-methyl-
	2.4

	23.1
	Phenol, 2,4- bis(1,1-dimethylethyl)-,phosphite (3:1)
	2.7
	21.5
	10,11-Dihydro-10-hydroxy-2,3-dimethoxydibenz(b,f)oxepin*
	1.9

	2.9
	2-Pentanone, 4-hydroxy-4-methyl-
	2.7
	19.6
	Phenol, 2,2'-methylenebis[6-(1,1-dimethylethyl)-4-methyl-
	1.6

	4.1
	Glycerin
	1.6
	19.0
	Methyl dehydroabietate
	1.3

	19.5
	2,2'-methylenebis[6-(1,1-dimethylethyl)-4-methyl- Phenol
	1.6
	9.7
	2,4-Di-tert-butylphenol
	1.3

	9.3
	9-Oxononanoic acid
	1.3
	20.2
	4H-1-Benzopyran-4-one, 2,3-dihydro-5,7-dihydroxy-2-phenyl-, (S)-
	1.1

	7.3
	Salicyl alcohol
	1.0
	4.1
	Hexanoic acid
	1.0
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