Supplement: Contact-separation-induced self-recoverable mechanoluminescence of CaF2:Tb3+/PDMS elastomer

Wenxiang Wang, Shanwen Wang, Yan Gu, Jinyu Zhou, Jiachi Zhang

National & Local Joint Engineering Laboratory for Optical Conversion Materials and Technology, Lanzhou University, Lanzhou 730000, P. R. China

Content

Supplementary Note 1: Microstructure and elemental composition of CaF2	1

Supplementary Note 2: Spectra of CaF2: Tb3+/Eu2+/Sm3+	16

Supplementary Note 3: Two-dimensional stretching machine	24

Supplementary Note 4: Sample preparation	28

Supplementary Note 5: Properties of Lu3Al5O12 and Y2O2S	29

Supplementary Note 6: Analysis of the contact interface	47

Supplementary Note 7: First-principles calculation of contact-separation	52

Supplementary Note 8: Additional first-principles calculations	62

Supplementary Note 9: Other factors affecting ML intensity	96

References	100

Supplementary Note 1: Microstructure and elemental composition of CaF2

Figure S1-1. Crystal structure of CaF2

Table S1-1. Crystallographic data of CaF2

| Formula | CaF2 |
| --- | --- |
| Crystal system | Cubic |
| Space group | Fm-3m (225) |
| Lattice parameters |  |
| a = b = c | 5.458 Å |
| α = β = γ | 90° |
| Cell volume | 162.634 Å3 |
| T | 289 K |
| Diffractometer | Rigaku D/Max-2400 |
| Radiation/Å | Cu-Ka (λ= 1.5405) |
| Absorption correction | multi-scan |
| 2θ range | 8°-80° |
| Z | 4 |
| Calculated Density | 3.189 g/cm3 |
| R-factors |  |
| Rwp | 0.0943 |
| Rp | 0.0672 |
| χ2 | 1.769 |

Table S1-2. Refined coordinates of all atoms, bond lengths of X-F and the unit cell parameters of the CaF2 as determined by the GSAS program.

| Space group |  | Fm-3m (225) - Cubic |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Cell |  | a = b = c = 5.458 Å |  |  |  |  |
| Ion coordinates | x | y |  | z | Occupancy | Uiso |
| Ca | 0.0000(0) | 0.0000(0) |  | 0.0000(0) | 1.000(0) | 0.0100(0) |
| F | 0.2500(0) | 0.2500(0) |  | 0.2500(0) | 0.2500(0) | 0.0100(0) |
| The bond lengths of X-F |  |  |  |  |  |  |
| Vector |  |  | Length |  |  |  |
| Ca_F |  |  | 2.36358(4) |  |  |  |

Table S1-3. The bandgap of CaF2 calculated by

Vienna Ab-initio Simulation Package (VASP)

| Band Character | Indirect |
| --- | --- |
| Band Gap (eV) | 7.3822 |
| Eigenvalue of VBM (eV) | -0.4827 |
| Eigenvalue of CBM (eV) | 6.8996 |
| Fermi Energy (eV) | 0.4076 |
| HOMO & LUMO Bands | 12 13 |
| Location of VBM | 0.500000 0.000000 0.500000 |
| Location of CBM | 0.000000 0.000000 0.000000 |

Figure S1-2. Calculated energy band structure of CaF2

Figure S1-3. Partial density of states (Ca atoms) of CaF2

Figure S1-4. Partial density of states (F atoms) of CaF2

Figure S1-5. X-ray photoelectron spectroscopy(XPS) spectrum of CaF2

Figure S1-6. High-resolution XPS spectra of Tb 3d

Figure S1-7. High-resolution XPS spectra of Eu 3d

Figure S1-8. High-resolution XPS spectra of Sm 3d

Figure S1-9. Infrared absorption spectrum of PDMS

Figure S1-10. Infrared absorption spectrum of CaF2:Tb3+

Figure S1-11. Raman spectroscopy of PDMS

Figure S1-12. Raman spectroscopy of CaF2:Tb3+

Figure S1-13. Elemental distribution map of CaF2:Eu2+.

Figure S1-14. Energy dispersive spectra (EDS) of CaF2:Eu2+

Table S1-4. Elements analysis of CaF2:Eu2+

| Element | Weight % | Atomic % | Error % |
| --- | --- | --- | --- |
| F | 64.94 | 80.04 | 8.68 |
| Ca | 33.85 | 19.77 | 2.44 |
| Eu | 1.21 | 0.19 | 57.30 |

Figure S1-15. Elemental distribution map of CaF2:Tb3+

Figure S1-16. Energy dispersive spectra (EDS) of CaF2:Tb3+

Table S1-5. Elements analysis of CaF2:Tb3+

| Element | Weight % | Atomic % | Error % |
| --- | --- | --- | --- |
| F | 51.83 | 70.21 | 9.78 |
| Ca | 45.79 | 29.41 | 2.47 |
| Tb | 2.38 | 0.39 | 56.76 |

Figure S1-17. Elemental distribution map of CaF2:Sm3+

Figure S1-18. Energy dispersive spectra (EDS) of CaF2:Sm3+

Table S1-6. Elements analysis of CaF2:Sm3+

| Element | Weight % | Atomic % | Error % |
| --- | --- | --- | --- |
| F | 89.15 | 98.17 | 4.50 |
| Ca | 0.84 | 0.44 | 90.83 |
| Sm | 10.01 | 1.39 | 42.73 |

Supplementary Note 2: Spectra of CaF2: Tb3+/Eu2+/Sm3+

Figure S2-1. Excitation spectrum of CaF2:Tb3+

Figure S2-2. Emission spectrum of CaF2:Tb3+

Figure S2-3. ML spectrum of CaF2:Tb3+

Figure S2-4. Luminescence decay curve of CaF2:Tb3+

Figure S2-5. Excitation spectrum of CaF2:Sm3+

Figure S2-6. Emission spectrum of CaF2:Sm3+

Figure S2-7. ML spectrum of CaF2:Sm3+

Figure S2-8. Luminescence decay curve of CaF2:Sm3+

Figure S2-9. Excitation spectrum of CaF2:Eu2+

Figure S2-10. Emission spectrum of CaF2:Eu2+

Figure S2-11. ML spectrum of CaF2:Eu2+

Figure S2-12. Luminescence decay curve of CaF2:Eu2+

Figure S2-13. Schematic diagram of a falling ball experimental setup

Figure S2-14. ML intensity of CaF2:Eu2+/PDMS in 50 repeated tests

Figure S2-15. ML intensity of CaF2:Tb3+/PDMS in 50 repeated tests

Figure S2-16. ML intensity of CaF2:Sm3+/PDMS in 50 repeated tests

Supplementary Note 3: Two-dimensional stretching machine

To investigate the ML self-recover ability of the composite under two-dimensional alternating stretching, we developed a dedicated stretching machine featuring a mechanical structure depicted in the figure below. To ensure utmost precision and force consistency during stretching, we equipped the machine with two high-precision stepping motors and a 1:19 planetary reducer. The control system is based on an MKS GEN-L V2.1 motherboard running on open source Marlin firmware6,7 which was made possible by the selfless dedication of the open source community. Following the debugging sessions, we achieved a stretching accuracy of 0.1 mm, which perfectly meets our experimental requirements.

Figure S3-1. Top and bottom isometric isometric view of the 2D stretching machine

Figure S3-2. Top view of the 2D stretching machine

Figure S3-3. Left view of the 2D stretching machine

Figure S3-4. Right view of the 2D stretching machine

Figure S3-5. Top and bottom isometric isometric view of the fixture

Figure S3-6. Right view of the fixture

Supplementary Note 4: Sample preparation

Figure S4-1. Preparation process of the four-leaf clover shape sample

First, weigh and mix the raw materials at a mass ratio of 10 (PDMS matrix) to 1 (PDMS curing agent) to 5.5 (phosphor powder) (i). Transfer the resulting slurry to a 35 mm petri dish (ii) and place it in a 60 °C oven for 5 hours to cure the PDMS (iii). Remove the cured PDMS from the petri dish (iv) and cut it into cubes (v). Take a square of the cured PDMS and place it in another petri dish. Add more PDMS to cover the square (vi), and put the petri dish back in the oven (vii). After curing, take out the sample and cut it according to the mold shape (viii) to obtain the sample (ix).

Supplementary Note 5: Properties of Lu3Al5O12 and Y2O2S

Figure S5-1. Crystal structure of Lu3Al5O12

Figure S5-2. Rietveld refinement of the Lu3Al5O12

Table S5-1. Crystallographic data of Lu3Al5O12

| Formula | Lu3Al5O12 |
| --- | --- |
| Crystal system | Cubic |
| Space group | I a -3 d |
| Lattice parameters |  |
| a（Å） | 11.9203 |
| b（Å） | 11.9203 |
| c（Å） | 11.9203 |
| α° = β° = γ° | 90 |
| Cell volume（Å3 ） | 1693.7978 |
| T /K | 289 |
| Diffractometer | Rigaku D /Max-2400 |
| Radiation /Å | Cu-Ka（λ= 1.5405） |
| Absorption correction | multi-scan |
| 2θ range° / | 10-100 |
| Z | 8 |
| Calculated Density | 6.6830 g/cm3 |
| R-factors |  |
| Rwp | 0.096 |
| Rp | 0.078 |

Table S5-2. Refined coordinates of all atoms, bond lengths of X-O and the unit cell parameters of the Lu3Al5O12.

| Space group |  |  | I a -3 d - Cubic |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cell |  |  | a = b = c = 11.9203 |  |  |  |  |  |
| Ion coordinates | x |  | y |  | z | Occupancy |  | Uiso |
| Al1 | 0.000000 |  | 0.000000 |  | 0.000000 | 1.0000 |  | 0.03356 |
| Al2 | 0.375000 |  | 0.000000 |  | 0.250000 | 1.0000 |  | 0.02022 |
| Lu1 | 0.125000 |  | 0.000000 |  | 0.250000 | 1.0000 |  | 0.01093 |
| O1 | 0.031599 |  | 0.051802 |  | 0.150646 | 1.0000 |  | 0.00573 |
| The bond lengths of X-O |  |  |  |  |  |  |  |  |
| Vector |  | Length |  | Vector |  |  | Length |  |
| Al1-O1 |  | 1.936(8) |  | Lu1_O1 |  |  | 2.295(7) |  |
| Al2_O1 |  | 1.739(8) |  | Lu1_O1 |  |  | 2.412(10) |  |

Table S5-3. The bandgap of Lu3Al5O12 Calculated by Vienna Ab-initio Simulation Package (VASP)

| Band Character | Direct |
| --- | --- |
| Band Gap (eV) | 5.0676 |
| Eigenvalue of VBM (eV) | 3.5630 |
| Eigenvalue of CBM (eV) | 8.6306 |
| Fermi Energy (eV) | 3.7840 |
| HOMO & LUMO Bands | 228 229 |
| Location of VBM | 0.000000 0.000000 0.000000 |
| Location of CBM | 0.000000 0.000000 0.000000 |

Figure S5-3. Calculated energy band structure of Lu3Al5O12

Figure S5-4. Partial density of states (Lu atoms) of Lu3Al5O12

Figure S5-5. Partial density of states (O atoms) of Lu3Al5O12

Figure S5-6. Partial density of states (O atoms) of Lu3Al5O12

Figure S5-7. Crystal structure of Y2O2S

Figure S5-8. Rietveld refinement of the Y2O2S

Table S5-4. Crystallographic data of Y2O2S

| Formula | Y2O2S |
| --- | --- |
| Crystal system | Trigonal |
| Space group | P -3 m 1 |
| Lattice parameters |  |
| a（Å） | 3.7817 |
| b（Å） | 3.7817 |
| c（Å） | 6.5822 |
| α° = β° | 90 |
| γ° | 120 |
| Cell volume（Å3 ） | 81.521 |
| T /K | 289 |
| Diffractometer | Rigaku D /Max-2400 |
| Radiation /Å | Cu-Ka（λ= 1.5405） |
| Absorption correction | multi-scan |
| 2θ range° / | 10-80 |
| Z | 1 |
| Calculated Density | 4.9270 g/cm3 |
| R-factors |  |
| Rwp | 0.1205 |
| Rp | 0.0932 |

Table S5-5. Refined coordinates of all atoms, bond lengths of X-O/S and the unit cell parameters of the Y2O2S.

| Space group |  |  | P -3 m 1 - Trigonal |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cell |  |  | a = b = 3.7817 c = 6.5822 |  |  |  |  |  |
| Ion coordinates | x |  | y |  | z | Occupancy |  | Uiso |
| Y1 | 0.333300 |  | 0.666700 |  | 0.282000 | 1.0000 |  | 0.00032 |
| O1 | 0.333300 |  | 0.666700 |  | 0.631000 | 1.0000 |  | 0.00032 |
| S1 | 0.000000 |  | 0.000000 |  | 0.000000 | 1.0000 |  | 0.00032 |
| The bond lengths of X-O/S |  |  |  |  |  |  |  |  |
| Vector |  | Length |  | Vector |  |  | Length |  |
| Y1_O1 |  | 2.29719 |  | Y1_S1 |  |  | 2.86582 |  |
| Y1_O1 |  | 2.25699 |  | Y1_S1 |  |  | 2.86557 |  |
| Y1_O1 |  | 2.25762 |  |  |  |  |  |  |

Table S5-6. The bandgap of Y2O2S Calculated by Vienna

Ab-initio Simulation Package (VASP)

| Band Character | Indirect |
| --- | --- |
| Band Gap (eV) | 3.0457 |
| Eigenvalue of VBM (eV) | 3.5572 |
| Eigenvalue of CBM (eV) | 6.6029 |
| Fermi Energy (eV) | 3.7839 |
| HOMO & LUMO Bands | 20 21 |
| Location of VBM | 0.000000 0.000000 0.500000 |
| Location of CBM | 0.333333 0.333333 0.000000 |

Figure S5-9. Calculated energy band structure of Y2O2S

Figure S5-10. Partial density of states (Y atoms) of Y2O2S

Figure S5-11. Partial density of states (O atoms) of Y2O2S

Figure S5-12. Partial density of states (S atoms) of Y2O2S

Figure S5-13. LPL spectrum of Lu3Al5O12:Ce3+

Figure S5-14. ML spectrum of Lu3Al5O12:Ce3+

Figure S5-15. LPL spectrum of Y2O2S:Eu3+

Figure S5-16. ML spectrum of Y2O2S:Eu3+

Figure S5-17. Bright field photographs(a, b) and dark field LPL photographs(c, d) of Y2O2S:Eu3+/PDMS(a, c) and Lu3Al5O12:Ce3+/PDMS(b, d) elastomers

Figure S5-18. ML photographs of Y2O2S:Eu3+/PDMS(a) and Lu3Al5O12:Ce3+/PDMS(b) elastomers

Lu3Al5O12:Ce3+ is a commercially available phosphor with a centrosymmetric structure that exhibits excellent ML properties when used in a PDMS composite, as demonstrated in our previous work.8 Interestingly, it was found that the ML properties of this phosphor are independent of the trap level, making it an ideal candidate for comparison. In contrast, Y2O2S:Eu3+ is another commercially available phosphor with a centrosymmetric structure that is known for its excellent long persistent performance. While some reports have suggested that this phosphor exhibits ML, we did not observe any ML in the Y2O2S:Eu3+/PDMS composite(Figure S5-16, Figure S5-18), possibly due to the lower tensile and tear strengths of PDMS. Therefore, this phosphor was chosen to represent sulfide in our study.

Supplementary Note 6: Analysis of the contact interface

Figure S6-1. Stress distribution and binding energies of the elastomer

Figure S6-1 illustrates the states and binding energies of the complex at different stages during two-dimensional stretching. Originally, prior to incorporating the phosphor into PDMS (Figure S6-1 i), there was no contact between the phosphor and PDMS, hence no interfacial stress (Figure S6-1 ii). The binding energy of the complex was E1 = -493.276 eV (Figure S6-1 iii). Upon incorporating the phosphor into PDMS (Figure S6-1 iv), the phosphor and PDMS were in contact but without interfacial stress (Figure S6-1 v). The binding energy of the complex was E2 = -492.898 eV (Figure S6-1 vi). Subsequently, the complex was stretched horizontally (Figure S6-1 vii) and concurrently subjected to tensile forces in the horizontal direction and compressive forces in the vertical direction (Figure S6-1 viii). Horizontally, the phosphor and PDMS were stretched apart. Calculation showed that the complex had the lowest binding energy when hydrogen atoms remained on the surface of the phosphor. The binding energy at this stage was E3 = -494.139 eV (Figure S6-1 ix), releasing energy of ΔE23 = 1.241 eV. The complex was then stretched vertically (Figure S6-1 x) and simultaneously subjected to tensile forces in the vertical direction and compressive forces in the horizontal direction (Figure S6-1 xi). Under the effect of horizontal compression , the phosphor and PDMS came into close contact again. At this point, the complex absorbed energy of ΔE23 = 1.241 eV and returned to E2, completing one two-dimensional stretching cycle.

In summary, during the cycling process, energy was released when the phosphor and PDMS separated and absorbed when they came into contact again. The requisite energy was provided by the external tensile forces.

Figure S6-2. The stress distribution and ML photo for the elastomer under stretching

Figure S6-3. The stress distribution and ML photo for the elastomer under falling ball

Figure S6-4. The stress distribution and ML photo for the elastomer under bending

Figures S7-2 to S7-4 present ML images of the complexes under different action modes, along with the corresponding stress distribution at the interface. The Figures indicate that the action modes which elicit ML also result in the separation of phosphor powder from the PDMS.

Figure S6-5. In situ micrographs(a, b) and stress distribution(c, d)

before(a, c) and after(b, d) stretching

When stretched, the randomly arranged phosphor particles (Figure S6-5 (a)) tend to become ordered, as shown in Figure S6-5 (b), which could be simulated by the finite element method as shown in Figure S6-5 (c-d).

Supplementary Note 7: First-principles calculation of contact-separation

Calculation Method：First-principles calculations are performed by vienna ab initio simulation package (VASP)1–5. The generalized gradient approximation(GGA) of Perdew-Burke-Ernzerhof (PBE) is used to describe the exchange-correlation functional. The cut-off energy for the plane wave basis is set to 400 eV and a 2×2×1 mesh is employed. All the structures were fully relaxed (atomic position) up to 10-5 eV /Å force minimization and max force of 0.01 eV/Å.

All transition states were calculated using the Transition State Tools for VASP-VTST method, with the stretching frequencies analyzed in order to characterize whether a stationary point is a minimum state without imaginary frequency or a transition state with only one imaginary frequency. For the transition state structures, frequency analysis is carried out, and zero point energy correction is carried out for all the energy obtained to eliminate the impact of vibration on the energy.

The reaction energy are defined as:

ΔE21 = E2 – E1

ΔE31 = E3 – E1

E23 = E2 – E3

Calculation parameters summary:

Cutoff energy: 400 eV

Electronic self-consistent convergence criterion: 10-5 eV/Å

Atomic relaxation convergence criterion: -0.01 eV/Å

K-point grid: 2×2×1

Functional: PAW-PBE

Figure S7-1. Initial state of CaF2/PDMS elastomer

E1 = -493.27614475 eV

Figure S7-2. Contact state of CaF2/PDMS elastomer

E2 = -492.89820746 eV

Figure S7-3. Separation state of CaF2/PDMS elastomer

E3 = -494.13918038 eV

Calculated to get:

ΔE21 = E2 – E1 = -492.89820746 - -493.27614475 = 0.378 eV

ΔE31 = E3 – E1 = -494.13918038 - -493.27614475 = -0.863 eV

ΔE23 = E2 – E3 = -492.89820746 - -494.13918038 = 1.241 eV

Figure S7-4. Initial state of Lu3Al5O12/PDMS elastomer

E1 = -1122.80316728 eV

Figure S7-5. Contact state of Lu3Al5O12/PDMS elastomer

E2 = -1121.72060209 eV

Figure S7-6. Separation state of Lu3Al5O12/PDMS elastomer

E3 = -1123.97150073 eV

Calculated to get:

ΔE21 = E2 – E1 = -1121.72060209 - -1122.80316728 = 1.083 eV

ΔE31 = E3 – E1 = -1123.97150073 - -1122.80316728 = -1.168 eV

ΔE23 = E2 – E3 = -492.89820746 - -494.13918038 = 2.251 eV

Figure S7-7. Initial state of Y2O2S/PDMS elastomer

E1 = -860.42780451 eV

Figure S7-8. Contact state of Y2O2S/PDMS elastomer

E2 = -858.92551482 eV

Figure S7-9. Separation state of Y2O2S/PDMS elastomer

E3 = -861.16371424 eV

Calculated to get:

ΔE21 = E2 – E1 = -858.92551482 - -860.42780451= 1.502 eV

ΔE31 = E3 – E1 = -861.16371424 - -860.42780451 = -0.736 eV

ΔE23 = E2 – E3 = -858.92551482 - -861.16371424 = 2.238 eV

Supplementary Note 8: Additional first-principles calculations

Calculation Method：First-principles calculations are performed by vienna ab initio simulation package (VASP)1–5. The generalized gradient approximation(GGA) of Perdew-Burke-Ernzerhof (PBE) is used to describe the exchange-correlation functional. The cut-off energy for the plane wave basis is set to 400 eV and a 2×2×2 Monkhorst-pack mesh is employed. All the structures were fully relaxed (atomic position) up to 10-5 eV /Å force minimization and max force of 0.01 eV/ Å.

Molecular dynamics methodology: Each polymer chain consists of 14 DMS monomers arbitrarily cross-linked to represent a simplified photo-polymerization process. The choice of such a short chain with a consistent degree of polymerization is in accordance with many polymer composite models employed in MD simulations to improve computational efficiency whilst maintain essential polymer features such as contact resistance, glass transition behavior, and thermo-mechanical properties, etc.

And the nanorods were homogenously distributed in the resin matrix due to the periodic boundary conditions applied in the three dimensions.

Calculation parameters summary:

Cutoff energy: 400 eV

Electronic self-consistent convergence criterion: 10-5 eV/Å

Atomic relaxation convergence criterion: -0.01 eV/Å

K-point grid: 2×2×1

Functional: PAW-PBE

Figure S8-1. Structures used in calculations

a=4.485 nm, b=4.485 nm, c= 4.55 nm

Figure S8-2. CaF2/PDMS composites with a mass ratios of 10.25%

a=4.773 nm, b=4.773 nm, c= 4.55 nm

Figure S8-3. CaF2/PDMS composites with a mass ratios of 13.73%

a=4.972 nm, b=4.972 nm, c= 4.55 nm

Figure S8-4. CaF2/PDMS composites with a mass ratios of 16.64%

a=5.462 nm, b=5.462 nm, c= 4.55 nm

Figure S8-5. CaF2/PDMS composites with a mass ratios of 20.55%

a=6.342 nm, b=6.342 nm, c= 4.55 nm

Figure S8-6. CaF2/PDMS composites with a mass ratios of 22.57%

a=7.154 nm, b=7.154 nm, c= 4.55 nm

Figure S8-7. CaF2/PDMS composites with a mass ratios of 25.39%

Figure S8-8. Radius of gyration of CaF2/PDMS composites dependent on mass ratios

Figure S8-9. Volumetric hydrogen bonds of CaF2/PDMS composites

dependent on mass ratios

Figure S8-10. Volumetric binding energy of CaF2/PDMS composites

dependent on mass ratios

Figure S8-11. Young’s modulus of CaF2/PDMS composites dependent on mass ratios

Figure S8-12. Shear modulus of CaF2/PDMS composites dependent on mass ratios

a=3.657 nm、b=3.657 nm、c= 4.55 nm

Figure S8-13. CaF2/PDMS composites with a diameter of 1 nm

a=4.972 nm、b=4.972 nm、c= 4.55 nm

Figure S8-14. CaF2/PDMS composites with a diameter of 1.5 nm

a=5.872 nm、b=5.872 nm、c= 4.55 nm

Figure S8-15. CaF2/PDMS composites with a diameter of 2 nm

a=7.416 nm、b=7.416 nm、c= 4.55 nm

Figure S8-16. CaF2/PDMS composites with a diameter of 2.5 nm

Figure S8-17. Radius of gyration of CaF2/PDMS composites dependent on diameter

Figure S8-18. Volumetric hydrogen bonds of CaF2/PDMS composites

dependent on diameter

Figure S8-19. Volumetric binding energy of CaF2/PDMS composites

dependent on diameter

Figure S8-20. Young’s modulus of CaF2/PDMS composites dependent on diameter

Figure S8-21. Shear modulus of CaF2/PDMS composites dependent on diameter

a=5.462 nm、b=5.462 nm、c= 3.55 nm

Figure S8-22. CaF2/PDMS composites with a length of 3 nm

a=5.462 nm、b=5.462 nm、c= 4.55 nm

Figure S8-23. CaF2/PDMS composites with a length of 4 nm

a=5.462 nm、b=5.462 nm、c= 5.55 nm

Figure S8-23. CaF2/PDMS composites with a length of 5 nm

a=5.462 nm、b=5.462 nm、c= 6.55 nm

Figure S8-24. CaF2/PDMS composites with a length of 6 nm

Figure S8-25. Radius of gyration of CaF2/PDMS composites dependent on length

Figure S8-26. Volumetric hydrogen bonds of CaF2/PDMS composites

dependent on length

Figure S8-27. Volumetric binding energy of CaF2/PDMS composites

dependent on length

Figure S8-28. Young’s modulus of CaF2/PDMS composites dependent on length

Figure S8-29. Shear modulus of CaF2/PDMS composites dependent on length

a=4.513 nm、b=4.513 nm、c= 4.55 nm

Figure S8-30. Lu3Al5O12/PDMS composites with a mass ratios of 10.31%

a=4.773 nm, b=4.773 nm, c= 4.55 nm

Figure S8-31. Lu3Al5O12/PDMS composites with a mass ratios of 13.78%

a=5.027 nm、b=5.027 nm、c= 4.55 nm

Figure S8-32. Lu3Al5O12/PDMS composites with a mass ratios of 16.61%

a=5.496 nm、b=5.496 nm、c= 4.55 nm

Figure S8-33. Lu3Al5O12/PDMS composites with a mass ratios of 20.57%

a=6.387 nm、b=6.387 nm、c= 4.55 nm

Figure S8-34. Lu3Al5O12/PDMS composites with a mass ratios of 22.62%

a=7.208 nm、b=7.208 nm、c= 4.55 nm

Figure S8-35. Lu3Al5O12/PDMS composites with a mass ratios of 25.43%

Figure S8-36. Radius of gyration of Lu3Al5O12/PDMS composites

dependent on mass ratios

Figure S8-37. Volumetric hydrogen bonds of Lu3Al5O12/PDMS composites

dependent on mass ratios

Figure S8-38. Volumetric binding energy of Lu3Al5O12/PDMS composites

dependent on mass ratios

Figure S8-39. Young’s modulus of Lu3Al5O12/PDMS composites

dependent on mass ratios

Figure S8-40. Shear modulus of Lu3Al5O12/PDMS composites

dependent on mass ratios

a=3.692 nm、b=3.692 nm、c= 4.55 nm

Figure S8-41. Lu3Al5O12/PDMS composites with a diameter of 1 nm

a=5.027 nm、b=5.027 nm、c= 4.55 nm

Figure S8-42. Lu3Al5O12/PDMS composites with a diameter of 1.5 nm

a=5.916 nm、b=5.916 nm、c= 4.55 nm

Figure S8-43. Lu3Al5O12/PDMS composites with a diameter of 2 nm

a=7.484 nm、b=7.484 nm、c= 4.55 nm

Figure S8-44. Lu3Al5O12/PDMS composites with a diameter of 2.5 nm

Figure S8-45. Radius of gyration of Lu3Al5O12/PDMS composites

dependent on diameter

Figure S8-46. Volumetric hydrogen bonds of Lu3Al5O12/PDMS composites

dependent on diameter

Figure S8-47. Volumetric binding energy of Lu3Al5O12/PDMS composites

dependent on diameter

Figure S8-48. Young’s modulus of Lu3Al5O12/PDMS composites

dependent on diameter

Figure S8-49. Shear modulus of Lu3Al5O12/PDMS composites dependent on diameter

a=5.496 nm、b=5.496 nm、c= 3.55 nm

Figure S8-50. Lu3Al5O12/PDMS composites with a length of 3 nm

a=5.496 nm、b=5.496 nm、c= 4.55 nm

Figure S8-51. Lu3Al5O12/PDMS composites with a length of 4 nm

a=5.496 nm、b=5.496 nm、c= 5.55 nm

Figure S8-52. Lu3Al5O12/PDMS composites with a length of 5 nm

a=5.496 nm、b=5.496 nm、c= 6.55 nm

Figure S8-53. Lu3Al5O12/PDMS composites with a length of 6 nm

Figure S8-54. Radius of gyration of Lu3Al5O12/PDMS composites

dependent on length

Figure S8-55. Volumetric hydrogen bonds of Lu3Al5O12/PDMS composites dependent on length

Figure S8-56. Volumetric binding energy of Lu3Al5O12/PDMS composites

dependent on length

Figure S8-57. Young’s modulus of Lu3Al5O12/PDMS composites dependent on length

Figure S8-58. Shear modulus of Lu3Al5O12/PDMS composites dependent on length

Supplementary Note 9: Other factors affecting ML intensity

Figure S9-1. ML intensity of CaF2:Tb3+/PDMS dependent on stretching speeds

The Figure S9-1 reveals a positive correlation between ML intensity and stretching speed, with greater ML intensity observed at higher stretching speeds. This can be attributed to the higher pulling force required for faster stretching speeds, which increases the probability of phosphor particles separation from the PDMS.

Figure S9-2. Transient stress distribution during stretching

Figure S9-2 displays the transient stress distribution of the sample during stretching, while Figure S9-3 depicts the stress curves of the composite center at various tensile speeds. The stress propagates in waves during stretching, and when the stretching speed is too slow (<6 mm/s), the stress is insufficient to excite ML, which agrees with the experimental findings.

Figure S9-3. Stress curve at the center of the elastomer

dependent on stretching speeds

Figure S9-4. ML intensities of the elastomer dependent on temperature

Figure S9-5. ML intensities of the elastomer dependent on relative humidity.

References

1.	Momma, K. & Izumi, F. VESTA 3 for three-dimensional visualization of crystal, volumetric and morphology data. Journal of applied crystallography 44, 1272–1276 (2011).

2.	Wang, V., Xu, N., Liu, J.-C., Tang, G. & Geng, W.-T. VASPKIT: A user-friendly interface facilitating high-throughput computing and analysis using VASP code. Computer Physics Communications 267, 108033 (2021).

3.	Perdew, J. P., Burke, K. & Ernzerhof, M. Generalized gradient approximation made simple. Physical review letters 77, 3865 (1996).

4.	Kresse, G. & Joubert, D. From ultrasoft pseudopotentials to the projector augmented-wave method. Physical review b 59, 1758 (1999).

5.	Kresse, G. & Furthmüller, J. Efficiency of ab-initio total energy calculations for metals and semiconductors using a plane-wave basis set. Computational materials science 6, 15–50 (1996).

6.	https://github.com/makerbase-mks/MKS-GEN_L

7.	https://github.com/MarlinFirmware/Marlin

8.	Wang, W. et al. Contact electrification induced mechanoluminescence. Nano Energy 94, 106920 (2022).

9.	Lin, F. et al. Modeling polyhedron distortion for mechanoluminescence in mixed-anion compounds RE2O2S: Ln3+. Chemistry of Materials 34, 5311–5319 (2022).

10.	Huang, N.-J. et al. Efficient interfacial interaction for improving mechanical properties of polydimethylsiloxane nanocomposites filled with low content of graphene oxide nanoribbons. RSC advances 7, 22045–22053 (2017).