Enhanced Photocatalytic activity of bio mediated Ag@Cu2O NPs towards Fampridine: Kinetic modelling and mechanistic pathways

Pratibha Attri1, Sangeeta Garg1*, Jatinder Kumar Ratan1, Ardhendu Sekhar Giri2

1Department of Chemical Engineering, Dr. B.R. Ambedkar National Institute of Technology, Jalandhar, India.

2Department of Chemical Engineering, Indian Institute of Science Education and Research, Bhopal, India.

*E-mail: [gargs@nitj.ac.in]

Supplementary Data

1. S Analytical methods for Adsorption

Langmuir, Freundlich, Sips, Hill and  Koble-Carrigan isotherms using a non-linear equation (Eq. 1S) [1].

q= Q0bCe1+bCe                                                                       (1)

Freundlich isotherm refers to multilayer adsorption with a non-uniform adsorption distribution. The isotherm of this sort have slope ranging from 0 to 1 represents adsorption intensity or surface heterogeneity. A value less than one indicates a chemisorption process, while 1/n greater than one indicates cooperative adsorption [2] Non-linearized for of it (Eq. 2).

qe= KfCe1/n                                                                                              (2)

Sips isotherm, which is derived from the Langmuir and Freundlich isotherms, is utilised for the heterogeneous adsorption system. When n = 1, the Sips equation is interpreted as the Langmuir equation, implying a homogenous adsorption process[3]. Heterogeneity was described by deviations from unity; the Sips non-linear equation is (Eq. 3).

qe=qmsKsCens1+KsCens                                                                                                  (3)

To have a clear grasp of the adsorption process of Fampridine over Ag@Cu2O NPs Koble-Carrigan and Hill isotherms were also implemented to experimental data. Langmuir and Freundlich, both isotherm were utilised to depict the non-linear equation of Koble-Carrigan isotherm is (Eq. 4)[4].

qe= aCen1+bCen                                                                                                       (4)

Different species binding onto homogeneous substrates was explained by the Hill adsorption isotherm. According to Hill isotherm adsorption was a cooperative phenomenon, by binding at one site on the adsorbent. Non-ideal competitive adsorption (NICA) non-linear form of Hills isotherm was expressed as follows

qe= qshCenhKd+Cenh                                                                                                             (5)

Fig. S.1. LC-MS of plant exctract (T. divaricate).

Fig. S2. EDX mapping of Ag@Cu2O NPs using plant extract (T. divaricate).

Fig. S3. Mass spectra of Fampridine degradation of 210 min on Ag@Cu2O NPs at optimum conditions

| FT-IR | Peaks (cm-1) | Functional groups and Structure | FT-IR |  | Peaks (cm-1) | Functional groups and Structure |
| --- | --- | --- | --- | --- | --- | --- |
| Plant Extract | 3310 | O-H (Alcohol, Water and Phenol) | Cu2O NPs |  | 3151 | O-H (Alcohol, Water and Phenol) |
|  | 1637 | C-O (Carboxyl ) |  |  | 2119 | (Alkynes) |
|  |  |  |  |  | 1585 | -C-C- Aromatics |
|  | 2123 | (Alkynes) |  |  | 610 | -M-O- Metal oxide |
| FT-IR | Common Peaks (cm-1) |  |  | Functional groups and Structure |  |  |
| Ag@Cu2O NPs | 3548 |  |  | O-H (Alcohol, Water and Phenol) |  |  |
|  | 2126 |  |  | (Alkynes) |  |  |
|  | 1804 |  |  | C=O Carboxyl bond |  |  |
|  | 1423 |  |  | N-O Nitro compound |  |  |
|  | 1353 |  |  | C-H Alkane |  |  |
|  | 617 |  |  | -M-O- Metal oxide |  |  |

Table S1. FT-IR peaks analaysis and comparasion for plant extract, Cu2O NPs and Ag@Cu2O NPs.

Table S2. XRD analysis peaks of Cu2O NPs and Ag@Cu2O NPs

| NPs | 2θ | FWHM | d-spacing [Å] | Rel. Int. [%] | hkl |
| --- | --- | --- | --- | --- | --- |
| Cu2O | 36.44 | 0.096 | 2.46 | 100 | (111) |
|  | 42.32 | 0.1344 | 2.13 | 27.8 | (022) |
|  | 61.40 | 0.1344 | 1.50 | 17.54 | (113) |
|  | 73.55 | 0.1536 | 1.28 | 9.91 | (222) |
| Ag@Cu2O | 36.99 | 0.1152 | 2.42 | 83.1 | (111) |
|  | 37.19 | 0.2304 | 2.41 | 77.9 | (111) |
|  | 39.24 | 0.096 | 2.29 | 8.3 | (002) |
|  | 41.12 | 0.3072 | 2.19 | 2.61 | (002) |
|  | 44.98 | 0.1152 | 2.04 | 16.63 | (022) |
|  | 62.55 | 0.4608 | 1.48 | 1.61 | (022) |
|  | 64.93 | 0.2304 | 1.44 | 9.74 | (113) |
|  | 75.74 | 0.4608 | 1.25 | 3.36 | (113) |

Table S3. Binding energy, area of peaks and Atomic concentration of elements analysed in the XPS spectrum of Ag@Cu2O NPs.

| Elements | Binding energy (eV) | Area (CPS eV) | Atomic (%) |
| --- | --- | --- | --- |
| Cu2p | 930.64 ± 0.10 | 980.27 | 24.5 |
|  | 931.34 ± 0.10 | 2279.59 |  |
|  | 941.92 ± 0.50 | 682.20 |  |
|  | 949.87 ± 0.010 | 397.55 |  |
|  | 951.21 ± 0.10 | 1015.21 |  |
|  | 960.64 ± 0.10 | 362.26 |  |
| Ag3d | 366.70 ± 0.12 | 321.50 | 3.01 |
|  | 367.04 ± 0.05 | 378.35 |  |
|  | 372.78 ± 0.07 | 460.05 |  |
| O1s | 528.32 ± 0.32 | 322.14 | 30.45 |
|  | 529. 72 ± 0.10 | 1021.74 |  |
|  | 530.25 ± 0.04 | 1589.90 |  |
| C1s | 282.43 ± 0.01 | 517.67 | 41.47 |
|  | 283.68 ± 0.01 | 145.86 |  |

# 2. S. Proposed mechanism for production of OH• using Ag@Cu2O NPs

Improved mechanism for  production of OH• and superoxide radical using  Ag@Cu2O NPs, in comparision to Cu2O NPs due to reduced recombination rate of electron and hole pairs is described from Eq. 6 to 22.

Cu2O+hv → e- Cu2 O+ h+Cu2O                                                                      (6)

Cu2O+H2O+2e-→2Cu+2OH-                                                                             (7)

Cu2O+2OH-→2CuO+H2O+2e-                                                                          8

e-Cu2O+ h+Cu2O→recombination                                                               (9)

e- Cu2O+ O2→O2-+H2O→HO2•+ OH-                                                            (10)

h+ Cu2O+ OH-→OH•                                                                                                   11

H2•+HO2•→ H2O2+O2                                                                                                       12

H2O2→decomposition                                                                                                       13

H2O2+ e- Cu2O→ OH•+OH-                                                                                   (14)

OH•+ Fampridine →Degraded products                                                                      (15)

h+ Cu2O+Fampridine→oxidation →Degradation                                                 (16)

The decomposition mechanism involved in degradation of Fampridine onto Ag@Cu2O NPs is expressed as follow:

Ag@Cu2O + hν visible light→Ag@Cu2O h++ e-                                                 (17)

e-+ O2→ O2- ∙                                                                                                                            (18)

O2-∙+ e-+ 2H+→ H2O2                                                                                                         (19)

H2O2+ e-+ H+→H2O+ OH∙                                                                                              (20)

h++ H2O → H++ OH∙                                                                                                             (21)

Fampridine+Active species OH∙, h+ →degraded intermediates                              (22)

As a result of above mechanism Fampridine molecules showed the higher degradation rate when exposed to visible light.

References

[1]	P. Nanta, K. Kasemwong, W. Skolpap , J. Environ. Chem. Eng. 6 (2018) 794–802.

[2]	J. López-Luna, L.E. Ramírez-Montes, S. Martinez-Vargas, A.I. Martínez, O.F. Mijangos-Ricardez, M. del C.A. González-Chávez, R. Carrillo-González, F.A. Solís-Domínguez, M. del C. Cuevas-Díaz, V. Vázquez-Hipólito, SN Appl. Sci. 1 (2019) 1–19.

[3]	A.A. Romzi, M.R.R. Kooh, L.B.L. Lim, N. Priyantha, C.M. Chan, Int. J. Environ. Anal. Chem. 00 (2021) 1–20.

[4]	P. Senthil Kumar, S. Ramalingam, C. Senthamarai, M. Niranjanaa, P. Vijayalakshmi, S. Sivanesan, Desalination. 261 (2010) 52–60.