Electronic Supplementary Material

Polyoxometalate decorated gold nanoparticles inhibit β-amyloid aggregation and cross the blood brain barrier in a µphysiological model.

Marta Perxés Perich1,2,†,╡, Sujey Palma-Florez2†, Clara Solé2, Sara Goberna-Ferrón1,╧, Josep Samitier2,3,4, Pedro Gómez-Romero1, Mònica Mir2,3,4,& () and Anna Lagunas2,3,& (), 1. Catalan Institute of Nanoscience and Nanotechnology, ICN2 (CSIC-BIST), Campus UAB, Bellaterra, Barcelona, E-08193, Spain. 2. Nanobioengineering Group, Institute for Bioengineering of Catalonia (IBEC) Barcelona Institute of Science and Technology (BIST), 08028 Barcelona, Spain. 3. CIBER-BBN, ISCIII, 28029 Madrid, Spain. 4. Department of Electronics and Biomedical Engineering, University of Barcelona, Martí i Franquès 1, 08028 Barcelona, Spain. † Both authors contributed equally. & Both authors contributed equally. ╡Materials Chemistry and Catalysis, Debye Institute for Nanomaterials Science, Utrecht University, 3584 CG Utrecht, The Netherlands ╧Instituto Universitario de Tecnología Química (CSIC-UPV), Universitat Politècnica de València, Avda. De los Naranjos s/n, Valencia 46022, Spain

Figure S1. Histogram of citrate capped gold nanoparticles (AuNPs@SC), fitted to a LogNormal distribution with the following parameters: Center = 15.95 nm, offset = 5,06 and log standard deviation = 0.11 nm. The size distribution was obtained by measuring the size of n = 522 particles from three different synthesis batches in Bright Field Scanning Transmission Electron Microscopy (BF-STEM) images.

Table S1:  IR peaks of different compounds synthetized compared in the last two columns with the literature.

| AuNPs@ POM | AuNPs@POM@PEG | POM | POM 1,2 | PEG 3 |
| --- | --- | --- | --- | --- |
|  | 1350.2 |  |  | 1343 |
|  | 1298.1 |  |  | 1279 |
|  | 1249.9 |  |  | 1240 |
|  | 1137.5 |  |  | 1130 |
|  | 1095.6 |  |  | 1094 |
| 987.6 | 987.6 | 989,5 | 988 |  |
| 943.2 | 941.3 | 943,2 | 945 | 951 |
| 869.9 | 868.0 | 872,9 | 875 |  |
| 858.3 | 852.5 | 852,5 | 855 | 840 |
| 798.5 | 796.6 | 790,8 | 805 |  |
| 731.0 | 727.2 | 713,7 | 730 |  |
| 513.1 | 509.2 | 505,6 |  |  |

Scheme S1. Structure of the β2 isomer of the monolacunary Keggin ion [SiW11O39]-8 with labelling of the different oxygen atoms. WO6 octahedra (blue) and SiO4 tetrahedra (yellow). Adapted from (Chermette and Lefebvre, 2012). 4

Figure S2. Non normalized UV-Vis spectra of AuNPs@POM@PEG in PBS after up to 14 weeks, showing particle long-term stability.

Figure S3. XPS spectra of AuNPs@POM. On the left, Au peaks. On the right, W peaks.

Figure S4. Representative fluorescence images of the Live/Dead assay obtained for endothelial cells under different treatment conditions. Green, red and blue signal indicate alive, death cells and cell nuclei, respectively.

References

1	A. Tézé and G. Hervé, Journal of Inorganic and Nuclear Chemistry, 1977, 39, 999–1002.

2	Alvin P. Ginsberg, Ed., Inorganic Syntheses, John Wiley & Sons Ltd, New York, 1991.

3	K. Shameli, M. Bin Ahmad, S. D. Jazayeri, S. Sedaghat, P. Shabanzadeh, H. Jahangirian, M. Mahdavi and Y. Abdollahi, Int J Mol Sci, 2012, 13, 6639–6650.

4	H. Chermette and F. Lefebvre, Comptes Rendus Chimie, 2012, 15, 143–151.