Appendix A.Supplementary date

Efficient Fluoride Removal Using Nano MgO: Synthesis, Mechanisms, and Performance Evaluation

BoWen Liua, Li Ai a, Ming Leia*, Hongfei Linb,c*

a Guangxi Key Laboratory of Chemistry & Engineering of Forest Products, School of Chemistry and Chemical Engineering, Guangxi Minzu University, Nanning 530006, China

b Guangxi Bossco Environmental Protection Technology Co., Ltd, Nanning 530007, China

c Guangxi Key Laboratory of Environmental Pollution Control and Ecological Restoration Technology, Nanning 530007, China

Corresponding Author: Ming Lei (leiming801015@yeah.net)；linhf@bossco.cc

The Langmuir adsorption model is used to calculate the maximum adsorption capacity, which can be expressed in the following form [1]:

(1)

where Ce is the equilibrium concentration of the anions in solution (mg/L); qe is the amount of anions adsorbed per unit mass of adsorbent at equilibrium (mg/g); qm denotes the theoretical saturated adsorption capacity (mg/g); b is Langmuir constant related to adsorption-desorption energy and affinity of binding sites for anions (L/mg).

The pseudo-second-order model has been widely used to describe the fluoride adsorption from aqueous solution. It can be expressed in the following form[2, 3]:

(2)

where qt and qe are the adsorption capacity at time t and equilibrium, respectively; k2 is pseudo-second-order rate constants. On the basis of the experimental data, the adsorption capacity of qe, qt and k2 could be concluded from the slope and intercept respectively.

Fig. S1 Adsorption isotherm of nano MgO for fluoride adsorption (C0 = 10-100 mg/L, pH = 6.5, 1 g/L, 25-45℃)

Table S1 Langmuir adsorption isotherm parameters for fluoride on nano MgO

| T (℃) | Langmuir parameters |  |  |
| --- | --- | --- | --- |
|  | Qe (mg/g) | KL (Lm/mol) | R2 |
| 25 | 122.27178 | 0.04118 | 0.97738 |
| 35 | 122.47078 | 0.0202 | 0.96312 |
| 45 | 122.0839 | 0.07839 | 0.95376 |

Table S2 Langmuir and Freundlich adsorption isotherm parameters for fluoride on nano MgO.

| Adsorbents | Langmuir parameters |  |  | Freundlich parameters |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Qe (mg/g) | KL (Lm/mol) | R2 | KF (g/L) | 1/n | R2 |
| MgO | 122.27178 | 0.04118 | 0.97738 | 3.87636 | 0.72185 | 0.96788 |

Table S3 Kinetic parameters for fluoride adsorption on the nanoMgO.

| Adsorbents |  | Pseudo-first-order kinetic model log (qe-qt) = logqe-k1t |  |  | Pseudo-second-order kinetic model t/qt = 1/ (k2qe2)+t/qe |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Qe,exp (mg/L) | k1 (1/min) | qe1 (mg/L) | R2 |  | k2 (g/(mg·min) | qe2 (mg/L) | R2 |
| MgO | 19.249 | 0.0599 | 18.0735 | 0.96438 |  | 0.00404 | 19.83744 | 0.98374 |

References:

[1] D. Kang, X. Yu, S. Tong, M. Ge, J. Zuo, C. Cao, W. Song (2013) Performance and mechanism of Mg/Fe layered double hydroxides for fluoride and arsenate removal from aqueous solution. Chem Eng J 228: 731-740. https://doi.org/10.1016/j.cej.2013.05.041

[2] R.M. Dhoble, S. Lunge, A.G. Bhole, S. Rayalu (2011) Magnetic binary oxide particles (MBOP): A promising adsorbent for removal of As (III) in water. Water Res 45: 4769-4781. https://doi.org/10.1016/j.watres.2011.06.016

[3] J.M. Gong, T. Liu, X.Q. Wang, X.L. Hu, L.Z. Zhang (2011) Efficient Removal of Heavy Metal Ions from Aqueous Systems with the Assembly of Anisotropic Layered Double Hydroxide Nanocrystals@Carbon Nanosphere, Environ Sci Technol 45: 6181-6187. https://doi.org/10.1021/es200668q