Supporting Information

Preparation of chitosan-iron oxide modified sludge-based biochar for effective removal of tetracycline from water: performance and mechanism

Yangyang Yanga, b, Shihao Lia, Zhenting Zhua, Lei Wana, Xun Wangb, Jun Houb, Songqi Liuc, Xiulei Fana*

a School of Environmental Engineering, Jiangsu Key Laboratory of Industrial Pollution Control and Resource Reuse, Xuzhou University of Technology, Xuzhou 221018, China

b Key Laboratory of Integrated Regulation and Resources Development on Shallow Lakes, Ministry of Education, College of Environment, Hohai University, Nanjing 210098, China

c School of Environmental Science and Engineering, Suzhou University of Science and Technology, Suzhou 215009, China

*Corresponding author:

E-mail: xlfan@xzit.edu.cn

Address: School of Environmental Engineering, Jiangsu Key Laboratory of Industrial Pollution Control and Resource Reuse, Xuzhou University of Technology, Xuzhou, 221018, China

# Statistical data analysis

The Raman, BET, and XPS characterization of 800BC and 800KBC.

| Fig.S1. Pore size distribution of BC800 (a) and KBC800 (b); The Raman spectra of KBC800 before (c) and after the degradation experiment (d); The XPS spectra of KBC800 before (e) and after the degradation experiment (f); The high-resolution XPS spectra of KBC800 before (g) and after (h) the degradation experiment. |  |
| --- | --- |