Synergy Effect of Nitrogen and Molybdenum on Activated Carbon Matrix for Selective Adsorptive Desulfurization:  Insights into Surface Chemistry Modification

Musa O. Azeez, Abdulkadir Tanimu, Khalid Alhooshani, Saheed A. Ganiyu*.

Department of Chemistry, King Fahd University of Petroleum & Minerals, 31261, Dhahran, Saudi Arabia.

Supplementary Information

EDX analysis of adsorbents

Fig. SI-1:  EDS images of (a) AC (b) AC-N (c) AC-N-Mo and (d) AC-Mo

Table SI-1:   Surface atomic percent of elements present in modified carbon.

| States | C1s | C1s | N1s | N1s | N1s | O1s | O1s | O1s | O1s | Mod3 | Mod3 | Mod3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BE (eV) | 284.5 | 283 | 396 | 398 | 401.6 | 530.2 | 530.8 | 530.9 | 531 | 227.8 | 230.8 | 233 |
| AC-N | 23.7 | 33.66 | 3.33 | - | - | - | 39.31 | - | - | - | - | - |
| AC-N-Mo | 16.89 | 32.83 | 1.97 | 0.93 | 0.28 | - | - | 46.8 | - | 0.18 | 0.09 | 0.03 |

NH3-TPD analysis of sorbents

Fig. SI-2:  Surface acidity by ammonia-temperature-programmed desorption (NH3-TPD) of adsorbents (A) AC (B) AC-N (C) AC-N-Mo and (D) AC-Mo

Table SI-2:   NH3-TPD of the adsorbents

| Adsorbents | Temp. (s) (oC) | Quantity (mmol/g at STP) |
| --- | --- | --- |
| AC | 410, 844 | 4.67, 0.31 |
| AC-N | 485 | 8.03 |
| AC-N-Mo | 421, 856, 935 | 6.23, 1.84 |
| AC-Mo | 214, 400, 847 | 0.22, 2.59, 0.60 |

Adsorption kinetics

Pseudo-first order equation as given by Lagergren 1988 is as shown in equation 4 below.

ln (qe  - qt)=lnqe - k1t……………4

Where qe  (mg/g) and qt (mg/g) denote quantity of sulfur adsorbed at equilibrium and time t (min) respectively, k1 (min-1) represents rate constant for pseudo- first order kinetics.

Fig. SI-3: Pseudo first order kinetics at the concentration of (a) 50 mg-S/L, (a) 100 mg-S/L, (a) 150 mg-S/L, (a) 200 mg-S/L

Pseudo-second order equation and the interpretation of the terms are expressed in equation 5 below:

tqt= 1k2qe2+ tqe……………5

Where qe (mg/g) and qt (mg/g) denote quantity of sulfur adsorbed at equilibrium and time t (min) respectively, k2 (g/(mg-S.min)) represents rate constant for pseudo second order kinetics model. The value of 1qe and 1k2qe2 are both obtained from the slope and intercept of the plot of tqt versus t.

Fig. SI-4: Pseudo second order kinetics at the concentration of (a) 50 mg-S/L, (a) 100 mg-S/L, (a) 150 mg-S/L, (a) 200 mg-S/L

Intraparticle-diffusion equation as given by Weber and Morris and the interpretation of the terms are given in equation 6 below:

qt=Ki.dt1/2+C……….. 6

Where qt (mg/g),  t1/2 (min1/2), Ki.d (mg/g.min), and C(mg/g) represent quantity of sulfur adsorbed at equilibrium, the square root of the contact time, the intraparticle diffusion rate constant and boundary layer thickness respectively.

Fig. SI-5: Intraparticle diffusion at the concentration of 100 mg-S/L

Fig. SI-6: Graphs of sulfur content as a function of concentration and quantity adsorbed at different time intervals

Table SI-3: Kinetic parameter of 100 mg-S/L on the investigated adsorbent materials

| 100 mg-S/L |  | Pseudo-first order |  |  |  | Pseudo-second order |  |  |  | Intraparticle diffusion |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorbent | qe(exp)a | qe(cal)a | k1(103)b | R2 |  | qe(cal)a | k2(103)c | R2 |  | Ki.d | C | R2 |
| AC | 17.96 | 2.57 | 2.7 | 0.7573 |  | 16.92 | 20.6 | 0.9999 |  | 0.1221 | 14.768 | 0.8270 |
| AC-N | 17.84 | 5.89 | 4.6 | 0.9213 |  | 17.01 | 4.9 | 0.9996 |  | 0.3579 | 10.404 | 0.9061 |
| AC-N-Mo | 19.94 | 6.92 | 2.4 | 0.9221 |  | 17.15 | 5.7 | 0.9989 |  | 0.2829 | 11.786 | 0.9340 |
| AC-Mo | 17.98 | 3.27 | 4.3 | 0.9760 |  | 17.42 | 9.5 | 0.9994 |  | 0.1659 | 14.151 | 0.9581 |

a: (mgS/g), b: (min-1), c: g/(mg-S.min)

Adsorption Isotherms

The Langmuir linear equation expressed in equation 7 governs the quantity of DBT adsorbed.

Ceqe=1kLqm+Ceqm……….. 7

Where Ce (mg/L), qe (mg/g), qm (mg/g) and kL represent equilibrium concentration, sorption capacity and maximum adsorption capacity, Langmuir constant related to adsorption energy respectively. The expression 1qm and 1kLqm are obtained from the slope and intercept of the plot of Ceqe  versus Ce.

The Freundlich isotherm is represented in equation 8 below;

lnqe=lnKF+1nlnCe…………8

Where KF (mg g-1) and n represents Freundlich constant related to adsorption capacity, and intensity respectively.

Fig. SI-7: Adsorption isotherm of adsorbents by Langmuir and Freundlich. (Initial conc. = 50-250 mg-S/L contact time = 24 h, adsorbent dosage = 100 mg, and 20 mL solution of isooctane containing DBT)

Table SI-4:   Isotherm parameters for adsorption of 50-200 mg-S/L DBT on adsorbent materials

|  | Langmuir |  |  |  |  | Freundlich |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Adsorbent | aqmax | bKL | R2 | RL |  | CKF | 1/n | n | R2 |
| AC | 41.3 | 0.056 | 0.9662 | 0.26 |  | 4.24 | 0.5246 | 1.90 | 0.9110 |
| AC-N | 43.9 | 0.052 | 0.9508 | 0.16 |  | 3.96 | 0.5546 | 1.80 | 0.9413 |
| AC-N-Mo | 36.1 | 0.118 | 0.8409 | 0.05 |  | 3.05 | 0.6383 | 1.57 | 0.9997 |
| AC-Mo | 42.9 | 0.060 | 0.9207 | 0.08 |  | 4.36 | 0.5397 | 1.85 | 0.9422 |

a: (mgS/g), b: (L/mg), c: (𝑚𝑔(1− 1 /𝑛 ) 𝑆 × 𝐿 1⁄𝑛 × 𝑔 −1)