Supplementary Materials

Superconductivity in a breathing kagome metals ROs2 (R = Sc, Y, Lu)

Karolina Górnicka1,2,3, Michał J. Winiarski1,2, Dorota I. Walicka3 and Tomasz Klimczuk1,2

1 Faculty of Applied Physics and Mathematics, Gdansk University of Technology,

ul. Narutowicza 11/12, 80-233 Gdańsk, Poland,

2Advanced Materials Centre, Gdansk University of Technology,

ul. Narutowicza 11/12, 80-233 Gdańsk, Poland,

3 Department of Quantum Matter Physics, University of Geneva,

24 Quai Ernest-Ansermet, 1211 Geneva 4, Switzerland.

Powder x-ray diffraction

Figure S1 presents the powder x-ray diffraction pattern for ScOs2, YOs2 and LuOs2 together with the LeBail refinement. All compounds crystallize in hexagonal centrosymmetric MgZn2 – type structure (P63/mmc, No. 194).

Figure S1. Powder x-ray diffraction pattern (pXRD) (red points) together with the LeBail refinement profile (black solid line) for ROs2 (R=Sc, Lu and Y) compounds.

Figure S2 presents a schematic view of the hexagonal structure of ROs2. The 4f (1/3, 2/3, z) site is occupied by RE atoms and the 2a (0,0,0) and 6h (x, 2x, 1/4) sites are occupied by Os atoms.

Figure S2. Crystal structure of ROs2 viewed along different orientations with R and

Os atoms represented by yellow and blue balls, respectively.

Magnetic property measurements

Figure S3 depicts the magnetization as a function of magnetic field at several, selected temperatures below the superconducting transition temperature Tc for all studied compounds. For each temperature, the experimental data obtained in small magnetic fields were fitted using the proportionality Mfit = −aH, appropriate for a full Meissner state. Comparing the value of prefactor a derived from the isotherm taken at T = 1.7 K with the ideal diamagnetism quantified as −1/4π, the demagnetization factor (N = 0.33-0.73) for all Laves compounds was found.

Figure S3.  The field-dependent magnetization curves M(H) for ScOs2, YOs2, and LuOs2 taken at different temperatures.

Electrical resistivity measurements

For a single-band type-II BCS superconductor, the orbital upper critical field at 0 K can be estimated from the Werthamer–Helfand–Hohenberg expression1,2:

|  | μ0Hc20=-ATcdμ0Hc2dT T=Tc | (1) |
| --- | --- | --- |

where A is the purity factor given by 0.693 for the dirty limit. Table S1 presents the µ0Hc2(0) value obtained from WHH and GL models for all investigated compounds.

Table S1. The upper critical field µ0Hc2(0) estimated from WHH and GL models.

| 0Hc2(0) | Unit | ScOs2 | YOs2 | LuOs2 |
| --- | --- | --- | --- | --- |
| GL | T | 2.58(1) | 2.23(2) | 1.64(5) |
| WHH | T | 1.90 | 1.62 | 1.37 |
| µ0Hc2p0 | T | 9.90 | 8.40 | 6.4 |

References

1.	Helfand, E. & Werthamer, N. R. Temperature and Purity Dependence of the Superconducting Critical Field, H c 2 . II. Phys. Rev. 147, 288–294 (1966).

2.	Werthamer, N. R., Helfand, E. & Hohenberg, P. C. Temperature and Purity Dependence of the Superconducting Critical Field, H c 2 . III. Electron Spin and Spin-Orbit Effects. Phys. Rev. 147, 295–302 (1966).