Supplementary information

Water-stable boroxine structure with dynamic covalent bonds

Xiaopei Li1,2,#, Yongjie Zhang2,#, Zhenqiang Shi1, Dongdong Wang1, Hang Yang1, Yahui Zhang1, Haijuan Qin3, Wenqi Lu1, Junjun Chen1, Yan Li1 and Guangyan Qing1,4,*

1CAS Key Laboratory of Separation Science for Analytical Chemistry, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian, P. R. China.

2Instrumental Analysis Center, School of Textile and Material Engineering, Dalian Polytechnic University, Dalian, P. R. China.

3Research Centre of Modern Analytical Technology, Tianjin University of Science &

Technology, Tianjin, P. R. China

4College of Chemistry and Chemical Engineering, Wuhan Textile University, Wuhan, P. R. China.

*Corresponding authors: qinggy@dicp.ac.cn

#X.L. and Y.Z. contributed equally to this work

Table of contents

Supplementary Materials and Measurements	2

Supplementary Figures 1–26	4

Supplementary Tables 1–9	34

References	46

Supplementary Materials and Measurements

Materials: Ethylenediamine (>99%), 2-hydroxyphenylboronic acid (HO-PBA, 97%), 10-hydroxybenzo[h]quinoline (HBQ, 98%), 4-formylphenylboronic acid (97%), boron tribromide (99.9% metals basis), and glycidyl methacrylate (GMA, 97%) were purchased from Aladdin reagent (Shanghai, China). 2-hydroxy-5-methylphenylboronic acid (CH3-HO-PBA, 97%) was purchased from Bide Pharmatech (Shanghai, China). 2-hydroxy-4-(trifluoromethyl)phenylboronic acid (CF3-HO-PBA, 98%) and (4-Formyl-2-methoxyphenyl)boronic acid (98%) were purchased from Leyan (Shanghai, China). 4-cyano-4-(phenylcarbonothioylthio)pentanoic acid (CPA, >97%) and dry methanol (99.9%, Water≤50 ppm) were purchased from macklin (Shanghai, China). Dry dichloromethane (99.9%, Water≤30 ppm) was obtained from J&K Scientific. Poly(ethylene glycol) methyl ether acrylate (PEGMEA, average Mn 480) was purchased from Sigma–Aldrich. Azobisisobutyronitrile (AIBN) was obtained from Tianjin guangfu fine chemical research institute. Other reagents and solvents were obtained from commercial suppliers. Unless otherwise noted, chemicals were used as received.

Measurements: Fluorescence spectra were measured on a PerkinElmer FL6500 fluorescence spectrometer with a 1 cm path−length quartz cell. Fluorescence absolute quantum yields of the liquid and solid samples were determined by an Edinburgh FLS980 spectrometer with an integrating sphere. Scanning electron microscope (SEM) measurements were carried out on a JEOL JSM−7800F instrument. For the liquid samples, SEM samples were prepared by dropping one droplet of water–THF (2:3, v/v) solution of HO-PBA, CH3-HO-PBA or CF3-HO-PBA onto clean silicon wafers and evaporating the solvent at room temperature and in open air. For solid samples, SEM samples were prepared by directly sticking the powder on the carbon tapes. Powder X-ray diffraction (XRD) patterns were collected by a PANAlytical X'pert Pro Powder X−ray diffractometer. The single−crystal XRD data were collected on a Bruker D8 Venture CMOS−based diffractometer (Mo–Kα radiation, λ=0.71073 Å) using the SMART and SAINT programs at 120 K. Final unit cell parameters were based on all observed reflections from integration of all frame data. The structures were solved in the space group by direct method and refined by the full−matrix least−squares using SHELXTL−97 fitting on F2. All non−hydrogen atoms were refined anisotropically. The hydrogen atoms were located geometrically and assigned fixed isotropic thermal parameters1. All nuclear magnetic resonance (NMR) experiments were performed on a Bruker AVANCE III 400 spectrometer equipped with a 5 mm BBFO probe. Fourier transform infrared (FT-IR) spectra were recorded on a Nicolet iS50 Fourier transform infrared (FT-IR) spectrometer equipped with an attenuated total reflection (ATR) accessory. The electrospray ionization quadrupole time-of-flight (ESI-Q-TOF) mass spectra were obtained on an Agilent 6540 Q-TOF mass spectrometer, and acetonitrile was used as mobile phase. Samples were dissolved in the solvent and ionized using an electrospray ionization (ESI) source in a negative mode. The ESI source parameters were as following: gas temperature 325 oC, drying gas 8 L·min−1, nebulizer 35 psig, capillary voltage 3500 V and m/z range 20–2000. An AB SCIEX TOF/TOF 5800 equipped with a neodymium: yttrium aluminum garnet (Nd: YAG) laser (349 nm wavelength) was used for matrix-assisted laser desorption ionization (MALDI)-TOF MS experiments. Trans-2-[3-(4-tert-butylphenyl)-2-methyl-2-propenylidene]malononitrile (DCTB) was used as a MALDI matrix. Silver trifluoroacetate (AgTFA) was used as cationization reagent. The sample (20 mg·mL−1), matrix (20 mg·mL−1) and cationization reagent (10 mg·mL−1) were, respectively, dissolved in dry THF. These solutions were mixed at a volume ratio of sample: matrix: cationization agent =1:10:1. The mixture solution (0.5 uL) was deposited on a MALDI sample plate, and the spots were dried in air at room temperature. The spectra were obtained in a negative reflector mode. UV–Raman spectra were recorded using a home-made single stage UV–Raman spectrograph with a spectral resolution of 2 cm−1. The single-frequency UV laser line at 244 nm was from an efficient external cavity frequency doubler (Wavetrain, Spectra-Physics) of the single-frequency laser at 488 nm laser (Genesis, CX 488, Coherent). The exciting source was with an output of 10 mW and the power of the laser at the sample was about 5.0 mW. Gel permeation chromatography (GPC) was performed on a PL-GPC220 chromatograph with N,N-dimethylformamide as the solvent. A MesoMR23-060V-I NMR analyzer (Suzhou Niumag Analytical Instrument Corporation, Suzhou, China) with a permanent magnet having resonance frequency 21 MHZ was used to measure the transverse spin-spin relaxation time (T2). The boron contents in poly(PEGMEA-co-AMA-PBA) and poly(PEGMEA-co-AMA-(HO-PBA)) were measured by using a PerkinElmer optima 8000 inductively coupled plasma optical emission spectrometer (ICP–OES). Theoretical calculations were calculated by the density functional theory (DFT) method with B3LYP density functional and 6-31G* basis set using the Gaussian 09 program.

Supplementary Figures 1–26

Supplementary Fig. 1 Crystal structure of CH3-HO-PBA dimer. a Crystal structure of CH3-HO-PBA dimer with thermal ellipsoids (CCDC 2280485). The dashed green line represents an intramolecular O–H…O hydrogen bond. b,c Packing mode of CH3-HO-PBA dimers viewed along the a axis (b) and b axis (c). d Packing interactions of CH3-HO-PBA dimers. The dashed blue and purple lines represent intramolecular O–H…O and C–H…O hydrogen bonds, respectively. e-g Packing mode of CH3-HO-PBA dimers in the left part (e), middle part (f), and right part (g) of (c).

Supplementary Fig. 2 Crystal structure of CF3-HO-PBA dimer. a Crystal structure of CF3-HO-PBA dimer with thermal ellipsoids (CCDC 2280486). The dashed green line represents an intramolecular O–H…O hydrogen bond. b Packing mode of CF3-HO-PBA dimers viewed along the a axis. c Packing interactions of CF3-HO-PBA dimers. The dashed orange line represents an intramolecular C–H…F hydrogen bond.

Supplementary Fig. 3 Exchange reaction between HO-PBA dimers and CF3-HO-PBA dimers. a MALDI-TOF mass spectrum of products from the mixture of HO-PBA dimers and CF3-HO-PBA dimers, acquired in a negative mode. b Illustration of the dynamic exchange between HO-PBA dimer and CF3-HO-PBA dimer.

Supplementary Fig. 4 Exchange reaction between CH3-HO-PBA dimers and CF3-HO-PBA dimers. a MALDI-TOF mass spectrum of products from the mixture of CH3-HO-PBA dimers and CF3-HO-PBA dimers, acquired in a negative mode. b Illustration of the dynamic exchange between CH3-HO-PBA dimer and CF3-HO-PBA dimer.

Supplementary Fig. 5 Crystal structure of HO-PBA dimer. a Packing mode of HO-PBA dimers viewed along the a axis. b-d Packing mode of HO-PBA dimers in the left part (b), the middle part (c) and right part (d) of (a).

Supplementary Fig. 6 SEM images of CH3-HO-PBA dimer and CF3-HO-PBA dimer. a,c SEM images displaying assembled morphology of CH3-HO-PBA dimer (a) and CF3-HO-PBA dimer (c), where the sample was prepared by dropping one droplet of CH3-HO-PBA or CF3-HO-PBA solution on a silicon wafer. b,d SEM images of the solid CH3-HO-PBA dimer (b) and CF3-HO-PBA dimer (d) sample.

Supplementary Fig. 7 XRD patterns of the solid CH3-HO-PBA dimer and CF3-HO-PBA dimer sample.

Supplementary Fig. 8 Luminescent behavior of CH3-HO-PBA dimer and CF3-HO-PBA dimer. a Fluorescence spectra of CH3-HO-PBA dimer (2×10-5 mol·L−1, λex=298 nm) and CF3-HO-PBA dimer (2×10-5 mol·L−1, λex=295 nm) in THF solution, as well as the solid CH3-HO-PBA dimer (λex=320 nm) and CF3-HO-PBA dimer (λex=318 nm) sample. b The absolute quantum yield (ΦF) of CH3-HO-PBA dimer and CF3-HO-PBA dimer in THF solution and in the solid state.

Supplementary Fig. 9 Fluorescent spectra and intensity changes (at 316 nm and 368 nm, inset) of HO-PBA dimer (2×10-5 mol·L−1) in methanol–water mixtures with different amounts of water (volume%), λex=288 nm.

Supplementary Fig. 10 a,b Calculated 1H (a) and 13C (b) NMR spectra of HO-PBA trimer in water by Gaussian at the B3LYP/6-31G* level.

Supplementary Fig. 11 Transformation of CH3-HO-PBA dimer into trimer upon exposure to water. a Fluorescence spectra and intensity changes (at 328 and 372 nm, inset) of CH3-HO-PBA dimer (2×10-5 mol·L−1) in THF–water mixtures with different amounts of water (volume%), λex=298 nm. b-e 1H (b, d) and 13C (c, e) NMR spectra of CH3-HO-PBA dimer in THF−d8 (b, c) and in D2O–THF−d8 (2:1, v/v) mixture (d, e) at room temperature, concentration: 8 mg·mL−1.The signals with heart and star mark correspond to H2O and THF, respectively. f ESI-Q-TOF mass spectrum of CH3-HO-PBA dimer in the methanol–water (5:1, v/v) solution, acquired in a negative mode. g UV–Raman spectra of the solid CH3-HO-PBA dimer sample (black) and CH3-HO-PBA trimer in an ACN–water (1:2, v/v) solution (red). h Relative fluorescence intensity at 372 nm of CH3-HO-PBA trimer (F/Fmax) as a function of pH value.

Supplementary Fig. 12 Fluorescence spectra and intensity changes (at 325 and 384 nm, inset) of CF3-HO-PBA dimer (2×10-5 mol·L−1) in THF–water mixtures with different amounts of water (volume%), λex=295 nm.

Supplementary Fig. 13 NMR spectra of CF3-HO-PBA dimer in CDCl3 and THF−d8. a,b 1H (a) and 1H -13C HSQC (b) NMR spectra of CF3-HO-PBA dimer in CDCl3 at room temperature. The signal with star mark (a) and that enclosed in blue circle (b) correspond to CHCl3. c,d 1H (c) and 13C (d) NMR spectra of CF3-HO-PBA dimer in THF−d8 at room temperature, concentrations: 8 mg·mL−1.

Discussion: In CDCl3, CF3-HO-PBA dimer exhibits six sets of signals in its 1H NMR spectrum (Supplementary Fig. 13a). The low solubility of CF3-HO-PBA dimer in CDCl3 makes it challenging to obtain a clear 13C NMR spectrum. As an alternative, a 1H-13C HSQC spectrum with higher sensitivity was measured, which displays six cross peaks (Supplementary Fig. 13b). The numbers of signals in both 1H NMR and 1H-13C HSQC spectrum of CF3-HO-PBA dimer in CDCl3 are consistent with the numbers of H atoms present in CF3-HO-PBA dimer. However, when CF3-HO-PBA dimer was dissolved in THF−d8, both 1H and 13C NMR spectrum display more sets of signals than the numbers of H and C atoms in CF3-HO-PBA dimer (Supplementary Fig. 13c,d). That is because a portion of CF3-HO-PBA dimer transforms into CF3-HO-PBA trimer due to the presence of a small amount of water in THF−d8 (Supplementary Fig. 11b), resulting in the coexisting of CF3-HO-PBA dimer and trimer. Upon addition of water into this THF−d8 solution, CF3-HO-PBA dimer completely transforms into CF3-HO-PBA trimer. Consequently, the numbers of 1H and 13C NMR signals in CF3-HO‑PBA dimer are reduced to three and five sets, respectively (Supplementary Fig. 14). Unlike CF3-HO-PBA dimer, both HO-PBA dimer (Fig. 3b,c in text) and CH3-HO-PBA dimer (Supplementary Fig. 11b,c) remain stable in THF−d8, despite the presence of a small amount of water in THF−d8 (Supplementary Fig. 11b). This result indicates that electron-withdrawing group of −CF3 improves the sensitivity of the dimeric structure to water.

Supplementary Fig. 14 a,b 1H (a) and 13C (b) NMR spectra of CF3-HO-PBA dimer in D2O–THF−d8 (2:1, v/v) mixture at room temperature, concentrations: 8 mg·mL−1.

Discussion: The two quartets enclosed in blue circle arise (Supplementary Fig. 14b) from the C-F coupling. The first quartet around 125.5 ppm with a large J-coupling corresponds to the carbon of the –CF3 group, and the second quartet around 134.5 ppm corresponds to the carbon bonded to the –CF3 group.

Supplementary Fig. 15 CF3-HO‑PBA trimer and its structure characterization. a ESI-Q-TOF mass spectrum of CF3-HO-PBA dimer in the methanol–water (5:1, v/v) solution, acquired in a negative mode. b UV–Raman spectra of the solid CF3-HO-PBA dimer sample (black) and CF3-HO-PBA trimer in an ACN–water (1:2, v/v) solution (red). c Relative fluorescence intensity at 384 nm of CF3-HO-PBA trimer (F/Fmax) as a function of pH value.

Supplementary Fig. 16 a,b Photos of the phenol, CF3-HO-PBA trimer and CH3-HO-PBA trimer solution after addition of Br2 (a) and FeCl3 (b).

Supplementary Fig. 17 1H NMR spectrum of product in THF−d8 from lyophilization of the THF–water (1:2, v/v) solution of HO-PBA trimer at room temperature, concentrations: 8 mg·mL−1.

Supplementary Fig. 18 Exchange reaction between HO-PBA trimers and CH3-HO-PBA trimers. a ESI-Q-TOF mass spectrum of products from mixing HO‑PBA dimers and CH3-HO‑PBA dimers together in the methanol–water (5:1, v/v) solution, acquired in a negative mode. b Illustration of the dynamic exchange between HO‑PBA trimer and CH3-HO‑PBA trimer.

Supplementary Fig. 19 Exchange reaction between CF3-HO-PBA trimers and CH3-HO-PBA trimers. a ESI-Q-TOF mass spectrum of products from mixing CF3-HO‑PBA dimers and CH3-HO‑PBA dimers together in the methanol–water (5:1, v/v) solution, acquired in a negative mode. b Illustration of the dynamic exchange between CF3-HO‑PBA trimer and CH3-HO‑PBA trimer.

Supplementary Fig. 20 Equilibration between HO‑PBA trimer–F− complexes and HO‑PBA trimer.

Supplementary Fig. 21 Ultra-strong binding capacity of CH3-HO‑PBA trimer toward F− in aqueous media. a 1H NMR spectra of CH3-HO‑PBA trimer (120 mmol·L−1) before and after the addition of one molar equivalent of NaF. The signals with star mark correspond to DMSO (2.5 ppm) and H2O, respectively. b,c Photos (b) and 19F NMR spectra (c) of NaF (120 mmol·L−1) before and after addition of one molar equivalent of CH3-HO‑PBA trimer. d 11B NMR spectra of CH3-HO‑PBA trimer (120 mmol·L−1) before and after addition of one molar equivalent NaF. All NMR measurements were carried out at room temperature using D2O–DMSO−d6 (1:6, v/v) mixtures as solvents.

Supplementary Fig. 22 Ultra-strong binding capacity of CF3-HO‑PBA trimer toward F− in aqueous media. a 1H NMR spectra of CF3-HO‑PBA trimer (120 mmol·L−1) before and after the addition of one molar equivalent of NaF. b,c Photos (b) and 19F NMR spectra (c) of NaF (120 mmol·L−1) before and after addition of one molar equivalent of CF3-HO‑PBA trimer. d 11B NMR spectra of CF3-HO‑PBA trimer (120 mmol·L−1) before and after addition of one molar equivalent NaF. All NMR measurements were carried out at room temperature using D2O–DMSO−d6 (1:6, v/v) mixtures as solvents.

Supplementary Fig. 23 Synthesis of poly(PEGMEA-co-GMA), poly(PEGMEA-co-AMA), poly(PEGMEA-co-AMA-PBA), poly(PEGMEA-co-AMA-(CH3O-PBA)) and poly(PEGMEA-co-AMA-(HO-PBA)).

Supplementary Fig. 24 GPC profiles of poly(PEGMEA-co-GMA).

Supplementary Fig. 25 Characterization of polymers. a ATR-FTIR spectra of poly(PEGMEA-co-GMA) (black), poly(PEGMEA-co-AMA) (red), poly(PEGMEA-co-AMA-PBA) (orange), poly(PEGMEA-co-AMA-(CH3O-PBA)) (cyan) and poly(PEGMEA-co-AMA-(HO-PBA)) (blue). b 1H NMR spectra of poly(PEGMEA-co-GMA) in CDCl3 at room temperature.

Discussion: In the ATR-FTIR spectrum of poly(PEGMEA-co-GMA) (Supplementary Fig. 25a, black line), the peak at 908 cm−1 corresponds to the epoxy groups of GMA, the peak at 1728 cm−1 is ascribed to the stretching vibrations of the ester groups in both GMA and PEGMEA2-4, and the peak at 1097 cm−1 originates from the stretching vibration of the ether bonds of PEGMEA. These peaks collectively indicate the presence of both GMA and PEGMEA fragments within the copolymer, indicating the successful synthesis of poly(PEGMEA-co-GMA). In the 1H NMR spectra of poly(PEGMEA-co-GMA) (Supplementary Fig. 25b), the signals at 2.62 (v) and 2.82 (v) ppm attribute to –CH2–of the epoxy ring in GMA unit. The signals at 3.21 (u) and 3.37 (w) ppm attribute to –CH– of the epoxy ring in GMA unit and –CH3 in PEGMEA unit, respectively2,5. By calculating the ratio of the integral of the signal at 3.21 (u) to that at 3.37 (w) ppm, the molar ratio of GMA to PEGMEA was determined to be 1:0.28 (poly(PEGMEA0.28m-co-GMAm)).

Upon reacting with ethylenediamine, the peak at 908 cm−1 associated with epoxy vibration disappears, and three new bands originating from N-H vibrations appear at 3360, 3300 and 1565 cm−1 in the ATR-FTIR spectrum of poly(PEGMEA-co-AMA) (Supplementary Fig. 25a, red line). These changes suggest the complete reaction of the epoxy group with ethylenediamine in the synthesis of poly(PEGMEA-co-AMA). Thus, the molar ratio of AMA to PEGMEA in poly(PEGMEA-co-AMA) is also 1:0.28 (poly(PEGMEA0.28m-co-AMAm)).

In the ATR-FTIR spectrum of poly(PEGMEA-co-AMA-PBA) (Supplementary Fig. 25a, orange line), a peak corresponding to the aromatic C=C stretching vibration is observed at 1609 cm−1, indicating the successful functionalization of PBA into poly(PEGMEA-co-AMA). The mass percentage of boron in poly(PEGMEA-co-AMA-PBA) was determined to be 1.49% using ICP–OES. Based on the boron content, the molar ratio of AMA to PBA in poly(PEGMEA-co-AMA-PBA) was calculated to be ca. 1:0.57 (poly(PEGMEA0.28m-co-AMAm-PBA0.57m).

In the ATR-FTIR spectrum of poly(PEGMEA-co-AMA-(CH3O-PBA)) (Supplementary Fig. 25a, cyan line), the appearance of peaks at 1608 cm−1, corresponding to the aromatic C=C stretching vibration, and at 1037 cm−1, corresponding to the stretching vibration of the Ar-O-C groups, provides strong evidences for the successful functionalization of CH3O-PBA into poly(PEGMEA-co-AMA). After reacting poly(PEGMEA-co-AMA-(CH3O-PBA)) with BBr3, the aromatic C=C stretching vibration shifts to 1612 cm−1, as shown in the ATR-FTIR spectrum of poly(PEGMEA-co-AMA-(HO-PBA) (Supplementary Fig. 25a, blue line). Moreover, the stretching vibration of the Ar-O-C groups at 1037 cm−1 disappears, indicating the complete conversion of poly(PEGMEA-co-AMA-(CH3O-PBA)) into poly(PEGMEA-co-AMA-(HO-PBA).

The mass percentages of boron in poly(PEGMEA-co-AMA-(HO-PBA)) was determined to be 1.06% using ICP–OES. Based on the boron content, the molar ratio of AMA to HO-PBA in poly(PEGMEA-co-AMA-(HO-PBA)) was calculated to be ca. 1:0.39 (poly(PEGMEA0.28m-co-AMAm-(HO-PBA)0.39m). The molar ratio of CH3O-PBA to AMA in poly(PEGMEA-co-AMA-(CH3O-PBA)) is also 1:0.39 (poly(PEGMEA0.28m-co-AMAm-(CH3O-PBA)0.39m)), since (poly(PEGMEA0.28m-co-AMAm-(HO-PBA)0.39m was synthesized by adopting BBr3 to convert methoxy groups of CH3O-PBAs in poly(PEGMEA-co-AMA-(CH3O-PBA)) into hydroxyl groups.

Supplementary Fig. 26 The proportion of peak areas of the three peaks, T21, T22 and T23, in T2 distribution curves of poly(PEGMEA-co-AMA-PBA) (1), poly(PEGMEA-co-AMA-(CH3O-PBA)) (2) and poly(PEGMEA-co-AMA-(HO-PBA)) (3) in water at room temperature.

Supplementary Tables 1–9

Supplementary Table 1 Crystal data and structure refinements for HO-PBA

| Empirical formula | C12H10B2O4 |
| --- | --- |
| Formula weight | 239.82 |
| Temperature (K) | 120 |
| Crystal size (mm3) | 0.16 x 0.12 x 0.12 |
| Crystal system | monoclinic |
| Space group | C 12/c 1 |
| a (Å) | 25.308(5) |
| b (Å) | 5.0812(10) |
| c (Å) | 17.183(4) |
|  | 90 |
|  | 91.498(9) |
|  | 90 |
| V (Å3 ) | 2208.9(8) |
| Z | 8 |
| Density ( g/cm3) | 1.442 |
| F (000) | 992.0 |
| Theta range for data collection | 2.83 to 27.18 |
| Index ranges | −32<=h<=32, −6<=k<=6, −22<=l<=22 |
| Reflections collected | 18588 |
| Independent reflections | 2557 [R(int)= 0.0681] |
| Final R indices [I>2sigma(I)] | R1= 0.0476, wR2=0.1056 |
| R indices (all data) | R1= 0.0764, wR2= 0.1198 |
| Goodness−of−fit on F2 | 1.034 |
| Highest difference peak and deepest hole (e Å−3) | 0.254 and -0.224 |

Supplementary Table 2 Bond lengths (Å) and angles for HO-PBA

| O2−B2 | 1.379(2) | C11−C12−O4 | 116.04(15) |
| --- | --- | --- | --- |
| O2−B1 | 1.407(2) | C11−C12−C7 | 122.32(16) |
| O3−C1 | 1.389(2) | C1−C2−C3 | 117.37(16) |
| O3−B2 | 1.370(2) | C1−C2−B1 | 117.76(15) |
| O1−H1 | 0.8400 | C3−C2−B1 | 124.87(16) |
| O1−B1 | 1.338(2) | C12−C7−B2 | 122.88(15) |
| O4−H4 | 0.8400 | C8−C7−C12 | 116.39(16) |
| O4−C12 | 1.387(2) | C8−C7−B2 | 120.72(16) |
| C1−C2 | 1.394(2) | C12−C11−H11 | 120.3 |
| C1−C6 | 1.388(2) | C10−C11−C12 | 119.43(17) |
| C12−C7 | 1.402(2) | C10−C11−H11 | 120.3 |
| C12−C11 | 1.382(2) | C2−C3−H3 | 119.5 |
| C2−C3 | 1.406(2) | C4−C3−C2 | 120.94(16) |
| C2−B1 | 1.545(3) | C4−C3−H3 | 119.5 |
| C7−C8 | 1.402(2) | C7−C8−H8 | 119 |
| C7−B2 | 1.552(3) | C9−C8−C7 | 122.02(17) |
| C11−H11 | 0.9500 | C9−C8−H8 | 119 |
| C11−C10 | 1.379(3) | C1−C6−H6 | 120.8 |
| C3−H3 | 0.9500 | C5−C6−C1 | 118.38(16) |
| C3−C4 | 1.387(2) | C5−C6−H6 | 120.8 |
| C8−H8 | 0.9500 | C3−C4−H4A | 120.2 |
| C8−C9 | 1.388(3) | C3−C4−C5 | 119.55(16) |
| C6−H6 | 0.9500 | C5−C4−H4A | 120.2 |
| C6−C5 | 1.381(2) | C6−C5−C4 | 121.22(16) |
| C4−H4A | 0.9500 | C6−C5−H5 | 119.4 |
| C4−C5 | 1.388(2) | C4−C5−H5 | 119.4 |
| C5−H5 | 0.9500 | C11−C10−H10 | 119.7 |
| C10−H10 | 0.95 | C11−C10−C9 | 120.53(17) |
| C10−C9 | 1.385(3) | C9−C10−H10 | 119.7 |
| C9−H9 | 0.95 | C8−C9−H9 | 120.4 |
| B2−O2−B1 | 121.16(14) | C10−C9−C8 | 119.29(17) |
| B2−O3−C1 | 121.78(14) | C10−C9−H9 | 120.4 |
| B1−O1−H1 | 109.5 | O2−B2−C7 | 119.49(15) |
| C12−O4−H4 | 109.5 | O3−B2−O2 | 121.77(16) |
| O3−C1−C2 | 120.73(15) | O3−B2−C7 | 118.74(16) |
| C6−C1−O3 | 116.73(15) | O2−B1−C2 | 116.73(15) |
| C6−C1−C2 | 122.54(16) | O1−B1−O2 | 120.43(16) |
| O4−C12−C7 | 121.63(15) | O1−B1−C2 | 122.83(16) |

Supplementary Table 3 Hydrogen bond data for HO-PBA

| D−H...A | d(D−H) | d(H...A) | d(D...A) | <(DHA) |
| --- | --- | --- | --- | --- |
| O4−H4...O2 | 0.8401 (14) | 1.9355 (11) | 2.6926 (19) | 149.371 (105) |
| O1-H1...O4i | 0.8401 (14) | 1.9755 (15) | 2.7982 (21) | 166.092 (105) |
| C9−H9...O3ii | 0.9500 (18) | 3.0058 (12) | 3.6799 (22) | 129.128 (110) |

Symmetry codes: (i) 0.5−x, 0.5+y, 0.5−z; (ii) x, 2-y, -0.5+z.

Supplementary Table 4 Crystal data and structure refinements for CH3-HO-PBA

| Empirical formula | C14H14B2O4 |
| --- | --- |
| Formula weight | 267.87 |
| Temperature (K) | 120 |
| Crystal size (mm3) | 0.15 x 0.12 x 0.12 |
| Crystal system | monoclinic |
| Space group | P 1 21/n 1 |
| a (Å) | 12.8607(14) |
| b (Å) | 5.0210(5) |
| c (Å) | 19.993(2) |
|  | 90 |
|  | 91.001(5) |
|  | 90 |
| V (Å3 ) | 1290.8(2) |
| Z | 4 |
| Density ( g/cm3) | 1.378 |
| F (000) | 560.0 |
| Theta range for data collection | 3.17 to 27.17 |
| Index ranges | −16<=h<=16, −6<=k<=6, −25<=l<=25 |
| Reflections collected | 15819 |
| Independent reflections | 2964 [R(int)= 0.0943] |
| Final R indices [I>2sigma(I)] | R1= 0.0513, wR2= 0.1112 |
| R indices (all data) | R1= 0.1077, wR2= 0.1322 |
| Goodness−of−fit on F2 | 1.016 |
| Highest difference peak and deepest hole (e Å−3) | 0.288 and -0.264 |

Supplementary Table 5 Bond lengths (Å) and angles for CH3-HO-PBA

| O2−B1 | 1.379(2) | C11−C10−C9 | 122.45(18) |
| --- | --- | --- | --- |
| O2−B2 | 1.397(3) | C11−C10−H10 | 118.8 |
| O1−C8 | 1.387(2) | C8−C14−H14 | 120.7 |
| O1−B1 | 1.378(3) | C8−C14−C13 | 118.59(18) |
| O3−H3 | 0.8400 | C13−C14−H14 | 120.7 |
| O3−C2 | 1.382(2) | C10−C11−C13 | 118.06(18) |
| O4−H4 | 0.8400 | C10−C11−C12 | 121.44(18) |
| O4−B2 | 1.342(2) | C13−C11−C12 | 120.49(18) |
| C9−C8 | 1.391(2) | O3−C2−C1 | 121.77(17) |
| C9−C10 | 1.405(3) | O3−C2−C3 | 116.75(18) |
| C9−B2 | 1.549(3) | C3−C2−C1 | 121.47(18) |
| C8−C14 | 1.384(3) | C5−C6−H6 | 118.4 |
| C10−H10 | 0.9500 | C5−C6−C1 | 123.29(19) |
| C10−C11 | 1.385(3) | C1−C6−H6 | 118.4 |
| C14−H14 | 0.9500 | C6−C5−C4 | 117.64(18) |
| C14−C13 | 1.385(3) | C6−C5−C7 | 120.41(18) |
| C11−C13 | 1.392(3) | C4−C5−C7 | 121.94(18) |
| C11−C12 | 1.507(3) | C2−C1−C6 | 116.75(17) |
| C2−C1 | 1.397(3) | C2−C1−B1 | 123.14(17) |
| C2−C3 | 1.384(3) | C6−C1−B1 | 120.11(18) |
| C6−H6 | 0.9500 | C14−C13−C11 | 121.58(18) |
| C6−C5 | 1.387(3) | C14−C13−H13 | 119.2 |
| C6−C1 | 1.399(3) | C11−C13−H13 | 119.2 |
| C5−C4 | 1.389(3) | C2−C3−H3A | 120.1 |
| C5−C7 | 1.509(3) | C2−C3−C4 | 119.71(19) |
| C1−B1 | 1.545(3) | C4−C3−H3A | 120.1 |
| C13−H13 | 0.9500 | C5−C4−H4A | 119.4 |
| C3−H3A | 0.9500 | C3−C4−C5 | 121.14(18) |
| C3−C4 | 1.386(3) | C3−C4−H4A | 119.4 |
| C4−H4A | 0.9500 | C11−C12−H12A | 109.5 |
| C12−H12A | 0.9800 | C11−C12−H12B | 109.5 |
| C12−H12B | 0.9800 | C11−C12−H12C | 109.5 |
| C12−H12C | 0.9800 | H12A−C12−H12B | 109.5 |
| C7−H7A | 0.9800 | H12A−C12−H12C | 109.5 |
| C7−H7B | 0.9800 | H12B−C12−H12C | 109.5 |
| C7−H7C | 0.9800 | C5−C7−H7A | 109.5 |
| B1−O2−B2 | 121.88(16) | C5−C7−H7B | 109.5 |
| B1−O1−C8 | 122.00(15) | C5−C7−H7C | 109.5 |
| C2−O3−H3 | 109.5 | H7A−C7−H7B | 109.5 |
| B2−O4−H4 | 109.5 | H7A−C7−H7C | 109.5 |
| C8−C9−C10 | 116.81(18) | H7B−C7−H7C | 109.5 |
| C8−C9−B2 | 118.01(17) | O2−B1−C1 | 120.84(18) |
| C10−C9−B2 | 125.14(17) | O1−B1−O2 | 121.07(18) |
| O1−C8−C9 | 120.54(17) | O1−B1−C1 | 118.09(17) |
| C14−C8−O1 | 116.96(16) | O2−B2−C9 | 116.48(17) |
| C14−C8−C9 | 122.50(18) | O4−B2−O2 | 120.83(18) |
| C9−C10−H10 | 118.8 | O4−B2−C9 | 122.69(18) |

Supplementary Table 6 Hydrogen bond data for CH3-HO-PBA

| D−H...A | d(D−H) | d(H...A) | d(D...A) | <(DHA) |
| --- | --- | --- | --- | --- |
| O3−H3...O2 | 0.8401 (14) | 1.9743 (14) | 2.7307 (20) | 149.334 (103) |
| O4-H4...O3i | 0.8399 (14) | 1.9635 (14) | 2.7942 (20) | 169.816 (103) |
| C14-H14...O1ii | 0.9501 (18) | 2.8202 (12) | 3.5042 (22) | 129.697 (112) |

Symmetry codes: (i) x, 1+y, z; (ii) 1−x, 1-y, 1−z.

Supplementary Table 7 Crystal data and structure refinements for CF3-HO-PBA

| Empirical formula | C14H8B2F6O4 |
| --- | --- |
| Formula weight | 375.82 |
| Temperature (K) | 120 |
| Crystal size (mm3) | 0.15 x 0.1 x 0.1 |
| Crystal system | monoclinic |
| Space group | P 1 21/c 1 |
| a (Å) | 15.995(3) |
| b (Å) | 4.9175(9) |
| c (Å) | 18.567(3) |
|  | 90 |
|  | 92.217(7) |
|  | 90 |
| V (Å3 ) | 1459.3(4) |
| Z | 4 |
| Density ( g/cm3) | 1.711 |
| F (000) | 752 |
| Theta range for data collection | 2.50 to 27.42 |
| Index ranges | −20<=h<=14, −5<=k<=6, −24<=l<=24 |
| Reflections collected | 11314 |
| Independent reflections | 3297 [R(int)= 0.0399] |
| Final R indices [I>2sigma(I)] | R1= 0.0615, wR2= 0.1545 |
| R indices (all data) | R1= 0.0722, wR2= 0.1610 |
| Goodness−of−fit on F2 | 1.102 |
| Highest difference peak and deepest hole (e Å−3) | 0.338 and -0.359 |

Supplementary Table 8 Bond lengths (Å) and angles for CF3-HO-PBA

| F4−C14 | 1.338(3) | C12−C11−C14 | 118.9(2) |
| --- | --- | --- | --- |
| F5−C14 | 1.338(3) | C10−C11−C14 | 120.0(2) |
| F6−C14 | 1.344(3) | C6−C1−C2 | 118.2(2) |
| O2−B1 | 1.401(3) | C6−C1−B1 | 117.6(2) |
| O2−B2 | 1.376(3) | C2−C1−B1 | 124.2(2) |
| O1−H1 | 0.8400 | O3−C6−C1 | 121.1(2) |
| O1−B1 | 1.336(4) | O3−C6−C5 | 116.9(2) |
| O4−H4 | 0.8400 | C5−C6−C1 | 122.0(2) |
| O4−C13 | 1.369(3) | C10−C9−H9 | 118.8 |
| F1−C7 | 1.331(3) | C10−C9−C8 | 122.4(2) |
| O3−C6 | 1.384(3) | C8−C9−H9 | 118.8 |
| O3−B2 | 1.371(3) | C11−C10−H10 | 120.5 |
| F3−C7 | 1.336(4) | C9−C10−C11 | 119.0(2) |
| F2−C7 | 1.327(4) | C9−C10−H10 | 120.5 |
| C12−H12 | 0.9500 | C1−C2−H2 | 119.4 |
| C12−C13 | 1.393(4) | C3−C2−C1 | 121.1(3) |
| C12−C11 | 1.389(4) | C3−C2−H2 | 119.4 |
| C13−C8 | 1.415(3) | C2−C3−H3 | 120.5 |
| C11−C10 | 1.393(4) | C2−C3−C4 | 118.9(3) |
| C11−C14 | 1.502(4) | C4−C3−H3 | 120.5 |
| C1−C6 | 1.397(4) | C6−C5−H5 | 121 |
| C1−C2 | 1.401(4) | C6−C5−C4 | 118.0(3) |
| C1−B1 | 1.561(4) | C4−C5−H5 | 121 |
| C6−C5 | 1.390(4) | C3−C4−C7 | 120.2(3) |
| C9−H9 | 0.9500 | C5−C4−C3 | 121.8(2) |
| C9−C10 | 1.381(4) | C5−C4−C7 | 118.1(3) |
| C9−C8 | 1.401(4) | C13−C8−B2 | 121.9(2) |
| C10−H10 | 0.9500 | C9−C8−C13 | 116.9(2) |
| C2−H2 | 0.9500 | C9−C8−B2 | 121.2(2) |
| C2−C3 | 1.386(4) | F4−C14−F6 | 106.5(2) |
| C3−H3 | 0.9500 | F4−C14−C11 | 112.5(2) |
| C3−C4 | 1.392(4) | F5−C14−F4 | 106.8(2) |
| C5−H5 | 0.9500 | F5−C14−F6 | 106.8(2) |
| C5−C4 | 1.391(4) | F5−C14−C11 | 112.5(2) |
| C4−C7 | 1.508(4) | F6−C14−C11 | 111.4(2) |
| C8−B2 | 1.558(4) | F1−C7−F3 | 105.9(3) |
| B2−O2−B1 | 122.0(2) | F1−C7−C4 | 112.9(2) |
| B1−O1−H1 | 109.5 | F3−C7−C4 | 112.0(3) |
| C13−O4−H4 | 109.5 | F2−C7−F1 | 106.5(3) |
| B2−O3−C6 | 121.5(2) | F2−C7−F3 | 107.2(3) |
| C13−C12−H12 | 120.5 | F2−C7−C4 | 111.8(3) |
| C11−C12−H12 | 120.5 | O2−B1−C1 | 115.8(2) |
| C11−C12−C13 | 119.1(2) | O1−B1−O2 | 121.4(2) |
| O4−C13−C12 | 115.9(2) | O1−B1−C1 | 122.7(3) |
| O4−C13−C8 | 122.6(2) | O2−B2−C8 | 119.2(2) |
| C12−C13−C8 | 121.5(2) | O3−B2−O2 | 121.9(2) |
| C12−C11−C10 | 121.0(2) | O3−B2−C8 | 118.9(2) |

Supplementary Table 9 Hydrogen bond data for CF3-HO-PBA

| D−H...A | d(D−H) | d(H...A) | d(D...A) | <(DHA) |
| --- | --- | --- | --- | --- |
| O4−H4...O2 | 0.8398 (19) | 1.9338 (18) | 2.6896 (19) | 149.177 (139) |
| C9-H9...F3i | 0.9500 (26) | 2.6448 (22) | 3.3071 (34) | 127.221 (162) |

Symmetry codes: (i) 1−x, -0.5+y, 0.5−z.

References

- Jiang, W., Jiao, C., Meng, Y., Zhao, L., Liu, Q. & Liu, T. Switching single chain magnet behavior via photoinduced bidirectional metal-to-metal charge transfer. Chem. Sci. 9, 617-622 (2018).

- Tzoumani, I., Soto Beobide, A., Iatridi, Z., Voyiatzis, G. A., Bokias, G. & Kallitsis, J. K. Glycidyl methacrylate-based copolymers as healing agents of waterborne polyurethanes. Int. J. Mol. Sci. 23, 8118 (2022).

- Zhang, G., Zhang, Q., Cheng, T., Zhan, X. & Chen, F. Polyols-infused slippery surfaces based on magnetic Fe3O4-functionalized polymer hybrids for enhanced multifunctional anti-icing and deicing properties. Langmuir 34, 4052-4058 (2018).

- Yang, W. J., Pranantyo, D., Neoh, K.-G., Kang, E.-T., Teo, S. L.-M. & Rittschof, D. Layer-by-layer click deposition of functional polymer coatings for combating marine biofouling. Biomacromolecules 13, 2769-2780 (2012).

- Xia, J., Lu, D., Han, Y., Wang, J., Hong, Y., Zhao, P., Fang, Q. & Lin, Q. Facile multifunctional IOL surface modification via poly(PEGMA-co-GMA) grafting for posterior capsular opacification inhibition. RSC Adv. 11, 9840-9848 (2021).