1 Morphology of RGO-CNT/TMC (Online Resource 1)

In order to investigate morphology of RGO-CNT/TMC, the SEM images of raw TMC and RGO-CNT/TMC were showed in Fig. 2. The morphology of raw TMC mainly presents a fibrous porous structure, formed by individual fibers (about 50 mm in diameter) intertwined with each other, forming a three-dimensional porous structure (Fig. 2A). And the structure remains the same after decorated with RGO-CNT complexes (Fig. 2D).

Further study about the fibers of raw TMC and RGO-CNT/TMC shows that the fabric surface of raw TMC was relative smooth (Fig. 2B). However, modification of the RGO-CNT complexes makes the fabric surface be cover by rough nanomaterials (Fig. 2E).

In addition, SEM images at larger magnification were also investigated to analyze the details of the nano-structure of the materials. The surface of the raw fiber keeps smooth at 10,000x magnification (Fig. 2C), while filamentous and flaky structures were observed on the surface of the RGO-CNT/TMC (Fig. 2F), caused by the loading of the RGO-CNT complexes.

2 Chemical structure of RGO-CNT/TMC (Online Resource 2)

Firstly, the IR spectra of raw TMC and RGO-CNT/TMC were investigated. For raw TMC (curve a in Fig. 3A), the stretching vibration peak of the O-H bond (3299 cm-1) was observed, as well as the stretching vibration peak of the C-H bond on the alkyl group at 2932 cm-1 and the stretching vibration peak of C-H bond on the aldehyde group at 2858 cm-1. The stretching vibration peaks of C=C bond and C=O bond appeared at 1636 cm-1 and 1537 cm-1, respectively. In addition, the stretching vibration of the C-O-C bond (1259 cm-1) also presented. According to the analysis of the peaks, there were hydroxyl groups, alkyl groups, aldehyde groups, ether groups, and C=C bond on the surface of raw TMC. The polar groups, such as hydroxyl groups and ether groups, brought hydrophilicity to the surface of raw TMC. Additionally, it was worth to notice that unsaturated bonds did not exist in the original cellulose. The appearance of C=C and C=O bonds on raw TMC was caused by adding reducing dye during the manufacturing processes of the textile matrix. The possible chemical structure of raw TMC was showed in Fig. 3G.

The surface infrared spectrum of RGO-CNT/TMC was showed in curve b of Fig. 3A. The O-H bond stretching vibration peaks at 3295 cm-1 was mainly from the hydroxyl groups on RGO-CNT complexes. Additionally, the peak of hydroxyl groups moved to lower wavenumber after the raw TMC was decorated with the RGO-CNT complexes, implying the effect of hydrogen bonds between them. The C-H bonds stretching vibration peaks on alkyl groups (2935 cm-1) and on aldehyde groups (2860 cm-1) decreased after modification of RGO-CNT complexes, owe to the RGO-CNT complexes covered the original surface of raw TMC. Based on the same reason, the stretching vibration peak of ether groups at 1259 cm-1 also declined. For RGO-CNT/TMC, the C=C bonds stretching vibration peak appeared at 1634 cm-1, which shifted to lower wavenumber compared with the same peak of raw TMC, due to the formation of benzene-like structure of RGO and CNT. The stretching vibration peaks of the C=O bonds (1540 cm-1) came from the carboxyl groups on RGO-CNT complexes. In summary, the main chemical groups on RGO-CNT/TMC were hydrophilic hydroxyl groups and carboxyl groups, which were introduced by incomplete reducing of RGO and CNT. And the main force between RGO-CNT complexes and TMC substrate may be hydrogen bonds.

To further understand the functional groups of the RGO-CNT/TMC, XPS spectra of C1s and O1s were measured. After comparing the C1s spectra of raw TMC (Fig. 3B) and RGO-CNT/TMC (Fig. 3C), it was found that there were four peaks in the spectrum of raw TMC. They were peaks of C-C bonds of 284.8 eV, C-H bonds of 284.5 eV, C-O bonds of 285.9 eV, and C=O bonds of 288.0 eV. The C-C bonds, C-O bonds, and C-H bonds were typical structure in original cellulose. The C=O bonds were caused by adding reducing dye during the manufacturing processes of the textile matrix. Therefore, the results of XPS C1s spectrum of raw TMC were coincident with the results of IR. The possible chemical structure of TMC was showed in Fig. 3G. After adding RGO-CNT complexes to TMC, the peak area of C-H bonds (284.5 eV) on alkyl groups decreased as showed in Fig. 3C, because the TMC substrate was covered by the RGO-CNT complexes, which were filled with unsaturated benzene-like structures. The peaks of C-O bonds (285.8 eV) and O=C-O bonds (288.1 eV) in Fig. 3C represented the hydroxyl groups and carboxyl groups on RGO-CNT complexes, which was consistent with the results of infrared spectroscopy.

Then, the O1s spectrum of raw TMC (Fig 3D) and RGO-CNT/TMC (Fig 3E) were compared. For raw TMC, there were O-H bonds peak at 531.5 eV, O-C bonds peak at 532.3 eV, and O=C bonds peak at 533.2 eV. The O-H bonds and O-C bonds came from the structure of original cellulose. The O=C bonds were formed in the reductive production process of the textile matrix. After decorated RGO-CNT complexes, the O-H bonds peak (531.6 eV), O-C bonds peak (532.5 eV), and O=C-O bonds peak (533.5 eV) arisen, due to the hydroxyl group and carboxyl groups of the RGO-CNT complexes.

The Raman spectra of raw TMC and RGO-CNT/TMC were characterized to deepen the understanding of the chemical structure (Fig. 3F). There were many peaks appearance in the spectrum of raw TMC (Fig. 3F curve a), such as vibrational peak of O-H bonds at 2900 cm-1, bending vibration peak of -CH2- at 1060-1610 cm-1, and twisted vibration peak of C-O-C bonds at 640 cm-1. All of them were typical chemical structure in natural cellulose. Nevertheless, the peaks of cellulose in spectrum of raw TMC almost disappeared in spectrum of RGO-CNT/TMC (Fig. 3F curve b), due to the RGO-CNT complexes had been covered on TMC substrate. Moreover, three new peaks appeared in spectrum of RGO-CNT/TMC. They were named D, G and 2D peaks. The D peak appeared at 1340 cm-1, representing defects in the graphite-like crystals of RGO and CNT. The defects resulted from the sp3 hybrid carbon atoms in hydroxyl groups and carboxyl groups on the surface of RGO and CNT. The G peak at 1580 cm-1 in RGO-CNT/TMC related to the in-plane vibration mode of sp2 hybrid carbon atoms in RGO-CNT complexes. The G peak was relative stronger than D peak, suggesting that a considerable perfect lattice composed by delocalized p bonds was observed in RGO-CNT complexes. This lattice structure was the foundation of the high conductivity of the two carbon nanomaterials and RGO-CNT/TMC. The 2D peak was at about 2690 cm-1, which was a frequency-doubled peak of D peak, representing the vibrational modes of double photonic lattices. The appearance of D, G and 2D peaks also implied that the modification of TMC substrate by RGO-CNT complexes was successful. In brief, the results of Raman spectra about raw TMC and RGO-CNT/TMC were coincident with the results of IR and XPS.

Summarily, the chemical structure of raw TMC was similar with cellulose except some unsaturated bonds such as C=C bonds and C=O bonds. There were hydroxyl groups and carboxyl groups on the surface of the RGO-CNT complexes. The lattice structure composed by delocalized p bonds in the complexes laid a good foundation to the high conductivity of RGO-CNT/TMC. Both of raw TMC and RGO-CNT complexes had hydrophilic surface and the hydrogen bonds were the main force between them.