Charge transfer complex mediated conversion of CO2 to CO fuel

Xuebo Cao*, Kai Wang, Mingming Chu, Yuanyuan Wu, Xingtian Zhang, Zhen Yan

College of Biological, Chemical Sciences and Engineering, Jiaxing University, Jiaxing, Zhejiang 314001, China

*Corresponding author. Email: xbcao@zjxu.edu.cn

Contents:

Supplementary Movie 1 | Movie shows the violent combustion of the CO product.

Supplementary Table 1 | A summary of various advanced electrochemical systems for the conversion of CO2 to CO.

Supplementary Table 2 | A summary of various advanced photochemical systems for the conversion of CO2 to CO.

Supplementary Table 3 | Structural formula for molecular ion or the fragments identified in Fig. S4.

Supplementary Table 4 | Structural formular for the compounds identified in Fig. S8.

Supplementary Table 5 | Selected standard potentials of CO2R.

Supplementary Fig. 1 | Time-dependent UV-vis absorption spectra of the [CuI∙∙∙NMI•‒] solution.

Supplementary Fig. 2 | Air-assisted oxidization experiment for [CuI∙∙∙NMI•‒] solution.

Supplementary Fig. 3 | Stability studies of the [CuI∙∙∙NMI•‒] solution.

Supplementary Fig. 4 | The time-off-flight mass spectrum of the [CuI∙∙∙NMI•‒] solution.

Supplementary Fig. 5 | Schematic illustration of time‒dependent in-situ ATR-IR studies.

Supplementary Fig. 6 | ATR-IR results of the [CuI∙∙∙NMI•‒] system.

Supplementary Fig. 7 | CO2 absorption capacities for the [CuI∙∙∙NMI•‒] system.

Supplementary Fig. 8 | The time-off-flight mass spectrum of the system with CO2.

Supplementary Fig. 9 | EPR spectrum for the [CuI∙∙∙NMI•‒] solution saturated by CO2.

Supplementary Fig. 10 | [CuI∙∙∙NMI•‒] as the mediator for electrocatalytic CO2R.

Supplementary Fig. 11 | Representative GC signals of CO2 feed and the converted CO.

Supplementary Fig. 12 | Analysis of the gaseous product using GC equipped with TCD.

Supplementary Fig. 13 | In-situ ATR−IR absorption spectroscopy study of the CO2R.

Supplementary Fig. 14 | Isotope tracer study using 13CO2 as the feedstock.

Supplementary Fig. 15 | Representative photograph of the reaction system.

Supplementary Fig. 16 | 1H-NMR spectroscopy studies of the reduction system.

Supplementary Fig. 17 | 13C–NMR spectroscopy studies of the reduction system.

Supplementary Fig. 18 | SEM image of the white colloid.

Supplementary Fig. 19 | XPS characterization of the white colloid.

Supplementary Fig. 20 | PXRD characterizations of the white colloid.

Supplementary Fig. 21 | Pressure of the CO2 reactant and the CO product.

Supplementary Fig. 22 | PXRD characterization of the red solid.

Supplementary Fig. 23 | Electrochemical regeneration of the reaction system.

Supplementary Fig. 24 | 1H-NMR and 13C-NMR spectroscopy studies of the regenerated NMI.

Supplementary Fig. 25 | Flow reduction of CO2 to CO in the bubbling reactor.

Supplementary Table 1 | A summary of various advanced electrochemical systems for the conversion of CO2 to CO.

| Catalytic Electrode (area)a |  | Electrolyte | Current (mA·cm-2) | Cathodic Potential or Cell Voltage (V) | CO Faradaic efficiency | CO2 flow rate (SCCM)a | Conversion of CO2 (R)b | CO evolution rate (vm, mmol min-1)b | Refs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| CoPc + phenol （4 cm2） | KOH (1 mol L-1) | 200 | 2.52 (Ecell) | 88% | 100 | 5.19 % | 0.219 | [1] |
| Ni-NCB （100 cm2） | KHCO3 (1 mol L-1) | 73.8 | 2.46 (Ecell) | 102.4% | 500 | 11.33 % | 2.33 | [2] |
| Fe3+–N–C （1 cm2） | KHCO3 (0.5 mol L-1) | 94 (jco) | -0.45 | 90% | 40 | 1.79% | 0.0292 | [3] |
| NiPc-OMe-MDE (0.95cm2) | KHCO3 (1 mol L-1) | 400 | -0.69 | 99.1% | 20 | 14.3% | 0.117 | [4] |
| Znδ+-NC (2.25 cm2) | KOH (1 mol L-1) | 1000 | 7 | 98% | 55 | 30.5% | 0.686 | [5] |
| Ni2/NC （1 cm2） | KHCO3 (1 mol L-1) | 150 | 1.25 | 94.3% | 20 | 5.39% | 0.044 | [6] |
| Ni-N4/C-NH2 （1 cm2） | KHCO3 (1 mol L-1) | 447.6 | -1 | 85% | 30 | 9.66% | 0.118 | [7] |
| Au/PE (10 cm2) | KHCO3 (0.5 mol L-1) | 25.5 (jco) | -0.6 | 92% | 50 | 3.89% | 0.0793 | [8] |
| Cu-APC （0.5 cm2） | NaHCO3 (0.2 mol L-1) | 8.6 (jco) | -0.78 | 92% | 20 | 0.164% | 1.34×10-3 | [9] |
| NPCA900 （1 cm2） | [Bmim]PF6/MeCN | 143.6 | -2.4 (vs. Ag/Ag+) | 99.1% | 20 | 5.42 % | 0.0442 | [10] |
| Mn-C3N4/CNT （1 cm2） | [Bmim]PF4 | 29.7 (jco) | -0.73 | 90.9% | NA | 9.23 | 9.23×10-3 | [11] |
| CoTAP-cov （1 cm2） | KHCO3 (0.5 mol L-1) | 25.4 | -1.35 | 100% | 5 | 3.87% | 7.9×10-3 | [12] |
| Zn-N3-C （1 cm2） | KHCO3 (0.1 mol L-1) | 6.64 (jco) | -0.65 | 95.6% | 10 | 0.506% | 2.06×10-3 | [13] |
| NiFe-DASC （1 cm2） | KHCO3 (0.5 mol L-1) | 50.4 | -0.8 | 94.5% | 10 | 3.63% | 0.0148 | [14] |
| DNG-SAFe （1cm2​） | KHCO3 (1 mol L-1) | 46.2(jco) | -0.79 | 89% | 30 | 1.17% | 0.0144 | [15] |
| AgNPS/GDE （1 cm2​） | CsOH (3 mol L-1) | 866 (jco) | 3 (Ecell) | 98% | 17 | 36% | 0.269 | [16] |

a CoPc = cobalt phthalocyanine; NCB = N-doped carbon black; NiPc-OMe-MDE = methoxy-substituted NiPc molecularly dispersed electrocatalysts (MDEs); PE = polyethylene; APC = atom-pair catalysts; NPCA = N, P-co-doped carbon aerogels; g-C3N4/CNT = graphitic carbon nitride on carbon nanotube; CoTAP-cov = Covalent ligation of Co tetrakis-(4-aminophenyl) porphyrin on CNTs; DASC = diatomic site catalyst; DNG-SAFe = single-atom Fe–N4 sites; AgNPS/GDE = Ag Nanoparticles/Gas diffusion electrode; SCCM = Standard Cubic Centimetre per Minute.

b Single-pass conversion rate (R) of CO2 was acquired using based on the data reported in the literatures. At first, the molar conversion rate CO2 to CO (i.e., CO evolution rate vm, in mol s-1 for calculation or mmol mim-1 for the Table) can be calculated in accordance with Equations 1 and 2:

FE = (mnF)/(It) = (vmnF)/I                                        (1)

vm = (FEI)/(nF)                                             (2)

where FE is the Faraday efficiency, m is the molar number (mol) of CO generated, n is the number of electrons exchanged (2 mol-1 for the conversion of CO2 to CO), F is Faraday’s constant (F = 96485 C mol-1), I is the current (Ampere, A), and t is the time (s).

Using vm, the volume conversion rate of CO2 (V’CO2, m3 s-1) in the electrolytic cell is obtained in accordance with Equations 3 and 4

pV’CO2 = vmRT                                             (3)

V’CO2 = (vmRT)/p                                            (4)

where p is the atmospheric pressure in Pa, R the ideal gas constant of 8.314 J mol-1 K-1, and T the temperature in K.

Thus, the single pass conversion of CO2 (R) is obtained in accordance with Equation 5

R = V’CO2/VCO2                                              (5)

where VCO2 is the flow rate (m3 s-1) of CO2 feed to the electrolytic cell.

Supplementary Table 2 | A summary of various advanced photochemical systems for the conversion of CO2 to CO

| Photocatalysta | Reaction medium | Light source | CO evolution rate (mmol/min)b | Ref |
| --- | --- | --- | --- | --- |
| (CoZn) (0.025 μM) | [Ru(phen)3] (PF6)2, TEOA in H2O/CH3CN | LED light (450 nm, 100 mW·cm-2) | 1.35×10-5 | [17]17 |
| NC@NiCo2O4 (1 mg) | [Ru(bpyp))3]Cl2·6H2O, TEOA in H2O/CH3CN | 300W Xe lamp (λ> 420 nm) | 4.37×10-4 | [18]18 |
| CTU/TiO2 (0.1 g) | H2O | 300 W Xe lamp (λ> 300 nm) | 5.22×10-5 | [19]19 |
| Ni(TPA/TEG) (1mg) | [Ru(bpy) 3]Cl2·6H2O, TEOA in H2O / CH3CN | 300W Xe lamp (λ> 420 nm) | 4.43×10-4 | [20]20 |
| TRP (15 mg) | NaHCO3 (1.36 g) H2SO4 (2 M, 10 mL) | 300 W Xenon lamp (λ> 400 nm) | 1.22×10-4 | [21]21 |
| Co3O4 (10 mg) | Ru(bpy)3]Cl2·6H2O, TEOA in H2O/CH3CN | 300W Xe lamp (λ> 420 nm) | 3.34×10-4 | [22]22 |
| [Co2(OH)L](ClO4)3 (0.025 μM) | [Ru(phen) 3](PF6)2, TEOA in H2O/CH3CN | LED light (450 nm) | 3.52×10-5 | [23]23 |
| BCN (50 mg) | H2O / CH3CN, TEOA, CoCl2, 2, 2-bipyridine | 300W Xe lamp (λ> 420 nm) | 7.92×10-5 | [24]24 |
| HR-CN (30 mg) | Co(bpy) 3Cl2, TEOA | visible light (λ>420 nm) | 1.48×10-4 | [25]25 |
| IrP/TiO2/ReP (10 mg) | BIH In DMF/H2O | 450 W Xe lamp (λ> 500 nm) | 6.96×10-5 | [26]26 |
| CsPbBr3/GO (4 mg) | Ethyl acetate | 100 W Xe lamp (150 mW cm-2) | 1.58×10-6 | [27]27 |
| CsPbBr3 (4 mg) | Ethyl acetate/H2O | 300 W Xe lamp (100 mW cm-2) | 2.87×10-7 | [28]28 |
| Coqpy@mpg-C3N4 (6 mg) | BIH and PhOH | Visible light (λ > 400 nm) | 7.98×10-7 | [29]29 |
| Cu/crystalline g-C3N4 (25 mg) | H2O | 300W Xe lamp (λ> 420 nm) | 5.14×10-5 | [30]30 |
| Ni-PCD@TD-CO (1 mg) | [Ru(bpy)3]Cl2, TEOA in H2O/CH3CN | visible light (λ>420 nm) | 7.98×10-6 | [31]31 |
| 2D-Ni2TCPE (1 mg) | [Ru(bpy)3]Cl2·6H2O, TEOA in H2O/CH3CN | Visible light (λ>420 nm) | 6.96×10-5 | [32]32 |
| CN/Bi9O7.5S6 (1 mg) | H2O | 300W Xe lamp (λ> 420 nm) | 6.18×10-7 | [33]33 |
| CsPbBr3/CTF-1-Ni (1 mg) | Ethyl acetate | 300-W Xe lamp (λ>400 nm) | 1.44×10-6 | [34]34 |
| CdSQD/NC (1 mg) | Co(bpy)32+ MeCN/H2O | 300-W Xe lamp (λ> 420 nm) | 8.7×10-5 | [35]35 |
| CDT-DCDA-490 (1 mg) | NaHCO3 solution/ cyclohexene | 300-W Xe lamp (λ> 420 nm) | 7.08×10-7 | [36]36 |
| BUT-110-50%-Co (1 mg) | H2O/TEOA | 300-W Xe lamp 320-780 nm | 1.07×10-7 | [37]37 |
| Au-NC@UiO-68-NHC (1 mg) | MeCN/CH3OH | 300-W Xe lamp | 2.57×10-6 | [38]38 |

a CTU = Cu (II) tetra(4-carboxylphenyl) porphyrin (CuTCPP) into UiO-66 MOF; TPA/TEG = terephthalic acid/triethylene glycol; TPR = treated rape pollen; L1 = N[(CH2)2NHCH2 (m-C6H4CH2NH(CH2) 2] 3); BCN = boron carbon nitride; HR-CN = g-C3N4 with a helical rodlike morphology; Coqpy@mpg = Co−quaterpyridine molecular complex to semiconductive mesoporous graphitic; Ni-PCD@TD-COF = a covalent organic framework hosting metalloporphyrin-based carbon dots; TCPE = 1,1,2,2-tetra (4-carboxylphenyl)ethylene); CTF = two-dimensional (2D) covalent triazine frameworks; CdSQD/NC = N-doped carbon (NC) supported CdS quantum dots; CDT-DCDA = phenyl-group-linked tri-s-triazine polymer semiconductor; BUT-110 = Zr6O4(OH)10(NDIDB)1.5(DCPP)1.5(H2O)6; NHC = N-heterocyclic carbenes; TEMOA = Triethanolamine; bpy = 2,2-bipyridine; BIH = a sacrificial electron donor; DMF = N,N-Dimethylformamide; LED = Light-emitting diode.

b CO evolution rates were available in the literatures.

Supplementary Fig. 1 | Time-dependent UV-vis absorption spectra of the brown solution. The solution for UV-vis absorption spectroscopy measurements was prepared by mixing copper powder (0.01 g) and NMI (1 mL) in a sealed quartz cuvette with an optical path of 1 mm. After shaking two minutes, the cuvette was placed in the UV-vis absorption spectrometer and the spectra were acquired at the time of 5, 10, 20, 30, 40, 50, 60, 80, and 100 minutes.

Supplementary Fig. 2 | (a) A air-assisted oxidization experiment was designed to identify the presence of soluble charge transfer complex [CuI∙∙∙NMI•‒]. If there were copper species in the brown solution, a colour change would be observed because of the transformation of Cu+ to Cu2+. So, the light brown supernatant was extract through a 0.22 μm pore sized syringe filter (to exclude the interference of Cu0 particles) and transferred to an open colorimeter tube. As expected, with the exposure of the solution to air, a colour change from brown to blue, a characteristic colour for Cu2+ ions, did occur. Ten hours later, the solution was grown by fine blue crystallites. (b) A magnified image clearly shows blue crystallites in the solution. The inset shows the photography of the crystallites taken with an optical microscope. (c) X-ray diffraction (XRD) patterns of the blue crystallites (black line) and the complex Cu(NMI)3CO3 reported in the reference39 (blue line). (d) Structure of the complex Cu(NMI)3CO3.

According to the results, it can be concluded that: (1) copper powder indeed dissolve in NMI and form soluble [CuI∙∙∙NMI•‒]; (2) [CuI∙∙∙NMI•‒] can capture ambient CO2 and thereby transform to Cu(NMI)3CO3 complex with the aid of the oxygen in air through the following equation (Eq. 6).

[CuI∙∙∙NMI•‒] + 2NMI + CO2 + 1/2O2 → Cu(NMI)3CO3        (6)

Supplementary Fig. 3 | Stability studies of the [CuI∙∙∙NMI•‒] system. (a) Photograph of freshly prepared [CuI∙∙∙NMI•‒] solution. (b) Photograph of [CuI∙∙∙NMI•‒] solution stored over one year. (c) UV-vis absorption spectra of freshly prepared [CuI∙∙∙NMI•‒] and [CuI∙∙∙NMI•‒] stored over one year. As seen, the two systems show almost identical colour and spectra, which demonstrates that the solution can keep unchanged in the sealed reagent bottle.

Supplementary Fig. 4 | The time-off-flight mass spectrum of the [CuI∙∙∙NMI•‒] solution. m/z denotes mass to charge ratio. Molecular ion or the fragments of NMI (m/z = 83.06), Cu(NMI) (m/z = 144.98), Cu(NMI)2 (m/z = 227.04), and Cu(NMI)3 (m/z = 309.07) are identified. Their structural formula are shown in Supplementary Table 3 below.

Supplementary Table 3 | Structural formula for molecular ion or the fragments identified in Supplementary Fig. 4.

|  | Structural formula | MS(ESI) m/z: (found) | Formula Weight (calculated) |
| --- | --- | --- | --- |
| I |  | 83.06 | 82.05 |
| I-a |  | 144.98 | 144.98 |
| II-a |  | 227.04 | 227.04 |
| III-a |  | 309.07 | 309.09 |

Supplementary Fig. 5 | Schematic illustration of the setup for studying the interactions between CO2 and [CuI∙∙∙NMI•‒] solution with time‒dependent in-situ attenuated total reflection infrared (ATR-IR) absorption spectrometer. The [CuI∙∙∙NMI•‒] solution prepared by 10 mL of NMI and 0.05 g of copper powder was added to the flask, followed by the injection of 5 mL of CO2 (purity 99.999%). ATR–IR spectra of the system were acquired in real time, as shown in Supplementary Fig. 6. For a comparison, the interaction of CO2 with individual NMI was also studied by the ATR–IR absorption spectrometer.

Supplementary Fig. 6 | (a, c) ATR-IR spectra of the [CuI∙∙∙NMI•‒] system and individual NMI upon the interaction with CO2. (b, d) Absorbances at the wavenumber of 2336 cm-1 for [CuI∙∙∙NMI•‒] and individual NMI upon the interaction with CO2.

For the [CuI∙∙∙NMI•‒] system (a), when CO2 was injected into the flask at the 500th second in the experiment, a band at 2336 cm-1 attributed to the asymmetric stretching vibration of CO2 is developed. The intensity of the 2336 cm-1 band is rapidly increased and approaches a platform (absorption saturation) within 370 seconds (c). As a Lewis base, individual NMI is also effective in absorbing Lewis acidic CO2 molecules. Consequently, when CO2 is injected into the flask at the 280th second in the experiment, a characteristic IR absorption band of CO2 at 2336 cm-1 yields (b). This band takes ca. 490 seconds to approach a platform (d). As seen, the [CuI∙∙∙NMI•‒] system exhibits a relatively short saturation absorption time towards CO2 than the single NMI system. This phenomenon can be interpreted by the fact that the anionic radical NMI•‒ in the [CuI∙∙∙NMI•‒] system is a potent nucleophile to attract Lewis acidic CO2 molecule.

Supplementary Fig. 7 | CO2 absorption capacities for the [CuI∙∙∙NMI•‒] system (red circle) and single NMI system (black circle). The experiments for quantitatively determining CO2 absorption capacities were conducted in parallel with time‒dependent in-situ ATR-IR measurements, as demonstrated in Supplementary Figs. 5, 6.

In details, 5 mL of CO2 was injected into the flask filled by 10 mL NMI or 10 mL [CuI∙∙∙NMI•‒] solution. The solution was stirred to promote the absorption of CO2. After that, CO2 remained in the headspace of the flask was analysed every 2.5 min interval using gas chromatography (GC). 100 microlitres of the gas phase was injected into the GC column (5A molecular sieve) using a gastight syringe. The gas concentration was averaged over five measurements. The gas chromatograph was equipped with a flame ionization detector (FID) and a methanizer. The methanation reactor can convert CO and CO2 to CH4 for detection. The results show that the [CuI∙∙∙NMI•‒] solution shows an absorption capacity of ca. 5 mmol L-1, almost two folds that of single NMI system.

Supplementary Fig. 8 | The time-off-flight mass spectrum of the [CuI∙∙∙NMI•‒] solution upon the interaction with CO2. New fragments were identified in the spectrum. They can be assigned to Cu(NMI)2CO2 (m/z = 270.02), Cu(NMI)2(CO2)2 (m/z = 315.97), Cu(NMI)3CO2 (m/z = 352.07), and Cu(NMI)3(CO2)2 (m/z = 396.06). Structural formula of these compounds are shown in Supplementary Table 4 below.

Supplementary Table 4 | Structural formular for the compounds identified in Supplementary Fig. 8.

|  | Structural formula | MS(ESI) m/z: （found） | Formula Weight (calculated) |
| --- | --- | --- | --- |
| II-b |  | 270.02 | 270.02 |
| II-c |  | 315.97 | 315.01 |
| III-b |  | 352.07 | 352.07 |
| III-c |  | 396.06 | 396.06 |

Supplementary Fig. 9 | EPR spectrum for the [CuI∙∙∙NMI•‒] solution saturated by CO2.

Supplementary Fig. 10 | [CuI∙∙∙NMI•‒] as the mediator for electrocatalytic CO2R. (a) Experimental set for studying electrocatalytic reduction of CO2. The cathode compartment was filled by [CuI∙∙∙NMI•‒] solution (acting as both mediator and catholyte). CO2 was continuously purged through the cathode compartment at 20 standard cubic centimetre per minute (sccm). The anode compartment was filled by 0.1 mol L-1 KOH solution (anolyte). Cathode and anode compartments were separated by proton exchange membrane (PEM). Glassy carbon, ruthenium–coated titanium mesh, and Ag/AgCl were used as the working electrode (WE), counter electrode (CE), and reference electrode (RE), respectively. After the CO2 passed through the cathode, it was allowed to directly enter the gas sampling loop of the GC for online gaseous analysis. (b) The schematic shows the details of the electrolytic cell. (c) GC measurements showed that CO (retention time ca. 0.7 min) could be detected when a cell voltage of 1.4 V was applied. The fraction of CO in the outlet gas is positively dependent on the cell voltage. (d) Relationships of CO production rate and single pass conversion with the applied cell voltage.

Supplementary Table 5 | Selected standard potentials of CO2R (V vs. SHE) at 1.0 atm and 25 oC40,41.

Supplementary Fig. 11 | Representative GC signals of CO2 feed (green line) and the converted CO (red line) in the experiments. For the aim of validating the accuracy of the GC signals, standard CO2 and CO samples were tested and the GC curves (black lines) were recorded for comparisons. Calibration of the gas chromatograph was done using calibration gases with 2000 to 500000 parts per million (ppm) CO or CO2 balanced in nitrogen. The product concentrations were averaged over five measurements.

Supplementary Fig. 12 | Analysis of the gaseous product using gas chromatograph equipped with a thermal conductivity detector (TCD). Black and red lines correspond to the GC curves of standard H2 sample and the gaseous product, respectively. The comparison reveals that a small amount of H2 was generated in the process of CO2R. This is because C2 hydrogen (See the inset) in the imidazole ring of NMI is weakly acidic (pka =6.88), which can react with Zn to yield H2.

Calibration of the gas chromatograph was done using calibration gases with 1%, 10%, and 50% hydrogen balanced in nitrogen and 100% hydrogen. The product concentrations were averaged over five measurements.

Supplementary Fig. 13 | In-situ ATR−IR absorption spectroscopy study of the CO2R using Zn as the reducing agent and [CuI∙∙∙NMI•‒] solution as the mediator. The experiment was conducted in the setup shown in Supplementary Fig. 5.

Supplementary Fig. 14 | Isotope tracer study using 13CO2 as the feedstock. In the mass chromatograms of the gaseous product, the m/z value of 29 is assigned to 13CO (m/z = 29). The characteristic mass fragment 13C (m/z = 13) from 13CO was also observed. The m/z value of 32 was assigned to O2 molecule. The m/z value of 28 is assigned to N2 (carrier gas: m/z = 28), rather than the 12CO (m/z = 28) molecule. This presumption is supported by the fact that the found m/z value of 14 is consistent with the fragment of N and the mass spectroscopy signal of 12C (m/z = 12) was not observed.

Supplementary Fig. 15 | Representative photograph of the reaction system. This system had been used for the conversion of CO2 to CO three times (namely thee cycles). After that, it is clearly seen that grey Zn was consumed and what left in the reactor were wite colloid, red solid, and transparent liquid.

Supplementary Fig. 16 | 1H nuclear magnetic resonance (1H-NMR) spectroscopy studies of pure NMI (a) and the transparent supernatant shown in Supplementary Fig. 15 (b). As seen, the 1H–NMR spectrum of the supernatant is identical to that of pure NMI. That is, possible liquid products such as formate and oxalate were not formed, which demonstrate that CO2R mediated by [CuI∙∙∙NMI•‒] exhibits high selectivity.

Supplementary Fig. 17 | 13C–NMR spectroscopy studies of pure NMI (a) and the transparent supernatant shown in Supplementary Fig. 15 (b). As seen, the 13C–NMR spectrum of the supernatant is also identical to that pure NMI, consistent with the 1H–NMR result shown in Supplementary Fig. 16.

Supplementary Fig. 18 | Scanning electron microscopy (SEM) image of the white colloid.

Supplementary Fig. 19 | X−ray photoelectron spectroscopy (XPS) characterizations of the white colloid. (a) The survey spectrum demonstrates that the colloid is a non−cupreous compound, as learn from the absence of Cu 2p peak at ca. 950 eV. The compound consists of Zn, O, N, and C elements. (b-d) High-resolution XPS spectra of (b) C1s, (c) O 1s, and (d) N 1s. The high-resolution XPS spectra suggests that Zn2+ ion, CO32- ion, and NMI are the constitutional units of the white colloid.

Supplementary Fig. 20 | (a) Powder X−ray diffraction (PXRD) pattern of the white colloid (Top) and the XRD pattern given in Ref. S39 (Down). (b) Structure of the complex Zn(NMI)2CO3.

Supplementary Fig. 21 | Relationship between the pressure of CO2 inputted into the reactor and the pressure of CO generated. It is always observed that the pressure of CO is approximately half that of CO2 feed.

Supplementary Fig. 22 | PXRD patterns of the copper powder used for CO2R reaction (black line) and the red solid shown in Supplementary Fig. 15 (red line). PXRD results demonstrate that copper maintains the zero valent state and is non-consumable in the process of CO2R reaction.

Supplementary Fig. 23 | (a) Linear sweep voltammetry (LSV) of Zn(CO3)(NMI)2 dissolved in 0.1 mol L-1 KOH solution. Lead cathode with a high overpotential for hydrogen evolution reaction was used as the work electrode. Platinum wire and Ag/AgCl were used as the counter electrode and reference electrode, respectively. The LSV was scanned at a rate of 5 mV s-1 at room temperature. In the violet region, the cathode current is associated with the reduction of oxidized layer (PbO2) of the lead electrode. In the green region, the cathode current is attributed to the reduction of Zn2+ ions. It can begin to observe a layer of metal plating on the surface of the lead electrode. The cathode current reached 0.5 kA m-2 (or 50 mA cm-2 at the potential of -0.45 V vs RHE). In the orange region, gas bubbles were formed on the lead electrode and accordingly, the cathode current can be associated with the hydrogen evolution reaction. (b) XRD pattern of the electrochemically reduced Zn. The asterisks (⁕) denote the signals from the lead electrode. (c) XRD pattern for standard Zn. (d) XRD pattern for standard lead.

Supplementary Fig. 24 | (a) 1H-NMR and (b) 13C-NMR spectroscopy studies of NMI released to the electrolyte after the electrolysis. Prior to the measurements, NMI was extracted from the electrolyte (0.1 mol L-1 KOH solution) by ethyl acetate. Ethyl acetate in the extractive liquid was then allowed to volatilize. The remained liquid was collected for the NMR spectroscopy characterizations. The recorded 1H–NMR spectrum (a) is identical to those shown in Supplementary Fig. 16. The recorded 13C–NMR spectrum (b) is identical to those shown in Supplementary Fig. 17. Both the results demonstrate that NMI is regenerative through the electrolysis of the complex Zn(CO3)(NMI)2.

Supplementary Fig. 25 | Flow reduction of CO2 to CO with the customized bubbling reactor. (a) Schematic of the bubbling reactor. The reactor was constructed of 10 gas washing bottles connected in series. Each bottle (volume 10 mL) was placed by 2 mL NMI, 0.1 g Cu, and 1 g Zn. (b) Photograph of the bubbling reactor. (c) GC signals at various CO2 flow rates (5~100 SCCM). (d) Dependence of CO fraction in the off–gas on CO2 flow rate. (e) Continuous production of nearly pure CO at 10 SCCM CO2 and ca. 86% CO at 30 SCCM CO2.

Supplemental References

1	Ren, S. et al. Molecular electrocatalysts can mediate fast, selective CO2 reduction in a flow cell. Science 365, 367-369 (2019).

2	Zheng, T. et al. Large-scale and highly selective CO2 electrocatalytic reduction on nickel single-atom catalyst. Joule 3, 265-278 (2019).

3	Gu, J., Hsu, C.-S., Bai, L., Chen, H. M. & Hu, X. Atomically dispersed Fe3+ sites catalyze efficient CO2 electroreduction to CO. Science 364, 1091-1094 (2019).

4	Zhang, X. et al. Molecular engineering of dispersed nickel phthalocyanines on carbon nanotubes for selective CO2 reduction. Nat. Energy 5, 684-692 (2020).

5	Li, S. et al. Low‐Valence Znδ+(0< δ< 2) Single‐Atom Material as Highly Efficient Electrocatalyst for CO2 Reduction. Angew. Chem. Int. Ed. 60, 22826-22832 (2021).

6	Ding, T. et al. Atomically precise dinuclear site active toward electrocatalytic CO2 reduction. J. Am. Chem. Soc. 143, 11317-11324 (2021).

7	Chen, Z. et al. Amination strategy to boost the CO2 electroreduction current density of M–N/C single-atom catalysts to the industrial application level. Energy Environ. Sci. 14, 2349-2356 (2021).

8	Li, J. et al. Efficient electrocatalytic CO2 reduction on a three-phase interface. Nat. Catal. 1, 592-600 (2018).

9	Jiao, J. et al. Copper atom-pair catalyst anchored on alloy nanowires for selective and efficient electrochemical reduction of CO2. Nat. chem. 11, 222-228 (2019).

10	Chen, C. et al. Boosting CO2 electroreduction on N, P‐co‐doped carbon aerogels. Angew. Chem. Int. Ed. 132, 11216-11222 (2020).

11	Feng, J. et al. A Mn-N3 single-atom catalyst embedded in graphitic carbon nitride for efficient CO2 electroreduction. Nat. Commun. 11, 1-8 (2020).

12	Gu, S., Marianov, A. N. & Jiang, Y. Covalent grafting of cobalt aminoporphyrin-based electrocatalyst onto carbon nanotubes for excellent activity in CO2 reduction. Appl. Catal. B: Environ. 300, 120750 (2022).

13	Zhang, Y., Jiao, L., Yang, W., Xie, C. & Jiang, H. L. Rational Fabrication of Low‐Coordinate Single‐Atom Ni Electrocatalysts by MOFs for Highly Selective CO2 Reduction. Angew. Chem. Int. Ed. 60, 7607-7611 (2021).

14	Zeng, Z. et al. Orbital coupling of hetero-diatomic nickel-iron site for bifunctional electrocatalysis of CO2 reduction and oxygen evolution. Nat. Commun. 12, 1-11 (2021).

15	Ni, W. et al. Electroreduction of carbon dioxide driven by the intrinsic defects in the carbon plane of a single Fe–N4 site. Adv. Mater. 33, 2003238 (2021).

16	Bhargava, S. S. et al. System design rules for intensifying the electrochemical reduction of CO2 to CO on Ag nanoparticles. ChemElectroChem 7, 2001-2011 (2020).

17	Ouyang, T. et al. Dinuclear Metal Synergistic Catalysis Boosts Photochemical CO2‐to‐CO Conversion. Angew. Chem. Int. Ed. 57, 16480-16485 (2018).

18	Wang, S., Guan, B. Y. & Lou, X. W. D. Rationally designed hierarchical N-doped carbon@ NiCo2O4 double-shelled nanoboxes for enhanced visible light CO2 reduction. Energy Environ. Sci. 11, 306-310 (2018).

19	Wang, L. et al. In-situ incorporation of Copper (II) porphyrin functionalized zirconium MOF and TiO2 for efficient photocatalytic CO2 reduction. Sci. Bull. 64, 926-933 (2019).

20	Niu, K. et al. A spongy nickel-organic CO2 reduction photocatalyst for nearly 100% selective CO production. Sci. Adv. 3, e1700921 (2017).

21	Jiang, Z. et al. Nature-based catalyst for visible-light-driven photocatalytic CO2 reduction. Energy Environ. Sci. 11, 2382-2389 (2018).

22	Gao, C. et al. Co3O4 Hexagonal Platelets with Controllable Facets Enabling Highly Efficient Visible‐Light Photocatalytic Reduction of CO2. Adv. Mater. 28, 6485-6490 (2016).

23	Ouyang, T., Huang, H. H., Wang, J. W., Zhong, D. C. & Lu, T. B. A dinuclear cobalt cryptate as a homogeneous photocatalyst for highly selective and efficient visible‐light driven CO2 reduction to CO in CH3CN/H2O solution. Angew. Chem. Int. Ed. 129, 756-761 (2017).

24	Huang, C. et al. Carbon-doped BN nanosheets for metal-free photoredox catalysis. Nat. Commun. 6, 1-7 (2015).

25	Zheng, Y., Lin, L., Ye, X., Guo, F. & Wang, X. Helical graphitic carbon nitrides with photocatalytic and optical activities. Angew. Chem. Int. Ed. 126, 12120-12124 (2014).

26	Kim, P. S. et al. Organometallic Iridium (III) Complex Sensitized Ternary Hybrid Photocatalyst for CO2 to CO Conversion. Chem. Eur. J. 25, 13609-13623 (2019).

27	Xu, Y.-F. et al. A CsPbBr3 perovskite quantum dot/graphene oxide composite for photocatalytic CO2 reduction. J. Am. Chem. Soc. 139, 5660-5663 (2017).

28	Hou, J. et al. Inorganic colloidal perovskite quantum dots for robust solar CO2 reduction. Chem. Eur. J. 23, 9481-9485 (2017).

29	Ma, B. et al. Efficient visible-light-driven CO2 reduction by a cobalt molecular catalyst covalently linked to mesoporous carbon nitride. J. Am. Chem. Soc. 142, 6188-6195 (2020).

30	Li, Y., Li, B., Zhang, D., Cheng, L. & Xiang, Q. Crystalline carbon nitride supported copper single atoms for photocatalytic CO2 reduction with nearly 100% CO selectivity. ACS nano 14, 10552-10561 (2020).

31	Zhong, H. et al. Covalent organic framework hosting metalloporphyrin‐based carbon dots for visible‐light‐driven selective CO2 reduction. Adv. Funct. Mater. 30, 2002654 (2020).

32	Zheng, H. L. et al. Photochemical In Situ Exfoliation of Metal–Organic Frameworks for Enhanced Visible‐Light‐Driven CO2 Reduction. Angew. Chem. Int. Ed. 59, 23588-23592 (2020).

33	Li, J. et al. Van der Waals heterojunction for selective visible-light-driven photocatalytic CO2 reduction. Appl. Catal. B: Environ. 284, 119733 (2021).

34	Wang, Q. et al. Coupling CsPbBr3 Quantum Dots with Covalent Triazine Frameworks for Visible‐Light‐Driven CO2 Reduction. ChemSusChem 14, 1131-1139 (2021).

35	Wang, F. et al. Ordered macroporous carbonous frameworks implanted with CdS quantum dots for efficient photocatalytic CO2 reduction. Adv. Mater. 33, 2102690 (2021).

36	Zhen, W., Sun, J., Ning, X., Shi, X. & Xue, C. Polymeric carbon nitride with internal np homojunctions for efficient photocatalytic CO2 reduction coupled with cyclohexene oxidation. Applied Catalysis B: Environmental 298, 120568 (2021).

37	Kong, X. J. et al. In Situ Porphyrin Substitution in a Zr (IV)‐MOF for Stability Enhancement and Photocatalytic CO2 Reduction. Small, 2005357 (2021).

38	Jiang, Y. et al. N‐Heterocyclic Carbene‐Stabilized Gold Nanoclusters in a Metal‐Organic Framework for Photocatalytic CO2 Reduction. Angew. Chem. Int. Ed. (2021).

39	Vaid, T. P., Kelley, S. P. & Rogers, R. D. Metal carbonate complexes formed through the capture of ambient O2 and CO2 by elemental metals in 1-methylimidazole: molecular Cu(CO3)(MeIm)3 and polymeric M(CO3)(MeIm)2·2H2O (M= Co, Zn). Dalton T. 46, 8920-8923 (2017).

40	Li, K., An, X., Park, K. H., Khraisheh, M. & Tang, J. A critical review of CO2 photoconversion: Catalysts and reactors. Catal. Today 224, 3-12 (2014).

41	Kubacka, A., Fernandez-Garcia, M. & Colon, G. Advanced nanoarchitectures for solar photocatalytic applications. Chem. Rev. 112, 1555-1614 (2012).