Supplementary Information

The adsorption amount qe (mg·g−1) was calculated using the following equation (Eq. (1)):

qe=(Ci-Ce)Vm                                                       (1)

where Ci and Ce represent the concentrations (mg·L−1) at the equilibrium and initial time, respectively, V is the solution volume (mL), and m is the mass of the adsorbent (g).

1 Adsorption models

1.1 Kinetic models

The fluoride removal kinetics in this study was investigated using pseudo-first-order kinetics, pseudo-second-order kinetics, and Weber-Morris models. The kinetic constant K was calculated using the following equations (2-4):

lgqe-qt=lgqe-K1×t2.303                          (2)

tqt=1K2-qe2+tqe                                                      (3)

qt=Kit0.5+C                                                             (4)

where qe and qt denote the adsorbed amount of fluoride (mg·g−1) at equilibrium and at time t, respectively.

1.2 Adsorption isotherms

The Langmuir, Freundlich, and Dubinin-Radushkevich (DR) models were used to investigate the adsorption isotherms in this study. The Langmuir and Freundlich constants (KL and KF) were calculated using the following equation (5) and equation (6), respectively:

Ceqe=1qmKL+Ceqm                                                        (5)

lgqe=lgKF+1nlgCe                                                   (6)

where qe is the adsorbed amount of fluoride on the Al/Y-CSBC at the equilibrium concentration of adsorbate in solution (mg·g−1), Ce denotes the concentration of fluoride at equilibrium (mg·L−1), and n is the Freundlich exponent related to the intensity of adsorption.

The Dubinin-Radushkevich (DR) models were fitted using the following equations (7-9):

lnqe=lnqm-βε2                                                       (7)

ε=RTln1+1Ce                                                        (8)

E=(2β)-12                                                                       (9)

where qe is the adsorbed amount of fluoride on the Al/Y-CSBC at the equilibrium concentration of adsorbate in solution (mol·g−1), Ce denotes the concentration of fluoride at equilibrium (mol·L−1), β is the parameters related to adsorption energy, ε is the adsorption potential, R (8.314 J·(mol⋅K) −1) is the gas constant, T (K) is the absolute temperature, and E (kJ·mol−1) is the free energy of adsorption.

The thermodynamic parameters adsorption enthalpy (△H), adsorption free energy (△G), and adsorption entropy (△S) were calculated using the thermodynamic equations (10-12) (Cao et al. 2022) by investigating the adsorption isotherms at three temperatures of 298, 308, and 318 K.

∆G=∆S-T∆H=-RTlnKT                             (10)

lnKT=∆SR-∆HRT                                                     (11)

KT=(1000·K·molecular weight of adsorbate)·adsorbate°γ           (12)

In which KT (dimensionless) is the apparent adsorption equilibrium constant of Van’t Hoff equation; K (L·mg−1) is the adsorption equilibrium constant, γ (dimensionless) is the activity coefficient, and [adsorbate]◦ (mol·L−1) is deemed as 1.

2 Adsorption mechanism

Under alkaline conditions, a large amount of surface hydroxylation occurs, resulting in a negative charge (14) and electrostatic repulsion with negative ions. On the contrary, under acidic conditions, they become protonated and positively charged (15) and are able to attract fluoride ions (16). The adsorption process is also affected by ion exchange (17) and surface complexation (18).

≡M++OH-→ ≡M-OH                                                   (13)

≡M-OH+OH-→ ≡M-O2-+H2O                              (14)≡M-OH+H+→≡M-OH2+

≡M-OH+H+→ ≡M-OH2+                                            (15)

≡MOH2++F-→ ≡M-F+H2O                                        (16)

≡M-OH+F-→ ≡M-F+OH-                                     (17)

≡M-OH+xF-→ ≡M-Fx+OH-                                 (18)

References

Cao X, Meng Z, Song E, Sun X, Hu X, Wenbin Li, Liu Z, Gao S, Song B (2022) Co-adsorption capabilities and mechanisms of bentonite enhanced sludge biochar for de-risking norfloxacin and Cu2+ contaminated water. Chemosphere 299:134414. https://doi.org/10.1016/j.chemosphere.2022.134414